## Slide 1: The Measurement of Wool Colour
Produced for the CRC for Premium Quality Wool undergraduate program by;
Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
Notes: This module examines how wool colour is measured, the sources of yellowness in wool, and importantly how discolouration of clean wool can affect the final product, particularly during dyeing.
Produced for the CRC for Premium Quality Wool undergraduate program by Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.

## Slide 2: Subjective vs Objective Colour
Subjective and greasy
  H0 no colour
  H1, 2
  H3 unscourable
Objective and scoured
  66% H3 to H0
  95% H1 to H0
Andrew Lindsay
Notes: Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
Research has shown that there is a particularly poor relationship between the greasy colour and scoured colour of wool.
Measurements for subjective appraisal are: H0 (no colour), H1 & H2 (light colour), H3 (unscourable colour). Wool with H2 or H3 colour are usually heavily discounted.
Research has found that 66% of lots given H3 subjectively should have been H0. 95% lots given H1 should have been given H0. There was a large overlap evident in these results.
These results are particularly important for growers with concerns over yellowness of their wool.
Objective wool colour measurement was introduced because of the lack of a reliable system when assessing wool subjectively.
The objective measurement of colour concentrates on the measurement of the colour of greasy wool AFTER it is scoured.

## Slide 3: Instrument
Colorimeter or Spectrophotometer
  Light Source (Illuminant C)
  Sample Holder
  (core sample)
%Reflectance (%R)
  Red (X)
  Green (Y)
  Blue (Z)
Andrew Lindsay
Notes: <number>
<footer>
Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
A Colorimeter or Spectrophotometer is used to obtain the Tristimulus values X, Y and Z.
A Colorimeter is a simpler form of a spectrophotometer that uses filters to simulate the response to light at various wavelengths, rather than continuously measuring over the whole visible spectrum. The main reason for the popularity of Colorimeters is cost, although in the last number of years spectrophotometers are in the reach of most laboratories.
In either case Illuminant C is used as the incident light, and a 2° observer angle is specified.
In most colour measurement situations, it is recommended that an integrating sphere is used to measure the reflectance. This device allows for any differences in the orientation and texture of the samples. However, in the case of the measurement of wool samples anomalous results have been returned in trials with integrating spheres, therefore their use is not recommended.
Both these instruments automatically calculate values for X, Y and Z tristimulus values.

## Slide 4: Standards
IWTO DTM 56:
  Method for the Measurement of the Color of Raw Wool.
  replaces pre-existing Australian and NZ standards
  covers differences in both test methods
Andrew Lindsay
Notes: Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
Previously, the standards used in Australia and NZ differed in the preparation of the sample for measurement.
The samples were scoured in Australia, while they are cleaned in a Waring blender in poly-ethylene glycol in NZ. The Australian standard used a Shirley Analyser to blend the fibres of the core samples and remove VM, while compressed air is used in NZ since there is not such a problem with VM in that country. The drying conditions for the samples are also quite different.
A Draft Test Method is now under consideration which overcomes these differences and is meant for world-wide usage by IWTO.

## Slide 5: Range of Wool Colour
Y- Z values
- 2 (very white) + 12 (very yellow)
Australian Merino fleece wool
  + 1 + 4
Y values
~ 50 (dull) 70 (bright)
Andrew Lindsay
Notes: <number>
<footer>
Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
In practice, Y-Z values range from -2 to 12.
New Zealand wools are more variable in colour as well as being of higher yellowness. It is difficult to find yellowness values exceeding +6 in Australia.
Y is not certified in Australia as yet. Efforts are being made by AWTA to get the use of this value certified for trading.
To the common observer a difference of >4.0 units in Y, and >2.5 units in Y-Z is noticeable.

## Slide 6: Colour in Greasy Wool: Causes
Breeding
Environment & Climate
  Topography, Light, Moisture, Humidity
Canary Yellow
  high alkaline suint, moisture, warmth
Bacterial Stain
Effect of fibre diameter (micron)
Andrew Lindsay
Notes: <number>
<footer>
Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
Several factors can influence the colour, in particular average yellowness, of greasy wool. These are listed above. The cases which cause most difficulty are Canary Yellow and Bacterial Stain which can cause unscourable colour.
Generally speaking, as the fibre diameter increases, the scoured colour of the wool becomes yellower, and the wool becomes less bright. The difference is more marked over a large range of fibre diameter.
This result reflects the breed of the animals, and the environment in which the wool is grown.

## Slide 7: Effect of Yellowness on Dyeability
Wavelength (nm)
Reflectance (%)
0
20
40
60
80
100
380
420
460
500
540
580
620
660
700
740
Wool (Y-Z = 0)
Wool (Y-Z = 10)
Pastel Pink tile
Andrew Lindsay
Notes: <number>
<footer>
Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
When dyeing, the reflectance of the final product at any wavelength will NEVER exceed the reflectance of the raw material at that wavelength.
Therefore wool of excessive yellowness cannot be dyed to pastel shades. Pastel shades are difficult to produce without a high quality background and often command a higher price.
For example, wool of excessive yellowness has poor reflectance in the blue region (same Y, different Y-Z). This means that a bright blue colour (higher Y-Z) could not be achieved using this wool.
Similarly bright shades could not be achieved using dull wool (same yellowness, reduced brightness).
The example shown here demonstrates how a wool with Y-Z=0 could be dyed to the pastel pink shade shown, while a wool with Y-Z=10 would be “off-shade” and too dull.
It is important that topmakers know what they are getting in a blend as far as colour is concerned. The colour of tops can be an important specification from their customers.
It should be noted that the colour of tops is usually expressed as Whiteness, which takes in the whole colour spectrum. For more information see the “Top Testing” module.

## Slide 8: Why measure?
assists in processing operation
  colour consistency, batch to batch
  accurately select wool
  develop new markets for ‘super-white’ wools
processor requirement for test certificate for colour
Andrew Lindsay
Notes: Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
Industry Views
“ We urge growers to provide the measurement of average yellowness on their greasy wool pre-sale to assist us in the processing operation. We are confident that price premiums will, in time, occur as buyers seek wools to meet specific orders”.
- Judith Turk, G. H. Michell & Sons
“ The lack of objective measurements for colour inhibits the processor’s ability to:
  (a) ensure the consistency of colour, batch to batch;
  (b) accurately select wool for specific products; &
  (c) develop new markets for ‘super-white’ wools which cannot be subjectively selected”.
  - Kook-Gyun Lee, Daeyu Company Ltd on behalf of Korean Wool Delegation
“We have required our Australian suppliers to provide Test Certificates for colour for over 2 years. Those Australian exporters who supply our wool can encounter difficulties because the clean colour data is not widely available on greasy wool in Australian auction catalogues. Such information is freely available to exporters in New Zealand”.
- Jim Robinson, Forstmann (12/10/1994)

## Slide 9: Average Yellowness Measurement (‘97/98)
State
Adoption
Rate (%)
Average
Y-Z
QLD.
41.2
2.2
N.S.W.
4.8
1.4
VIC.
33.7
1.2
TAS.
32.9
0.8
S.A.
23.5
1.0
W.A.
10.9
1.1
AUST.
19.7
1.3
Andrew Lindsay
Notes: <number>
<footer>
Written by: Mr. Andrew Lindsay, Australian Wool Testing Authority Ltd.
Some of the processing industry views are included in the previous slide. These reflect the importance of the colour of wool to the processor. Unfortunately this requirement has not been reflected in the market, and therefore the uptake of colour measurement has been relatively slow in the industry.
The table shows the State adoption rate for colour measurement in 1997/98 and also the average yellowness measured in each State.