## Slide 1: Implications of Contamination (non-VM)
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer & Ms. Lorraine Osborne, The University of New South Wales.
Notes: <number>
<footer>
This module examines the sources of non-VM contamination in raw wool, the effect of this contamination on handling and processing, and the prevention of this type of contamination.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.

## Slide 2: Contaminants in Wool
grease, dirt, suint etc.
pesticides
brands etc.
vegetable matter (VM)
non-VM
  potential fibrous faults
  man-made origin
  preventable
P. Auer & L. Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
There are many contaminants in wool, as listed in this slide.
This module focuses on non-VM contamination. This type of contaminant is very damaging and costly to subsequent processing, especially when it forms fibrous faults, which are very difficult to remove.
Generally, these non-VM faults have a man-made origin, and they are usually preventable with good housekeeping procedures and careful handling.

## Slide 3: Types of Non-VM Contaminants
fibrillating plastics
film plastics
textile fibres
hairs / feathers
solid objects
  plastic
  metal
  wood
P. Auer & L. Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Source: Abbott, G.M., Blanchonette, I. And Heintze, G.N., (1996) Packaging and Contamination, In: Proceedings of Top-Tech ‘96, CSIRO, Geelong, p363.
There are numerous types of within-bale contamination being found in Australian wool. The two most common items likely to produce fibrous faults are haybale twines and woven plastic fertiliser or seed bags. Other items include plastic tapes, plastic film, bristles and hairs, strings and threads, solid metal and plastic objects, feathers, elastration rings, wire and articles of clothing.
Plastic materials used in packaging are often heat drawn during manufacture to increase strength. As a consequence of this increased molecular orientation in the longitudinal direction, there is a propensity for the material to spit lengthwise into many fine fibres when lateral tension is applied. This mechanism is known as fibrillation. Plastic bags and films which have not been heat treat drawn have no preferred direction of splitting and are therefore much more difficult to fibrillate into fine fibres. They are therefore less likely to remain as contaminants in wool during processing.
Plastic twines and woven bags are made from either polypropylene (PP) or high-density polyethylene (HDPE). PP has a higher strength than HDPE and also fibrillates more readily. Haybale twines and woven fertiliser bags are made from PP whereas most woolpacks are woven from HDPE tapes. It is necessary to distinguish clearly between PP and HDPE fibres for the source of the contamination to be correctly identified. This can be done firstly by melting point, PP melting at 170°C and HDPE at 135°C. The colour of the melted bead is another indicator of origin with haybale twines being mostly black and red and fertiliser bags clear or white. The HDPE in woolpacks is mostly beige in colour except for the two green or blue identifictaion stripes in the regular and premium packs respectively.
Plastic contaminants other than PP and HDPE may also be identified by melting point with nylons melting in the range 213-250°C, polyester at 250°C and low-density polyethylene at 108°C .
Other possible contaminants in wool are brown and red fibres from jute woolpacks or greenish fibres from sisal haybale twines. These are cellulosic fibres which burn like paper rather than melt. It is important to examine the appearance of these fibres closely to distinguish them from fibrous types of vegetable matter.

## Slide 4: Cost of Contamination
isolated disasters
  large pieces
fault in end-product (fabric)
  inspection
  removal
total cost
  approx. $M6 per year (10c/kg)
other fibres
  cotton also has problems
P. Auer & L. Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
When non-VM contamination does cause a problem, it sometimes occurs as an isolated incident where a large piece of material has got through and contaminates a whole batch. These large faults are far and above the usual level of background faults that occur, and are also a problem. Potentially large faults can cause the biggest problems if undetected.
If non-VM contamination ends up in the end product, which may be a fabric, then it is expensive to remove. The fabric must be inspected and the fault removed manually. The fault can be detected with the right equipment at the yarn stage, but this also leads to a loss of production, and joins in the yarn during the winding process before folding.
Other potential costs include a delay in delivery of the product to the customer or a claim for faults which have been overlooked by the manufacturer.
In wool processing, a decision needs to be made as to the point(s) at which inspection should take place as well as the level of inspection that can be justified in terms of the cost and quality of the product. In some mills the greasy wool is thoroughly inspected as it is removed from the bale whereas in others only final fabric may be examined.
Highest costs reported are;
i) A large vertical worsted mill spends $0.04 /kg clean for inspection prior to carding plus $A0.34/kg for removing manmade contaminant faults from their woven fabrics.
ii) A knitwear producer calculated that plastic contamination in dark, solid shade garments cost $A0.52/kg clean to remove. In a total of 155 tonnes of wool the monthly costs varied between $A0.18 and $A1.42/kg.
An estimate of total costs would be about $6 million per year over the whole Australian clip.
Other fibres experience non-VM faults during processing, but wool is known to be the worst offender.

## Slide 5: Modes of Contamination
within-bale
  on-farm source
from woolpacks
  farm (dividers)
  testing
  handling
during processing
  processors
P. Auer & L. Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
The modes of non-VM contamination are listed.
Within-bale contamination can be attributed to a farm source, and includes such things as haybale twine and woven plastic fertiliser and seed bags.
Contamination from woolpacks usually occurs after the wool has been baled, but the use of woolpack material for dividers and the like doesn’t eliminate the farm source. Such things as jute yarn, high density polyethylene (HDPE), and nylon fibres could come from this source.
The incidence of non-VM contamination occuring during processing is difficult to measure. It is also very difficult to prove.

## Slide 6: Within- Bale Contamination
Incidence
  amounts of within-bale contaminants most commonly found in wool fabrics
Woollen
weaver
(Aust)
Woollen
weaver
(OS)
Worsted
weaver
(Aust)
Worsted
weaver
(OS)
Worsted
weaver
(OS)
Worsted
weaver*
(OS)
Fault
PP twine
PP bag
VM
0.22
3.8
1.32
0.26
0.37
0.03
0.88
13.0
0.11
0.12
0.32
0.02
-
-
1.54
4.82
1.23
1.83
* using wool which was sorted for faults before processing
Faults per Tonne of Fabric
P. Auer & L. Osborne
Source: Abbott, G.M. et al (1996)
Notes: Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Source: Abbott, G.M., Blanchonette, I. And Heintze, G.N., (1996) Packaging and Contamination, In: Proceedings of Top-Tech ‘96, CSIRO, Geelong, p364.
The number of non-pack contaminants found in Australian wool increases as the quality of wool decreases. In the carbonising sector, wool is manually sorted for stains and other faults before carding. It has been found that in 15.5 million kgs of clean wool there were a total of 25300 within-bale contaminants. This equates to 1.6 faults per tonne. Feathers (35%) were the most common contaminant in the carbonised wool followed by haybale twine (17%) with PP fertiliser bags occuring very infrequently (0.17%). However, the total weight of the PP bags was a third that of the twines thus indicating that such faults were relatively large and therefore potentially serious if fibrillated into colourless fibres.
A topmaker using good quality wools found 0.3 within-bale contaminants per clean tonne when greasy wool was thoroughly inspected before scouring. The main contaminants were nylon sewing thread from HDPE packs (23%), other synthetic thread (23%) and metal bale clips (12%) with haybale twine only 5.5% and fertiliser bags only 1.4% of faults. It should be noted that undyed nylon is not generally regarded as a contaminant in undyed wool because when a wool/nylon mixture is dyed, both fibres take up a similar amount of colour.
The results in the table above show large differences in the number of faults found by processors. In the worsted sector, haybale twine occurred much more frequently in fabric than in greasy wool except where the greasy wool was already sorted for faults. This exacerbation of the problem is to be expected because short lengths of bale twine have been shown to fibrillate into 50 or more fine fibres during processing. Contamination from PP bags in fabric was well in excess of the levels found in the greasy wool, and varied widely between mills. Again a large lightly-pigmented fault occuring infrequently breaks down into a much larger number of faults.
The incidence of vegetable matter faults in the fabrics in the above survey was actually higher than that of other within-bale contaminants.

## Slide 7: Contamination from Woolpacks
types of woolpacks
  jute
  HDPE
  nylon
    hidden contamination
  AS/NZ 4546:1999
causes of contamination
  accidents
  testing
  offcuts
P. Auer & L. Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
In the past four types of woolpacks have been used in Australia, jute, HDPE, Premium HDPE and nylon. However, in 1999 with the introduction of standard AS/NZS 4546:1999, ‘Specification for woven woolpacks for greasy wool’, nylon is now the only approved material for Australian woolpacks. New Zealand may have either nylon or HDPE.
Nylon is the preferred material for woolpacks, since it has an affinity for wool dyes. Therefore any nylon contamination is largely hidden if it manages to make it through processing, and is small enough in diameter; whereas HDPE takes up no dye and becomes much more apparent as a fault when wool is dyed.
The causes of woolpack contamination are accidental damage, damage during sampling (perhaps by faulty test equipment), and the inclusion of fabric off-cuts or dividers inside the packs during pressing.
Whatever the source, the important point to remember is that small pieces of potentially fibrillating material end up in the raw wool before processing.

## Slide 8: Pack Specification
AS/NZS 4546:1999
AS/NZS 4547.1 to .4
performance and testing requirements
P. Auer & L. Osborne
Source: AS/NZS 4546:1999
Nylon HDPE Test Method
Breaking Force [N(min)]
Extensibility of fabric at 500N
[%(max)]
Tearing force (both directions)
[N(min)]
Seam strength [N(min)]
Fibrillation [Grade(min)]
Adhesion of wool
to the anti-slip coating
Surface frictional properties (N)
Handling resistance (N(min))
Warp-way 2450
Weft-way 2450
10
400
1200
n/a
no adhesion
 3.5
n/a
Warp-way 1760
Weft-way 1570
n/a
400
880
3
no adhesion
 3.5  5.5
700
AS 2001.2.3
Method A
As above
AS 2001.2.10
AS 2001.2.20 (A)
AS/NZS 4547.1
AS/NZS 4547.2
AS/NZS 4547.3
AS/NZS 4547.4
Notes: Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Source: AS/NZS 4546:1999
As previously mentioned in 1999 new standards for woven woolpacks were introduced.
The standard AS/NZS 4546, “Specification for woven woolpacks for greasy wool” provides the wool industry with the minimum requirements for aspects of woven woolpacks affecting their use, durability, possible contamination of contents and their disposal. The performance and testing requirements of woolpacks or woolpack fabric is listed in the above table.
Standards AS/NZS 4547 are four standards for the ‘Methods of testing woolpacks for greasy wool”;
Method 1: Fibrillation of woven, HDPE fabric
Method 2: Adhesion of wool to anti-slip coating
Method 3: Surface fictional properties of fabric
Method 4: Handling resistance

## Slide 9: Non-Fibrillation Index (HDPE)
1
2
4
3
5
Fibrillation Grade
P. Auer & L. Osborne
Source: AS/NZS 4547.1:1999
Notes: Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Pictures sourced from AS/NZS 4547.1:1999
HDPE woolpacks are light beige in colour. When the lightly-pigmented HDPE tapes become fibrillated they are very difficult to detect as a contaminant in wool. Although the fault may not be very noticable in light or pastel shaded fabrics it is a serious problem in darker coloured wool fabrics. The faults only become visible when the fabric is dyed and removing such faults at the fabric stage is very expensive.
Contamination from the woolpack is brought about by some form of damage to the pack which causes it to shed tapes or fibres into the wool. HDPE pack tapes have the ability to fibrillate into many very fine fibres which are not removed during processing.
Damage to wool packs can either be delibrate or accidental. Delibrate damage occurs in things like sampling and handling procedures such as core and grab sampling and bale handling hooks. Accidental damage can happen at all stages of handling from the shearing shed to the loading/unloading of shipping containers.
A method of reducing the effects of pack contamination is to produce packs from plastics which fibrillate less during wool processing and which are therefore more likely to be removed in carding.
The fibrillation index is a measure of the likelihood of the ends of broken woolpack tapes to appear either cleanly cut of fuzzy. The picture above shows the five different index grades, 1 being the worst. This index plays an important role in the specification of woven woolpacks.
Earlier work done by CSIRO researchers showed the effect on the behaviour of HDPE tapes when processed together with wool. Results below found for the removal of 330mm HDPE pack tapes during processing.
Fibrillation index Weight % removed in carding Faults per kg of fabric
3.0 39.7 1915
4.0 55.4 1096
4.5 66.2 807

## Slide 10: Contamination from Woolpacks
Incidence
  before processing
  after processing
  relative to VM
Woollen
weaver
(Aust)
Woollen
weaver
(OS)
Worsted
weaver
(Aust)
Worsted
weaver
(OS)
Worsted
weaver
(OS)
Worsted
weaver*
(OS)
Fault
HDPE
faults
Output
(tonnes)
0.85
0.15
1.54
1.47
0.29
0.11
364
164
621
507
605
2299
* using wool which was sorted for faults before processing
Woolpack Faults per Tonne of Fabric
P. Auer & L. Osborne
Source: Abbott, G.M. et al (1996)
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Source: Abbott, G.M., Blanchonette, I. And Heintze, G.N., (1996) Packaging and Contamination, In: Proceedings of Top-Tech ‘96, CSIRO, Geelong, p366
Prior to the introduction of nylon woolpacks investigations were carried out to assess the extent of the problems associated with woolpack contamination. One such investigation showed that in a total of 5.5million clean kgs of wool carbonised in Austraila there were 0.04 HDPE faults removed by manual sorters per tonne of wool inspected. This low level of contamination is nevertheless significant because it is offset by the high weight of the faults.
In the case of topmaking wools, an overseas processor found 4.4 HDPE faults per clean tonne for imported greasy wool and 0.45 faults per tonne for imported scoured wool. This large difference could be due to pack faults being easier to detect when the pack is first removed from the greasy wool rather than after the wool is scoured. Another possible explanation is that scoured wool is compressed to high shipping densities in new or repaired packs whereas greasy wool is dumped in the original packs which have been damaged in sampling.
Tha table above shows the HDPE faults per tonne of fabric found by the same wool fabric producers referred to in the previous table for contamination by PP twine and PP bags. Here again large differences between processors in the number of faults was observed in the end product. In two cases the HDPE faults were similar in number to the PP faults, in another two, HDPE faults predominated while the remaining two mills had most problems with PP faults. It is interesting to note that the larger mill, using pre-sorted wool, which processed more fabric in the same period had predominately HDPE woolpack contamination, a result more likely to represent the overall situation.

## Slide 11: Avoidance of Contamination
on-farm surveillance
clip accreditation
trace-back schemes
better woolpacks
  nylon multi-filament packs
better handling
  pressing
  sampling
  dumping
P. Auer & L. Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
In has been shown that non-VM contamination in wool arises from a number of sources. Removal of these contaminants is expensive, therefore particular attention needs to be taken by woolgrowers in removing all types of fibrillating plastic from the shearing sheds and paddocks. These plastics have the unique ability to produce many more faults in the end product than were originally present in the greasy wool.
Clip accreditation schemes have attempted to address this problem with strict adherence to certain clip preparation methods. The operators of these schemes audit the farm and a buyer can have more confidence that the clip with acceditation is far less likely to have non-VM contamination.
When a sale lot of wool is cored and then tested the alkali insoluble sample is also examined for within-bale contaminants. If any contamination is found the whole lot is inspected and rebaled at the growers expense.
Stronger better constructed woolpacks reduce the contamination problem from the woolpack. With the introduction of only nylon woolpacks in Australia during 1999 this problem will be greatly improved.
Better handling procedures can also reduce the risk of contamination. Making sure the bale doesn’t move during pressing in the wool shed will reduce the number of holes made by the side pinning press, and thus reduce contamination from small pieces of bale fabric pushed into the bale. Closely monitoring sampling procedures will also eliminate some pack contamination. Core holes which are too close together allow tapes to be pushed into the bale and incorrect positioning of grab holes or too much wool being grabbed can initiate tearing of the bale with resulting contamination. The metal staps wound around compressed bales for dumping can cut into the bale causing contamination, it is recommended that the strapping should be oriented at right angles to the base ie. going across the seams of the base of the bale to reduce damage.

## Slide 12: Detection / Removal
Sirosorter
  discontinued work
Siroclear
  detects yarn faults during winding
UV Fluorescence
  describe concept and results
  discontinued work
P. Auer & L. Osborne
Notes: <number>
<footer>
Written by: Dr. Peter Auer and Ms. Lorraine Osborne, The University of New South Wales.
Over the years much research has gone into the development of techniques and equipment to detect and remove faults from wool, yarns and fabric.
Sirosorter developed by CSIRO Division of Wool Technology was a photodetecting device used on-line to identify discolouration ie. stained wool, and contamination in the scoured or carbonised wool.
Siroclear is a device developed by CSIRO which detects yarn faults during winding (the operation which takes singles yarn of bobbins and on to cones ready for folding).
Siroclear can detect dark fibres and VM and non-VM faults at high processing speeds using specialised detectors. When a fault is detected the winding is stopped, the fault is removed and the yarn is spliced with a high-grade splice developed at CSIRO.
This may seem like the answer to prayers about lowering contamination, but there is a trade-off. If there are too many faults, the production efficiency of winding plummets. It is far better to remove the faults at the source, which is usually the farm.
Research at CSIRO which has now been discontinued looked into incorporating a UV fluorescence tracer into HDPE bale material. This allowed HDPE contamination to be identified under a UV light. This method could identify HDPE contamination in partly loose wool, top, yarn and fabric.
Little attention has been paid to the distinction between within-bale contamination and woolpack contamination probably because correct identification could be difficult. Now with the introduction of nylon woolpacks this problem will be eliminated. Within-bale contamination originates on-farm where a number of measures can be implemented to prevent or alleviate contamination problems.

## Slide 13: References
Top-Tech ‘96
  Abbott, G.M. and Blanchonette, I. (1996) Wool Packaging, Contamination and all that Stuff, page 116.
  Abbott, G.M., Blanchonette, I. and Heintze, G.N., (1996) Packaging and Contamination, page 362.
P. Auer & L. Osborne