## Slide 1: Sources of Variation in the Non-fibre components of the Fleece
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module looks at sources of variation in the non-fibre components of the fleece: wax, suint, vegetable matter (VM) and dirt. Within-fleece gradients in these traits are outlined, including the appropriateness of the mid-side for estimating fleece averages.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Non-fibre components of the greasy fleece: Sources of Variation (%) #
# as % of total variation within mob
Within
Between
Non-genetic
factors
%
suint
36
64
Year,
bstatus, age
% wax
42
58
Year, age
% dust
82
18
Year
% VM
89
11
Year, age
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Sources:
Thornberry, K.J. and Atkins, K.D. (1984). Aust. J. Exp. Agric. Anim. Husb. 24:72.
Mortimer, S.I. and Atkins, K.D. (1993). Aust. J. Agric. Res. 44: 1523.
These results relate to 4 strains of Merino (fine, medium non-Peppin and 2 medium Peppins) in one environment only. The within-fleece and between-fleece components are expressed as a % of total within-mob variation. These values don’t indicate actual level of variation (i.e. could be a large % of a very small amount of variation).
Between-fleece variation in suint and wax is greater than within-fleece gradients, whereas within-fleece gradients in dust and vegetable matter are large compared to differences between fleeces.
“bstatus” = status of birth and rearing i.e. single, twin etc.

## Slide 3: Within-fleece gradients for non-fleece components
Suint
Dust
VM
Wax
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
In this figure, the arrows indicate the gradient from least to most.
Suint% shows an increase from backline to belly. Given its water-soluble nature, this gradient is likely to reflect the tendency for suint to be leached from the backline in response to fleece wetting, which would be greater at this site than on the side or belly of the sheep.
Wax% shows an increase from mid-side to backline and from hindquarters to forequarters. This reflects the gradient in follicle density as well as the reduction in the suint content of the mid-side and backline of the fleece.
The dust% is generally greatest along the backline, reflecting the more open nature of the fleece at this site.
VM% increase towards the breech and belly regions of the fleece, reflecting the proximity of these regions to pasture species that contribute vegetable fault.
Reference:
Thornberry, K.J. and Atkins, K.D. (1984). Aust. J. Exp. Agric. Anim. Husb. 24: 72.

## Slide 4: Correlation between site measurement and estimated fleece average
Mid
Shoulder
Mid
Side
Mid
Rear
Suint %
0.93
0.94
0.91
Wax %
0.88
0.89
0.90
Dust %
0.60
0.90
0.74
VM %
0.57
0.56
0.67
Washing Yield %
0.65
0.87
0.83
Brad Crook
Source: Thornberry and Atkins (1984)
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Thornberry, K.J. and Atkins, K.D. (1984). Aust. J. Exp. Agric. Anim. Husb. 24: 72.
For suint and wax, most sample sites provide a reasonably reliable estimate of the fleece average. For VM and dust, the within-fleece gradients cause all sites to be less reliable in estimating the fleece average, except for the mid-side sample for dust %. No single site provides a reliable estimate of vegetable matter content in the overall fleece.
The most reliable sample site for estimates of washing yield (where VM is ignored) is the mid-side.