## Slide 1: Within-fleece Gradients in the Components of Clean Fleece Weight
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module considers the gradients within the fleece (or across the body) in wool production per unit area of skin and the components traits of fibre diameter, staple length and follicle density. The appropriateness of the mid-side sample for estimating the fleece (or sheep) average is discussed.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Across-body variation in wool production per unit area of skin (grams per cm2)
Brad Crook
Source: Young and Chapman (1958)
0.217
0.189
0.154
0.188
0.236
0.175
0.220
0.181
0.137
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Young, S.S.Y. and Chapman, R.E. (1958). Aust. J. Agric. Res. 9:363
The arrows indicate a gradient from least to most. There is a large gradient in wool production per unit area of skin from the belly to the backline, with a lesser gradient from hind to forequarters.

## Slide 3: Across-body variation in average fibre diameter (m)
22.0
22.1
21.4
21.5
22.3
20.8
23.0
23.3
23.2
Brad Crook
Source: Young and Chapman (1958)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Young, S.S.Y. and Chapman, R.E. (1958). Aust. J. Agric. Res. 9:363
The arrows indicate a gradient from least to most. There is a general anteroposterior gradient in fibre diameter, such that hind section of the fleece is usually the coarsest. There is no consistent dorso-ventral trends.

## Slide 4: Across-body variation in staple length (cm)
6.7
6.9
6.8
6.7
6.8
6.7
6.6
6.9
6.0
No consistent
gradients.
Brad Crook
Source: Young and Chapman (1958)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Young, S.S.Y. and Chapman, R.E. (1958). Aust. J. Agric. Res. 9:363
There are no significant gradients within the fleece for staple length.

## Slide 5: Across-body variation in follicle density (no. per mm2)
61.8
50.6
46.8
55.3
62.9
56.8
57.2
44.5
36.8
Brad Crook
Source: Young and Chapman (1958)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Young, S.S.Y. and Chapman, R.E. (1958). Aust. J. Agric. Res. 9:363
The arrows indicate the gradient from least to most. Large gradients in follicle density exist from belly to backline and from hind to forequarter. Thus differences in wool production per unit area of skin between regions of the body are mainly a reflection of follicle density gradients. Contrast this with between sheep differences, which arise mainly from fibre volume (length and diameter).

## Slide 6: Measurements of fibre diameter and staple length taken from the mid-side have the highest correlation (r > 0.85) with the overall fleece average
Brad Crook
Notes: Written by: Dr. Brad Crook, The University of New England.
Mid-side sampling site - centred on the 3rd-last rib, half-way between the mid-line of the back and mid-line of the belly
As the fleece is highly variable in terms of fibre diameter and staple (fibre) length, and characterised by gradients in each trait across the body, the question arises: how do you sample a fleece to test overall average diameter and staple length for the fleece? Measurements made on samples taken from the mid-side have been shown to provide the best estimate of the overall fleece average.
Some growers measure diameter at the hip bones, to indicate the upper limit of diameter within the fleece. However, this sampling site does not provide as strong an indication of overall fleece diameter compared to the mid-side.