## Slide 1: Fleece Weight: Greasy vs Clean
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module defines greasy and clean fleece weights, as well as the measurement of washing yield used in flock testing. The phenotypic correlations between fleece weight, yield and the non-fibre components of the fleece are also given.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Fleece Weight: greasy vs clean
Greasy fleece weight (GFW)
follicles
fibres
wax and suint
contaminants
dust
VM
Clean fleece weight
(CFW)
estimated
measured
x yield%
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
greasy fleece weight (GFW) - total weight arising from weight of wool fibres + weight of wax and suint + weight of contaminants (e.g. dust/dirt, vegetable matter)
clean fleece weight (CFW) - estimate of total weight of fibre in the fleece; derived from GFW and yield%
CFW = Y% x GFW
100
washing yield - calculated from dried, scoured sample weight as % of original greasy sample weight; no adjustment for VM and dirt remaining in sample after scouring; used in flock testing (individual sheep/fleece measurements)
schlumberger dry combed top and noil yield - indicates yield of fibre processed into top; adjusts for weights of VM, grease and dirt (ash) remaining after scouring used in sale of wool (wool clip / sale lot measurement)

## Slide 3: Phenotypic correlations between fleece weight, yield & non-fibre components of the fleece
Brad Crook
Source: Mortimer and Atkins (1989, 1993); Thornberry and Atkins (1984)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Sources:
Mortimer, S.I. and Atkins, K.D. (1989). Aust. J. Agric. Res. 40: 433.
Mortimer, S.I. and Atkins, K.D. (1993). Aust. J. Agric. Res. 44: 1523.
Thornberry, K.J. and Atkins, K.D. (1984). Aust. J. Exp. Agric. Anim. Husb. 24:72.
Given the definition of washing yield, it is not surprising to find a negative phenotypic correlation between yield and each of suint%, wax% and dust% and a lack of a strong correlation with VM%.