## Slide 1: Staple Strength: The Potential Role of Length Variation
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New Engalnd.
Notes: <number>
<footer>
This module looks at fibre length variation within a staple and how this can influence staple strength. The major context of this is the presence of shed fibres within the staple.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Crimped length variability
1
2
clamp
clamp
clamp
clamp
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Increased variation in crimped fibre length may increase the potential for some fibres in the staple to be held by one clamp only. These fibres that do not traverse the whole distance between the clamps will contribute to the linear density of the staple, but will not bear the load when the clamps move apart in the staple strength testing procedure. So linear density overestimates the amount of load-bearing material in the staple and thus measurements of staple strength decline.
Fibre length variation exists within all staples, with some staples having higher than average variation. Another source of fibre length variation is shed fibres, resulting from shut-down of part of the follicle population while other follicles continue to produce a fibre. Shed fibres may or may not be held by a clamp during staple strength measurement.

## Slide 3: Fibre Ends
BROKEN FIBRE SHED FIBRE
Brad Crook
Source: Schlink, T. (1998)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Schlink, T. (1998). Follicle shutdown and staple strength. CRC for Premium Quality Wool, Wool Biology lecture series.
Primitive sheep have a photoperiod driven follicle cycle that leads to an annual shedding of the fleece. However, Merino shedding appears to be driven by nutrition rather than photoperiod, but this should not be ignored. It is important to be aware of follicle shutdown as it results in increased length variation within the staple and consequently, lower staple strength.
These scanning electron micrographs show the difference between fibres that have been broken and fibres that have been shed from the follicle. The magnification of the photos are different and both fibres actually have the same fibre diameter at the point of break. When examining staples and fleeces for shed fibres the staples are washed in a solvent and then hot water and stained with picric acid (yellow) and eosin (pink). The fibres are then examined with a microscope and the proportion of fibres with IRS (inner root sheath) (stains pink) still attached to the fibre is estimated. These fibres have been shed from follicles which have shutdown and look like the fibre in the right hand photo.

## Slide 4: Staple strength and fibre shedding
Brad Crook
Source: Schlink and Dollin (1995)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Schlink, T.C. and Dollin, A.E. (1995). Wool Tech. Sheep. Breed. 43:268.
In Merino sheep, the incidence of shedding under normal grazing conditions is generally low (<1%) and linked more to seasonal changes in feed, physiological condition and stress. However, Schlink and Dollin (1995) found the incidence to range from 0 to 30% in adult Merino wethers in the Mediterranean environment of WA, under conditions resulting in body weight loss during late summer. Those wethers with high levels of shed fibres produced the lowest staple strengths. But note that at levels <5% shed fibres, staple strength still ranged from as low as 20 to as high as 60 N/ktex. So obviously other causal factors are involved.

## Slide 5: Staple strength and fibre shedding
Brad Crook
Source: Schlink and Dollin (1995)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Schlink, T.C. and Dollin, A.E. (1995). Wool Tech. Sheep. Breed. 43:268.
The above figure refers to non-supplemented pregnant and lactating Merino ewes, lambing in autumn. The strong exponential decline in staple strength with an increase in shed fibre level is evident.