## Slide 1: Defining the Measurement of Staple Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module provides a basic definition of the measurement of staple strength and position of break.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Measurement of Staple Strength
clamp
clamp
Staple length (mm)
Staple weight (grams)
grams / metre
(ktex)
Force to break (Newtons)
1N  100 grams
Staple strength in Newtons per ktex:
force corrected for staple thickness
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
The force required to break a staple under extension is measured in Newtons, where 1N is approx. equal to 100 grams. The absolute force required is a function of the amount of fibre material present and capable of bearing the load. Thicker staples require more force to break than do thinner staples, as there is more load-bearing material present within the staple. Thus measurements of staple strength are adjusted for staple linear density, this being the weight per unit length (expressed as grams per metre, or kilotex). This gives units of Newtons per kilotex.

## Slide 3: Measurement of Position of Break
TIP
BASE
Tip portion (grams)
As % of staple weight
TIP BREAK <33%
MID BREAK 33-66%
BASE BREAK >66%
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
When a staple is extended to breaking point, it usually breaks at the relatively weakest point of the staple. The point (or position) of break in the staple is measured by way of the weight of the tip section as a percentage of the staple weight.
The position of break (POB) is of importance to top-makers in that it influences subsequent fibre length in the wool top and level of short fibre removed during combing. A tip or base break is preferable over a mid break. However, there are currently no market signals indicating the influence of POB on clean price.