## Slide 1: Sources of Variation in Staple Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module looks at sources of variation in staple strength. Gradients within the fleece are discussed as is the use of the mid-side for estimating the fleece average.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Across-body variation in Staple Strength (N/ktex)
Brad Crook
Source: Rottenbury et al. (1981)
31
33
36
36
34
31
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Rottenbury, R.A., Bow, M.R., Kavanagh, W.J. and Caffin, R.N. (1981). Wool Tech. Sheep. Breed. 29:143
The arrows indicate gradients from least to most. Gradients in staple strength tend to be small and inconsistent. The backline may be slightly lower in strength due to effects of weathering.

## Slide 3: Sources of Variation in Staple Strength (%)#
Within fleece 21
Within regions 18
Between regions 3
Fleece x region 14
Between fleeces 65
# as % of total within mob variation
Brad Crook
Source: Rottenbury et al. (1981)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Rottenbury, R.A., Bow, M.R., Kavanagh, W.J. and Caffin, R.N. (1981). Wool Tech. Sheep. Breed. 29:143.
Variation in staple strength between sheep is greater than within-fleece variation in staple strength. A range of at least 40 N/ktex can be observed between individual sheep within a mob. For within-fleece variation, staples within a region of the fleece exhibit greater variation in strength than does average strength between regions. However, note that the fleece by region component is significant, indicating substantial differences between sheep in the within-fleece gradients for staple strength.

## Slide 4: Measurements of Staple Strength taken from most sites provide a reliable estimate of the fleece average. Mid-side sample likely to be best.
0.88
0.93
0.97
0.96
0.92
0.91
Dam age and b/rearing status effects appear to be negligible.
Between-year variation significant.
Brad Crook
Source: Rottenbury et al. (1981)
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Rottenbury, R.A., Bow, M.R., Kavanagh, W.J. and Caffin, R.N. (1981). Wool Tech. Sheep. Breed. 29:143.
Measurements of staple strength taken from most regions of the fleece provide a relatively reliable estimate of the overall fleece average. Given that mid-side sampling is best for diameter, staple length and yield, this sample can also be used to obtain a reliable estimate of fleece average staple strength.
In terms of non-genetic handicaps for staple strength, dam age and birth-rearing status appear to have negligible effects. Year to year variation in average flock staple strength can be high.