## Slide 1: Staple Strength: The Potential Role of Initial Diameter, Rate of Change in Diameter and L/D Ratio
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module introduces the concepts of initial fibre diameter, rate of change in fibre diameter and the length/diameter ratio (L/D). Attention is given to how these measurements may relate to staple strength.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Diameter response to increasing nutrition: the influence of “initial” fibre diameter
NB: phenotypic, not genetic
Initial
FD
Final
FD
Abs. change
in FD
% change
in FD
18.0
21.0
3.0
16
22.0
26.0
4.0
18
24.0
29.0
5.0
21
26.0
31.7
5.7
22
28.0
34.3
6.3
23
Brad Crook
Source: Hynd,P. (unpubl.)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Thompson, A. (1993). In “Merino Sheep Breeding - Some Directions for the Future”, ed. D.R. Gifford, SARDI, p 18.
One study by Hynd, cited by Thompson (1993) suggested that finer diameter sheep may be less sensitive to diameter increases following an increase in the level of feed. The 18 micron animal, after being fed on a higher plane of nutrition, increased diameter to 21 microns, representing a 3 micron or 16% increase in diameter. The 28 micron individual, on the other hand, increased by 6.3 microns, representing a 23% increase. In other words, the broader wool type was more responsive in terms of diameter to an increase in feeding level.

## Slide 3: Rate of Change in Diameter (micron per mm)
Hansford and Kennedy (1988)
rate of change vs SS: -0.43 (P<0.05)
rate of change >> minimum FD
18
19
20
21
22
23
24
0
4
8
12
16
20
24
28
32
Length of Staple (mm)
Fibre Diameter (m)
Max. diam = 22 micron
Min. diam = 20 micron
0.5 m/mm
0.2 m/mm
0.125 m/mm
“A”
“B”
“C”
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Hansford, K.A. and Kennedy, J.P. (1988). Proc. Aust. Soc. Anim. Prod. 17:415.
The rate of change in fibre diameter reflects the rate at which diameter change occurs along a given length of the staple. In this graph, the difference between the minimum and maximum diameters in the profile is 2 microns. However, for sheep A, this difference is spread over an 8 mm length of the staple, giving a change of 0.5 micron per mm. Sheep B has the same diameter difference spread over a 20 mm length of the staple, giving a rate of change of 0.2 micron per mm. Sheep C has the lowest rate of change, as the 2 micron difference is spread over a 32 mm length of the staple.
Hansford and Kennedy (1988) demonstrated that sheep with a high rate of change tended to produce lower staple strengths (SS). An individual that is capable of buffering the change in diameter along the staple by spreading the change over a longer length of staple should theoretically achieve a higher staple strength.

## Slide 4: Response in fibre length and diameter to nutritional change: the influence of L/D ratio
Brad Crook
Source: Hynd< P.(1992)
Trait

FD

L

L/

D
Initial FD
+ 0.53
- 0.16
- 0.54
L/D
- 0.66
- 0.08
+ 0.51
NB: phenotypic, not genetic
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Hynd, P.I. (1992). Proc. Aust. Soc. Anim. Prod. 19:152.
The L/D ratio is the ratio of the length growth rate of fibres to the average diameter of the fibres. Hynd (1992) demonstrated that sheep with a high L/D ratio displayed greater length responsiveness to nutritional change compared to diameter responsiveness, suggesting that high L/D individuals could buffer against nutritional change by responding in terms of length rather than in diameter. This implies that diameter variation and rate of change could be lower in high L/D animals.
It also demonstrated again that animals of high diameter were more responsive in terms of diameter following nutritional change.