## Slide 1: Overview of Potential Determinants of Staple Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module provides a theoretical framework within which to view the various determinants of staple strength. It introduces the notions of localised and generalised fibre weakness.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New New England.

## Slide 2: Staple Strength
Variations in load-bearing material in staple
Inherent strength of
constituent fibres
Localised weakness
Most/all of fibre length
Physical changes
Structural changes
?
Fibre length variation
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
Variations in staple strength can arise from variations in the load-bearing material within the staple and variations in the inherent strength of the fibres in the staple.
Variations in the load-bearing material are generally associated with a localised weak point along the staple, such as happens when fibre diameter diminishes. It may also result from variation in fibre length, such that not all fibres are held by both clamps.
The inherent strength of the fibre refers to the strength of the actual fibre material, and is a feature which should be reflected along the length of the whole fibre. It implies that some fibres are composed of weaker material, such that they break at lower forces than other inherently stronger fibres. It is a reflection of structural and/or chemical differences between fibres.
There may be an interaction between the two in that changes in the physical dimensions of the fibre may be associated with changes in the structural or chemical components of the fibre. Either way, any factor which influences the load-bearing capacity of wool fibres can impact on the strength of the staple.

## Slide 3
1
2
3
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
The measurement of staple strength corrects for the average linear density of the staple, rather than linear density at the point of break. It is easier to understand the implications of this if we look at things from an individual fibre point of view. Fibres 1 and 2 are uniform in diameter along the fibre length of each, but the two fibres differ in terms of force required to break as fibre 2 has more material to bear the load. Force corrected for average linear density of the fibre likely to be similar. Fibre 3 has slightly lower average diameter over the whole fibre compared to fibre 2 due to a localised diminution in diameter. The diameter at the constriction is similar to that for fibre 1. The force to break fibre 3 will be lower than that for fibre 2 and similar to that for fibre 1 BUT average linear density of fibre 3 will be similar to that for fibre 2 (slightly lower). So corrected force likely to be lower than fibre 1 and 2.
Summary:
Average diameter (over whole fibre): Fibre 2 > 3 >>> 1
Average linear density of fibre: Fibre 2 > 3 >>> 1
Force to break: Fibre 2 >>> 3 = 1
Force to break (adjusted for linear density): Fibre 2 = 1 >> 3
The same principle applies to a staple with a diminution of diameter. The measurement is based on average staple linear density, but force to break is influenced mainly by linear density at point of break (i.e. at diminution).