## Slide 1: Fibre Diameter Profiles
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module looks at fibre diameter profiles, this being the pattern of change in fibre diameter along the length of the staple. Specific parameters of the profile are identified. Differences between sheep within a mob and differences between genetic groups within a flock are shown, suggesting a degree of genetic control of the diameter response to environmental changes.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New New England.

## Slide 2: Fibre diameter profile of a staple
17
18
19
20
21
36
44
52
60
68
76
84
Distance from tip (mm)
Fibre diameter (micron)
Max.
Min.
Position of break
Rate of change
(m per mm)
28
20
12
4
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
Changes in fibre diameter throughout the wool growth period (i.e. along the staple) are reflected in the fibre diameter profile. Features of this profile which have been discussed in relation to staple strength are the minimum diameter in the profile (point of lowest diameter), variation in diameter and rate of change in diameter per mm of staple between the maximum and minimum diameters.
The position of break generally equates to the point of minimum diameter.

## Slide 3: Between-flock differences in diameter response patterns throughout the year
Brad Crook
Source: Hansford (1994)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
Source: Hansford, K.A. (1994). In “WOOLSPEC94: Specification of Australian Wool and its Implications for Marketing and Processing”. CSIRO Division of Wool Technology, J1.
Although the diameter profile reflects the response of the sheep to environmental changes throughout the year, there is evidence to suggest that some flocks respond differently to the same scenario of environmental change, and even within a mob, some individuals will respond differently to others. This suggests that there are certain biological / physiological mechanisms which underpin diameter response patterns, and that these could vary at both the flock and individual levels. That is, there may be some flocks and certain individual animals that are less sensitive to environmental change, in terms of diameter. These flocks / individuals may be able to buffer against environmental change in a way that reduces the potential for staple strength to decline.