## Slide 1: Premiums and Discounts for Staple Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module demonstrates the nature of premiums and discounts for measured staple strength at auction. The dependency of the premiums and discounts on fibre diameter is shown, as is the non-linear relationship between measured staple strength and clean price.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Staple strength premiums & discounts#: 1st quarter, 1997-98
# additionally measured wools only
-140
-120
-100
-80
-60
-40
-20
0
20
15
17
19
21
23
25
27
29
31
33
35
37
39
41
43
45
47
49
51
53
55
Staple strength (N/ktex)
prem. / disc. (cents per kg clean)
Fine
Medium
Broad
Thresholds
:
F: 35
M: 34
B: 30
Brad Crook
Source: IWS Pricemaker Quarterly
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
The relationship between staple strength and clean price is not linear and is not constant across diameters. There are threshold strengths above which there are only slight premiums paid per increment in strength, whereas below these thresholds, substantial penalties are incurred. For fine wools (18.5-20.5 m), the premiums and discounts are greater compared to those for medium (20.5-22.5 m) and broad (22.5-24.5 m) wools of the same strength.
The implications are:
1. The return from improving staple strength depends on where the flock average sits relative to the threshold.
2. Staple strength is economically more important for fine wool producers compared to broader types.