## Slide 1: Staple Strength: The Potential Role of Intrinsic Fibre Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module provides a basic introduction to intrinsic fibre strength. Brief mention is made of how intrinsic strength may influence measured staple strength.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Intrinsic Fibre Strength
minimum FD and rate of change in FD cannot account for all variation in SS
fibres of same FD at POB can differ markedly in breaking load
suggests differences in the inherent strength of fibre material
  chemical composition
  arrangement of cell types
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
When considering the fibre diameter (FD) profile parameters, minimum fibre diameter and rate of change of fibre diameter, and how, in combination, they relate to staple strength (SS), it becomes apparent that there are other sources of variation in staple strength which have not been accounted for. At best, diameter profile parameters account for 60% of the variation in staple strength within a mob. Furthermore, for fibres of the same diameter at the point of break (POB), there can be large differences in the breaking load. This suggests that differences in the inherent strength of the fibre material may also constitute a source of variation in staple strength.
This subject is reviewed by: Hynd, P.I. and Schlink, T.C. (1992). In “Management for Wool Quality in Mediterranean Environments”, ed. P.T.Doyle, J.A.Fortune and N.R.Adams., Department of Agriculture WA, p. 92-98.

## Slide 3: Intrinsic Fibre Strength
1
2
3
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Intrinsic fibre strength is defined as the force required to break a fibre, divided by the cross-sectional area at the point of break. Thus it is a measurement of strength that is adjusted for the amount of material present at the breaking point.
In the diagram, fibre 1 has a lower cross-sectional area compared to fibres 2 and 3, the latter two having the same cross-sectional area. More force is required to break fibre 2 compared to fibre 1, but when adjusted for differences in cross-sectional area, the fibre strengths are similar (much the same as correcting for differences in average linear density). Fibre 3, on the other hand, requires less force to break compared to fibre 2, even though they both have the same cross-sectional area. This implies that the strength of the fibre material at the point of break is inherently weaker for fibre 3 compared to fibre 2.

## Slide 4: Cortical cell types
Brad Crook
orthocortex and paracortex
  chemically and structurally different
staple strength may decline with increasing % of paracortex BUT not conclusive
relative proportions can vary along the fibre and can be influenced by nutrition
  fibres are chemically and structurally variable along their length, but is this important?
finer fibres have higher % paracortical cells
  does this explain why finer fibres may be weaker?
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
The cortex of the wool fibre contains two main cortical cell types - orthocortex and paracortex - which differ in their chemical composition and arrangement of structural components.
Also, proportions of ortho- and para- cortex in the fibre can vary throughout the growth period and can alter with changes in nutrition. So chemical and structural changes along the length of the fibre exists.
note: finer fibres contain a higher proportion of paracortical cells.

## Slide 5: Staple strength vs % paracortical cells
Brad Crook
Source: Thompson (1993)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Thompson, A. (1993). In “Merino Sheep Breeding - Some Directions for the Future”, ed. D.R. Gifford, SARDI, p 18.
Thompson (1993) cites some evidence to suggest a reduction in SS as % paracortex increases. Paracortical cells contain more disulphide cross-links which could make them stronger BUT may also make them less elastic (more brittle). Later work by Thompson (unpub.) showed no significant relationship between cortical cell type % and SS.

## Slide 6: Staple strength vs cortical cell types
Brad Crook
Source: Hansford and Kennedy (1990)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Hansford, K.A. and Kennedy, J.P. (1990). Proc. Aust. Soc. Anim. Prod. 18: 484.
Hansford and Kennedy (1990) found no significant associations between cortical cell type % and SS in Merinos.