## Slide 1: Staple Strength: The Influence of Fibre Diameter and Diameter Variation
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module looks at the relationship between average fibre diameter and staple strength, and diameter variation and staple strength. The greater contribution of along-fibre diameter variation for low strength wool is discussed.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New New England.

## Slide 2: Staple strength vs minimum fibre diameter
SS = 2.71.MinFD
R
2
= 0.2386
20
30
40
50
60
12
13
14
15
16
17
18
Min. diameter in staple profile (micron)
Staple strength (N/ktex)
Brad Crook
Source: Crook, B. (unpubl.)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
Within a mob of sheep, those individuals with a lower minimum diameter in the profile tend to be associated with lower staple strength. However, there are always individuals that do not conform to this trend. As an example, animals with a minimum profile diameter of approx. 15 microns in the graph above show a range in staple strength from 32 to 54 N/ktex.

## Slide 3: Average fibre diameter vs minimum diameter in the profile
MinFD = 0.91.AvFD
R
2
= 0.5919
12
13
14
15
16
17
18
14
15
16
17
18
19
20
Average fibre diameter
Minimum diameter in profile
Brad Crook
Source: Crook, B. (unpubl.)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
Within a mob of sheep, there is a strong correlation between minimum profile diameter and the average fibre diameter of the mid-side sample. Therefore, those individuals of finer average diameter within a mob tend to be those with lower staple strength. This is a phenotypic association. It merely indicates that factors which reduce average fibre diameter at some point along the staple, and thus average diameter overall, also tend to reduce staple strength.

## Slide 4: Staple Strength and Diameter Variation
Sound# Tender#
Within Staples 80 86
Between fibres 64 43 Along fibres 16 43
Within Fleeces 4 3
(between sites)
Between Fleeces 16 11
# as % of total within mob variation
Brad Crook
Source: Rottenbury et al. (1981)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
Source: Rottenbury, R.A., Bow, M.R., Kavanagh, W.J. and Caffin, R.N. (1981). Wool Tech. Sheep. Breed. 29:143.
For sound wools, these being those testing >30 N/ktex (approx.), the between-fibre variation in diameter is the largest source of variation in diameter within a mob of sheep. For tender wools, these testing <25 N/ktex, the along-staple component of diameter variation is greater, accounting for a similar level of within-mob variation as that accounted for by between-fibre differences.
This indicates that an increase in diameter variation along the staple gives rise to a reduction in staple strength. The reason for this is that it creates a relative weak point along the staple, compared to a perfectly uniform fibre (staple).

## Slide 5: Staple Strength and Diameter Variation
Ritchie and Ralph (1990) - SW WA (high rain / mixed)
CVFD vs SS: -0.83
Swan et al. (1995) - Nth T’lands NSW (high rainfall)
CVFD vs SS: -0.29
Gifford et al. (1995) - SE SA (cereal-sheep)
CVFD vs SS: -0.18, - 0.40
Denney (1990) - central NSW (cereal-sheep)
along-staple variation vs SS: -0.30
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New New England.
Sources:
Ritchie, A.J.M. and Ralph, I.G. (1990). Proc. Aust. Soc. Anim. Prod. 18:543.
Swan, A.A., Lax, J. and Purvis, I.W. (1995). Aust. Assoc. Anim. Breed. Genet. 11:516.
Gifford, D.R., Ponzoni, R.W., Ancell, P.M.C., Hynd, P.I., Walkley, J.R.W. and Grimson, R.J. (1995). Wool Tech. Sheep Breed. 43: 24.
Denney, G.D. (1990). Aust. J. Exp. Agric. 30:463.
Across a diverse range of environmental conditions (summer- and winter- dominant rainfall areas; high vs medium annual rainfall), diameter variation has a strong association with staple strength. By this, individuals with higher levels of diameter variation within a mob are associated with lower staple strengths, at least at a phenotypic level.
Environments which create high levels of variation in diameter throughout the year generally produce lower staple strength on average compared to less seasonal environments. But within all environments, there exists a negative association between staple strength and diameter variation.