## Slide 1: Associations Between Style Traits and Fibre Diameter Variation
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module presents the phenotypic correlations between diameter variation and a number of style traits (crimp definition, staple thickness, staple structure, dust penetration and greasy colour).
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Mid-side diameter variation and components of style: phenotypic associations
* All traits assessed (scored), with lower score indicating better performance
Traits *
(scored)
Peppin
SA
Fine
(Crook et al. 1995)
(James &
Ponzoni 1992)
(Lax et al. 1995)
Crimp definition
0.23
0.25
0.33
Staple thickness
0.23
0.32
0.31
Staple structure
0.30
0.32
-
Dust penetration
0.01
-
0.08
Greasy colour
0.03
0.10
0.12
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Sources:
Crook, B.J., Piper, L.R. and Mayo, O. (1995). Aust. Assoc. Anim. Breed. Genet. 11: 591.
James, P. and Ponzoni, R. (1992). Wool Tech. Sheep Breed. 40: 25.
Lax, J., Swan, A.A. and Purvis, I.W. (1995). Aust. Assoc. Anim. Breed. Genet. 11: 516.
At the phenotypic level, diameter variation is associated with aspects of fleece structure, including crimp definition. Higher variability is associated with poorer crimp definition, thick staples and reduced staple structure. Associations between diameter variation and assessed dust penetration and wool colour are negligible.