## Slide 1: Style and the Australian Wool Clip
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module introduces the concept of raw wool style and provides a breakdown of state and national clips into the various style grades. It reflects the influence of environmental factors on style, suggesting that style is a function of the interaction between fleece and environment.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Style
Brad Crook
a grading system used to distinguish between wools which are EXPECTED to have DIFFERENT processing performance and DIFFERENT end-product attributes
  Style grades 1-7 for Merino fleece wools
  grade 1 is best, grade 7 is worst
technology for objective measurement of style is currently underway
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Style should be considered as a composite trait. In many respects, it is a summation of those attributes of the wool that are considered to be of importance in some way to the processor, but are not measurable. Style is the summation of traits that are assessed by eye and hand. By obtaining this information, processors expect to get a more accurate picture of the potential processing performance of the wool, beyond that indicated by measured traits.
Subjective assessments are always hampered by concerns over repeatability of assessment and agreement between assessors. CSIRO is currently developing technology for the objective measurement of style traits.

## Slide 3: Style grade profile of greasy Merino wool sold at auction in each state: 1992-93 to 1994-95
0%
20%
40%
60%
80%
100%
NSW
WA
Vic
SA
Qld
Tas
Aust
% of bales
MF7
MF6
MF5
MF4
MF1-3
Brad Crook
Source: Wool International
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Wool International
National % of bales in each Merino style grade 92/93 - 94/95:
MF1 - Choice 0.003%
MF2 - Superior 0.007%
MF3 - Spinners 0.51%
MF4 - Best Topmakers 27.0%
MF5 - Good Topmakers 65.8%
MF6 - Average Topmakers 6.4%
MF7 - Inferior Topmakers 0.25%
State differences reflect environmental differences as well as Merino type effects. It is evident that Victoria and Tasmania produce the largest proportions of the highest style grades, with Queensland, South Australia and Western Australia producing a higher proportion of lower style grades, reflecting in part the more arid nature of parts of their woolgrowing environments.
MF1-7 refers to AWEX-ID description of style, whereas the descriptions Choice, Superior, Spinners, Best Topmaker etc. are derived from the old Australian Wool Corporation typing system.