## Slide 1: Fibre Diameter Variation Defined
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module examines the parameters derived from the measured distribution of fibre diameter. It defines average diameter, standard deviation of diameter, coefficient of variation of diameter and coarse edge. The relationship between average diameter and diameter variation is shown.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Fibre diameter variation (FDV)
is an inherent feature of wool
while there is an average fibre diameter (AFD), there is variation around this mean
variation occurs:
  between fibres at 1 point in staple
  along fibres within a staple
  between staples within a site
  between sites within a fleece
  between sheep within a mob
no direct economic value at present
Fibre diameter distribution
(FDD)
0
100
200
300
400
500
600
1
3
5
7
9
11
13
15
17
19
21
23
25
27
29
31
33
35
37
39
41
43
45
47
49
fibre diameter
frequency
Brad Crook
Notes: <number>
<footer>

## Slide 3: Parameters of the FDD:
Brad Crook
average fibre diameter (AFD, µm)
standard deviation (SD, µm)
  indicates amount of spread in diameters around AFD
  68% diameters: AFD ± 1SD
  95% diameters: AFD ± 2SD
  if AFD = 20 µm and SD = 3 µm, then:
    68% diameters in range 17-23 µm
    95% diameters in range 14-26 µm
coefficient of variation (CV%)
  a relative measure of variation: (SD/AFD) x 100%
% fibres >30 µm
  “coarse edge”, “prickle factor”
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Standard deviation of diameter (SD) - indicates how narrow or wide the distribution of diameter is (i.e.. a measure of actual variation). Assuming normality, 68% of fibre diameters lay within 1 SD either side of the mean diameter; 95% of fibre diameters lay within 2 SD either side of the mean. A diameter distribution with SD = 1.5 micron is narrower than a diameter distribution with SD = 2.5 micron.
Coefficient of variation of diameter (CV%) - expresses SD as % of mean. It is a measure of relative variation.
% of fibres exceeding 30 micron - if % fibres >30 micron in the fabric exceeds 5%, prickle can be detected (depending on fabric construction, finishing, etc.).
Measures of AFD and SD are more precise than measures of CV%. The precision of %fibres>30 increases as number of fibres in this coarse “edge” increases.

## Slide 4: Standard deviation vs CV%
AFD
CV% when
SD=3.5
SD when
CV=20%
19
18.4
3.8
22
16.0
4.4
25
14.0
5.0
same spread,
different CV%
different spread,
same CV%
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
It is important to realise the difference between the two measures of variation. SD measures actual spread while CV% measures spread relative to the mean. It is possible to have samples with the same spread in diameter but differing in CV% due to differences in mean diameter. Also, it is possible to have samples similar for CV%. CV% should never be used as a measure of actual spread in diameters (i.e. not to be used for assessing whether one distribution is narrower or wider than another).

## Slide 5: AFD vs SD: within-flock
2
3
4
5
6
14
16
18
20
22
24
Average Fibre Diameter (µm)
Standard Deviation (µm)
Brad Crook
Source: Crook et al. (1994)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Crook, B.J., Piper, L.R. and Mayo, O. (1994). Wool Tech. Sheep Breed. 42: 304.
As AFD of the fleece increases, SD increases. BUT note in the graph that 1 m change in AFD is associated with a 0.21 m change in SD. i.e. AFD changes faster than SD. Thus actual spread in diameter declines with decreasing diameter, but CV% may increase.