## Slide 1: Within-fleece Gradients in Diameter Variation
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module examines within-fleece gradients for diameter variation, measured as either the standard deviation of diameter in the wool sample or the along-staple variation in diameter. Non-genetic sources of variation in these measurements are also discussed. The influence of skin folds on diameter variation is mentioned.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Within-fleece gradients
Standard deviation
Between-year variation significant for FDV.
Increased variation on skin folds / wrinkles.
Along-staple variation
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
The arrows indicate a gradient from least to most. There are significant gradients in diameter variation across the body. There is an anteroposterior increase in the standard deviation of diameter, and a lesser increase dorso-ventrally. This reflects the gradients in average fibre diameter. Along-staple variation in diameter may also increase towards the rear of the sheep.
Annual changes in diameter variation can be substantial, depending on seasonality of pastures.
Wool sampled from the crest of a skin fold or wrinkle also tends to be higher in mean and variation of diameter, compared to wool sampled from smooth skin area.
References:
Denney, G.D. (1990). Aust. J. Exp. Agric. 30:463.
Olivier, J.J., Cloete, S.W.P. and Bezuidenhout, A.G. (1993). S. Afr. J. Anim. Sci. 23: 201.
Sutton, J.M., Williams, A.J., Nicol, H.I. And Thornberry, K.J. (1995). Wool Tech. Sheep. Breed. 43:183.