## Slide 1: Resistance to Wool Discolouration
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module addresses some of the fleece factors which differentiate susceptible and resistant types in terms of wool discolouration. This helps to explain in part the difference between the Merino strains in the relative brightness and whiteness of the wool produced.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Susceptible vs Resistant types
No difference between susceptible and resistant types
in terms of amino acid composition of wool fibres
Brad Crook
Source: Aitken et al. (1994)
potassium content
Trait
suint content (%)
wax/suint ratio
in suint (mg/g)
fresh suint pH
yield (%)
fibre diameter (µm)
Range
1.4-15.4
1.6-20.4
0.4-19.9
4.5-8.5
55.4-86.5
19.4-29.7
Susceptible
types have
higher
lower
higher
higher
lower
higher
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Aitken, F.J., Cottle, D.J., Wilkinson, B.R. and Reid, T.C. (1994). Aust. J. Agric. Res. 45: 391.
A comparison of sheep ranging in level of susceptibility to discolouration showed significant differences in the chemistry of the suint. Sheep susceptible to discolouration were characterised by higher levels of suint in the fleece, higher concentration of potassium in the suint and a more alkaline suint. They also tended to be of higher average fibre diameter.

## Slide 3: Merino strain comparison: wax and suint
Wax %
Suint %
Wax:suint
ratio
Fine
18.3 – 23.2
7.0 – 9.2
2.2 – 3.9
Medium
non-
Peppin
16.9 – 17.8
7.2 – 9.1
2.0 – 2.8
Medium
Peppin
17.0 – 22.0
7.7 – 11.1
1.7 – 2.7
Strong
14.3
8.6
1.7
Brad Crook
Source: Thornberry et al. (1980)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Thornberry, K.J., Kowal, E.A.B. and Atkins, K.D. (1980). Proc. Aust. Soc. Anim. Prod. 13: 95.
There are significant differences between Merino strains and between bloodlines within a strain for wax content, suint content and wax:suint ratio.