## Slide 1: The Chemical Reactions Involved in Wool Discolouration
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module summarises the chemical reactions likely to occur when wool discolouration results. The importance of moisture, heat, fleece chemistry and microbial activity is highlighted.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Yellow discolouration can result from:
also microbe-specific pigments (incl. red, blue, green, brown) occurring in stained bands
Brad Crook
decomposition of fibre keratin
  exposure to UV light (sunlight)
  heating
  high pH (alkaline conditions)
non-fibre components of the fleece
  chemical reactivity of suint components
  by-products of microbial activity
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Irrespective of whether wool is in a greasy, semi-processed or final fabric form, yellow discolouration can occur due to decomposition of the fibre protein (e.g. exposure to ultra-violet light; sustained high temperature; alkaline conditions).
However, the natural yellow discolouration that can be observed in some fleeces in the field is generally the result of a series of chemical reactions occurring within the fleece. It is a reflection of the chemical reactivity of the fleece, especially the suint component, combined with climatic conditions (moisture and temperature) and microbial activity.

## Slide 3: Chemical reactions: 1. Maillard reaction
“Browning” phenomenon involving certain amino acids and carbohydrates
glyceraldehyde orange brown
(medium)
glycolaldehyde yellow-brown
(medium)
white Merino wool
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
When white Merino wool is placed into solutions of glyceraldehyde or glycolaldehyde, a reaction takes place which results in discolouration of the wool. These reactive carbohydrate solutions, when combined with amino acids within the fleece, generate discolouration, a process referred to as the Maillard reaction.
So, one of the “requirements” for wool to discolour is for specific reactive carbohydrates to be present within the fleece environment.
Reference: Hoare, J.L. and Stewart, R.G. (1971). J. Text. Instit. 62: 455.

## Slide 4: Maillard reaction
Suint consists principally of potassium salts of various carboxylic acids
Some of these compounds are involved in microbial metabolism
Simple carbohydrates (e.g. glycolaldehyde) are derived
Reactivity with amino acids in “yolk” and skin debris to produce yellow discolouration
Wool fibres absorb discolouration, to give unscourable colour
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
This slide outlines the steps whereby microbial activity combined with suint chemistry yields reactive carbohydrates capable of generating a Maillard reaction involving proteins within the fleece. These proteins are more likely to be derived from the non-fibre components of the fleece, rather than the wool fibre proteins themselves.

## Slide 5: Chemical reactions: 2. Formation of carbonates
salts of carboxylic acids
formation of bicarbonates
and carbonates
glycolaldehyde
generate alkaline conditions,
facilitating decomposition of
keratin and discolouration
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
The microbial activity involved in formation of the reative carbohydrates also results in formation of carbonates, causing a rise in the pH of the fleece. As conditions become more alkaline, the wool fibres become more prone to decomposing and absorbing the yellow discolouration present in the “yolk” of the fleece.

## Slide 6: Chemical reactions: 3. Deamination of amino acids
Brad Crook
Microbes may degrade skin and “yolk” proteins to amino acids, producing ammonia (involved with discolouration of stored wool)
Potassium may act as a catalyst in this breakdown
Potassium may aid the speed of absorption of yellow pigments associated with discolouration
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
The microbial population is also implicated in wool discolouration via the formation of ammonia (a major causal factor of greasy wool discolouration in storage) as a result of degrading the non-fibre components of the fleece.
Furthermore, the potassium present within the suint is likely to act as a catalyst in this reaction as well as possibly increasing the speed of absorption of the discolouration into the fibre.
So the following factors are likely to be critical in determining the level of yellow discolouration present in wool:
  1. Quantity of suint produced (suint%) - affecting the concentration of reactive carbohydrates (i.e. Maillard reaction) and (bi)carbonates that may be produced (i.e. affect on pH increase) and total amount of potassium present;
  2. Potassium concentration - amount per gram of suint salts, affecting microbial deamination of amino acids;
  3. Temperature and moisture - affect size of the microbial population and rate of microbial activity.