## Slide 1: Incubated Colour Test
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module presents the incubated colour test as a means of identifying susceptible genotypes when environmental factors are not conducive to discolouration. The relationships between determinants of discolouration and the colour forming during incubation are shown.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2
expression of discolouration depends on warm temperatures and high humidity
  chemical reactivity:
    temperature dependent e.g. Maillard reaction
  microbial activity:
    moisture and temperature dependent
  rate of colour absorption by fibre:
    faster in wet conditions than in dry
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
A combination of moisture and warm temperature is required for discolouration to occur. Susceptible sheep can only express their susceptibility if the environmental conditions are conducive to discolouration. It could therefore be expected that greater levels of discolouration would be found in areas with a summer-dominant rainfall pattern.

## Slide 3: Incubated Colour
Brad Crook
Source: Aitken et al. (1994)
40°C
100% RH
5-7 days
Resistant to discolouration
Susceptible to discolouration
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Aitken, F.J., Cottle, D.J., Wilkinson, B.R. and Reid, T.C. (1994). Aust. J. Agric. Res. 45: 391.
Wool samples can be given an artificial challenge for discolouration by incubating the sample at high temperature (40°C) and humidity. This simulates the climatic factors required to induce discolouration in susceptible fleeces.

## Slide 4: Phenotypic correlations
Post-incubation
Absorbance#
0.85
- 0.72
0.95
0.74
- 0.20
Pre-incubation
suint content (%)
wax/suint ratio
potassium content
in suint (mg/g)
fresh suint pH
yield (%)
fibre diameter (µm)
0.69
Brad Crook
Source: Aitken et al. (1994)
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Aitken, F.J., Cottle, D.J., Wilkinson, B.R. and Reid, T.C. (1994). Aust. J. Agric. Res. 45: 391.
Each of the traits associated with susceptibility to discolouration has a high phenotypic correlation with the level of discolouration achieved after incubation. The absorbance of the wool extract at 430 nm is the measure of discolouration, a high absorbance value reflecting a higher level of discolouration.