## Slide 1: Dark Fibre Contamination
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module examines dark fibre contamination in the Merino industry, focusing on the sheep-derived sources of this contamination. It provides detailed discussion on the role of pigmented skin spots and isolated pigmented fibres in contributing to dark fibre contamination and discusses potential genetic strategies for reducing isolated pigmented fibres. It also looks at urine stain, given that it is the major source of dark fibre contamination and identifies the major management and clip preparation factors affecting dark fibre contamination associated with urine stain.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Dark fibre contamination
Brad Crook
Critical limits for white and pastel shade fabrics:
100 dark fibres per kg wool top
4 staples per 160kg bale greasy wool
 10 dark fibres per million white fibres
discounts if exceeded:
  50 cents per kg top
  4-15% reduction in selling price
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Spinners may specify a limit on dark fibre content to the topmaker such that the top may be rejected if the limit is exceeded (due to compensation claims likely to be made by fabric maker).
For high quality fabric in the white and pastel trade, the critical limit of dark fibres is 30-100 dark fibres per kg top, equating to 10 dark fibres per million white fibres or 4 staples per greasy bale. For ultra-high quality fabrics, the critical limit is 10 dark fibres per kg top or 1 staple per 100 bales.
If limits are exceeded, it could result in discounts of up to 50 cents relative to the selling price of a dark fibre free top, or a 4-15% reduction in selling price.

## Slide 3: Sources of dark fibres
Brad Crook
sheep-derived vs non-sheep
types dark enough to cause problems in fabric are:
  pigmented fibres (melanin)
  repeated urine staining
excluded types: canary stain, dag stain, water stain, fly-strike stain
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
There are a number of sources whereby dark fibres may be introduced during processing BUT the major source is associated with the greasy wool. Dark fibres in greasy wool are derived from sheep and non-sheep (e.g. baling twine) sources. The sheep-derived types dark enough to cause problem in fabrics are naturally pigmented fibres and urine-stained fibres. Canary stain, dag stain, fly-strike stain and water stain result in fibres with darkness below the critical colour threshold.
One study of merino tops showed that those with dark fibre content below or just above commercial limit of 100 per kg top contain both pigmented and urine-stained fibres. Tops with dark fibre content far exceeding the limit show the majority to be urine-stained fibres. Another study of tops produced in various commercial mills from 85 consignments of Australian wool, showed the presence of dark fibres in almost every sample, whereas only 1 wool pack fibre was found in one sample of top.

## Slide 4: Sources of pigmented fibres
Coloured sheep
Coloured birth coat fibres (on white lambs)
Pigmented skin spots
Isolated pigmented fibres (IPFs)
*
*
Brad Crook
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Sources of pigmented fibres:
1. Coloured sheep - black or brown pigmentation in Merino sheep is the result of a recessive gene which follows simple Mendelian inheritance. Approximately 6% of white sheep in Australia are heterozygous for the recessive gene, while up to 5% of sheep in a white flock may show obvious pigmentation. Patterns of pigmentation in which pigmented areas are asymmetrically placed and visible at birth in an otherwise white coat, does not follow simple Mendelian inheritance. Refer to the Wool Biology modules “Genetic Regulation of Melanin Synthesis” and “Melanocyte Distribution” for more detail.
2. Pigmented birth coat fibres - lambs may display a patch of brown or tan coloured fibres in the birth coat, usually on back of neck. It is assumed that these fibres shed soon after birth (or that pigmentation is inhibited early in life) as they are not readily apparent in the adult white fleece.
3. Pigmented skin spots - discussed in more detail on following slides
4. Isolated pigmented fibres - discussed in more detail on following slides

## Slide 5: The occurrence of pigmented skin spots and skin spots bearing pigmented fibres
Brad Crook
Source: Fleet and Forrest (1984)
0
10
20
30
40
50
60
70
80
1.5
2.5
3.5
4.5
5.5 (a)
5.5 (b)
8.5
Age (years)
% sheep
% with pigmented skin spots
% with skin spots bearing
pigmented fibres
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Fleet, M.R. and Forrest, J.W. (1984). Wool Tech. Sheep Breed. 32: 83-90.
3. Pigmented skin spots - these are often located along the back-line of sheep, with the development of spots being related to exposure of the skin to sunlight (causing activation and proliferation of melanocytes). These melanocytes can migrate downward to the follicle base where wool pigmentation can occur, such that they may bear a sparse population of pigmented wool fibres. However, not all pigmented spots produce pigmented wool fibres.
In the study by Fleet & Forrest (1984), no hogget sheep had pigmented wool fibres while older sheep showed a trend for increased incidence of pigmented spots bearing pigmented fibres. Only one of the 276 sheep aged 1.5-2.5 years was observed with a spot bearing pigmented fibres, compared to 53% for 8.5 year old sheep. Only the oldest sheep (8.5 years) showed >10 spots bearing pigmented fibres. Only 4.2% of spots from all age groups contained over 100 pigmented fibres. Premature shearing (5a vs 5b) increased the total number of pigmented spots (3.5x) but the increase in the number of spots bearing pigmented fibres was not as marked (1.8x). It was concluded that pigmented skin spots are unlikely to be an important source of dark fibres for Merino sheep 1.5-5.5 years age.

## Slide 6: Isolated pigmented fibres (IPF’s)
Breed
% with
% of affected with
(no. IPFs per 10 grams):
IPFs
< 1
1-10
>10
Merino
(n=515)
42
48
43
9
C’dale
(n=377)
32
45
43
12
Notes: Written by: Dr. Brad Crook, The University of New England.
Source:
Fleet, M.R., Pourbeik, T., Ancell, P.M. and Lynch, B.W. (1990). Aust. Assoc. Anim. Breed. Genet. 8: 511-514.
Fleet, M.R., Pourbeik, T., Ponzoni, R.W., Mortimer, S.I. and Rogan, I.M. (1991). Aust. Assoc. Anim. Breed. Genet. 9: 400-403.
4. Isolated pigmented fibres - these can occur throughout an otherwise white fleece and are extremely difficult to detect from inspection of sheep or the fleece. Most appear to contain black pigment but darkness can vary along fibre length.
The study of Fleet et al. (1991) was based on 515 hogget fleeces from 4 Medium Peppin Merino flocks run in one location. The study of Fleet et al. (1990) was based on 377 hogget fleeces obtained from a single Corriedale flock. The heritability for IPF count was estimated as 0.16 in the Merino study and 0.45 for Corriedale study.

## Slide 7: Age trends in isolated pigmented fibres (IPFs)
Fleece
IPFs per kg
wools

1 yr
1-2 yrs

2 yrs
Sheep
188
19
6
Sale lots
(n=161)
204
44
23
Brad Crook
Source: Burbidge and McInnes (1994)
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Burbidge, A. and McInnes, C.B. (1994). In “WOOLSPEC94: Specification of Australian Wool and its Implications for Marketing and Processing”. CSIRO Division of Wool Technology, N1.
Isolated pigmented fibres in the fleece were found to decline in number as sheep age BUT the risk of IPFs being present throughout lifetime of sheep still existed. Fleece wool from lambs, weaners and hoggets is likely to have higher IPF counts than fleece wool from adult sheep.

## Slide 8: Non-fleece pigmentation
birthcoat halo hairs 0.68
pigmented kemp fibres:
  face, legs, horn sites, ears 0.18 - 0.83
eyelashes 0.50
pigmented skin:
  nose, mouth, eyes, ears 0.17 - 0.74
hooves and horns 0.65
h2
Brad Crook
Source: Fleet et al. (1991)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Fleet, M.R., Pourbeik, T., Ponzoni, R.W., Mortimer, S.I. and Rogan, I.M. (1991). Aust. Assoc. Anim. Breed. Genet. 9: 400-403.
The phenotypic correlation between non-fleece pigmentation types is high and positive (0.46-87). There is a general trend for higher incidence of some non-fleece pigmentation types in Merino-derived breeds (e.g. Corriedale; Border Leicester x Merino) compared to pure Merinos due to the breeds used in development of the crossbred types.
It is worth noting the comments of John Ryrie Graham in 1870 - “All merino sheep, without exception, should be free from pigmented spots on the legs and face; and in the case of rams, no black strip on the horns or pigmented spots on the roof of the mouth can be tolerated”. This reflects an attitude that non-wool pigmentation may be an indicator of sheep heterozygous for fleece pigmentation types. There is no evidence to support this. But can they be used as indicator traits for the presence of isolated pigmented fibres throughout the fleece?

## Slide 9: Non-fleece pigmentation vs isolated pigmented fibres (IPFs)
Breed
“Trait”
% sheep showing IPFs with
“trait”:
Present (high)
Absent (low)
Merino (1)
Leg spots
64
22
Merino (2)
Leg spots
56
18
C’dale (3)
Horn sites
71
36
Leg spots
57
36
Nose colour
45
24
Brad Crook
Source: Fleet et al. (1987), (1991); Fleet (1985)
Notes: Written by: Dr. Brad Crook, The University of New England.
Sources:
Fleet, M.R., Rogan, I.M., Ponzoni, R.W. and Stafford, J.E. (1987). In “Merino Improvement Programs in Australia”, Proceedings of a National Symposium, AWC, p175.
Fleet, M.R., Smith, D.H. and Pourbeik, T. (1991). Wool Tech. Sheep Breed. 39: 24-34.
Fleet, M.R. (1985). Wool Tech. Sheep Breed. 33: 5-13.
(1) Fleet, Rogan, Ponzoni and Stafford (1987): Peppin merino hogget ewes - of those sheep with leg spots and IPFs, 33% had >10 dark fibres per 100g greasy. Of those without leg spots BUT with IPFs, 8% had >10 dark fibres per 100g greasy.
(2) Fleet, Smith and Pourbeik (1991): adult merino ewes - lower incidence of IPFs in sheep without pigmented leg fibres.
(3) Fleet (1985): Corriedale ewes - greater incidence of IPF in sheep with dark noses, pigmented leg spots or pigmented fibres at horn sites compared to pink noses, no leg spots and no horn sites pigmentation respectively

## Slide 10: Non-fleece pigmentation vs Isolated pigmented fibres (IPFs)
Criteria for culling
Average IPF per kg:
% culled
Criteria
present
Criteria
absent
Birthcoat halo hair
460
147
28
Hogget (- eyelash)
413
115
na
Hogget (+ eyelash)
363
33
na
Hogget + Lamb
345
15
68
Brad Crook
Source: Fleet et al. (1995)
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Fleet, M.R., Mortimer, S.I., Hynd, P.I. and Gallagher, J.R. (1995). Aust. Assoc. Anim. Breed. Genet. 11: 318-322.
Skirted hogget Merino fleeces were measured for IPFs per kg. Hogget ewes were scored for visible fibre pigmentation as lambs (face, legs, horn sites, eyelashes, ears and birthcoat halo hair pigmentation) and as hoggets (face, legs, horn sites, eyelashes, ears). Hoggets were then “culled” according to different criteria, with the average IPF count of “culled” sheep then being compared to those not “culled”.
Only when all hogget or all hogget and lamb criteria were considered could the average IPF of non-culled sheep be reduced below the threshold of 100 dark fibres per kg. BUT of the “culled” sheep, up to 69% were below the threshold. Across all criteria, 5-16% of non-culled sheep showed IPF counts exceeding the threshold and 56-69% of “culled” sheep showed IPF counts below the threshold
Most types of non-fleece pigmentation have a low positive phenotypic and genetic correlation with IPFs (depending on the level of non-fleece pigmentation in flock). Pigmented leg spots/fibres, pigmented fibres at the horn sites and pigmented birthcoat halo hairs show the most potential as indicator traits (but not completely indicative).

## Slide 11: Factors influencing urine stain:
Brad Crook
mulesing
crutching (ewes) and ringing (wethers)
pizzle dropping (wethers)
shearing technique
method of clip preparation
breeding
environment
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Urine stain is the major source of dark fibre contamination derived from Merino sheep. Factors influencing urine stain include:
1. mulesing - this increases the bare area in the crutch region so that less wool is available for repeated urine staining (reduced by 15% relative to unmulesed). The main purpose is to reduce soiling of the crutch region, reducing the likelihood of breech strike.
2. crutching (ewes and wethers) and ringing (wethers) - to reduce soiling of the crutch and pizzle regions, reducing the likelihood of breech and pizzle strike.
3. pizzle dropping (wethers) - this extends the penis (pizzle) below the wool line, thereby reducing soiling of the pizzle region and reducing the likelihood of pizzle strike and pizzle rot.
4. shearing technique - during shearing, the belly wool is removed first and with it urine stain of wool of wethers (and rams). But during shearing of ewes, stained wool is removed in two stages - the left crutch is shorn at early stage and the right crutch is shorn near end of shearing cycle, with no attempt to separate stained wool until shearing is complete.
5. breeding - there is likely to be a genetic influence on the degree of wool cover down rear legs.
6. environment - diet and fluid intake influence frequency of urination and may influence chemical composition of urine.

## Slide 12
Sheep:
crutched,
mulesed
Stain
(% of clip)
Dark fibre content
(no. per kg):
Skirted
fleece
Unskirted
fleece
Bellies
Wethers - c,m
1
150
300
42,700
Ewes - nil
7
2650
4900
1000
Ewes - c
1
280
410
4600
Wethers - c,m
1
70
430
83,500
Ewes - c
1
260
500
na
Brad Crook
Source: Rottenbury et al. (1987)
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Rottenbury, R.A., Charlton, D., Smith, L.J. and Eley, J.R. (1987) Wool Tech. Sheep Breed. 34(3): 156-165.
The above table shows the dark fibre concentration in tops produced from different clips, some of which represent different management practices (c=crutched; m=mulesed). The major points to note are:
1. Most of the dark fibre contamination associated with wethers is contained within the belly wool.
2. Crutching significantly reduces dark fibre contamination in ewes.
3. Relatively high levels of dark fibre in tops from clips appraised as having very low levels of stained wool (as % of clip).
4. The clip with the highest level of stain (7%) still had very high levels of dark fibre contamination in the fleece wool line.
5. Clip preparation (as indicated by skirted vs unskirted fleece lines) influences the concentration of dark fibres in the subsequent top.

## Slide 13: Influence of crutch-shear interval on dark fibre content in greasy wool
0
500
1000
1500
2000
2500
<= 3 months
> 3 months
uncrutched
Dark fibres per kg
fleeces
skirtings
15
11
70
302
251
2366
Brad Crook
Source: Burbidge and McInnes (1994)
Notes: Written by: Dr. Brad Crook, The University of New England.
Source: Burbidge, A. and McInnes, C.B. (1994). In “WOOLSPEC94: Specification of Australian Wool and its Implications for Marketing and Processing”. CSIRO Division of Wool Technology, N1.
The most common industry practice is to crutch ewes and wethers more than 3 months prior to shearing (4-6 months) depending on the potential fly hazard. The concentration of urine stained fibres in greasy wool increases rapidly as the interval between crutching and shearing exceeds 3 months. An interval of 3 months or less does not enable repeated urine staining to develop sufficient colour intensity or stained fibre length to be of concern. If the crutch-to-shear interval exceeds three months, modified shearing techniques and clip preparation procedures are required but this will increase the cost.