## Slide 1: Genetic Variation in Staple Strength
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Brad Crook, The University of New England.
Notes: <number>
<footer>
This module examines sources of genetic variation in staple strength, including between strain, between flock and within flock variation. The heritability of staple strength in a number of environments is reported, as are predicted gains in staple strength that could be achieved under single trait selection.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Brad Crook, The University of New England.

## Slide 2: Strain and environment effects
Armidale, NSW
Bakers Hill, WA
Fine
Medium
Fine
Medium
Staple strength
(N/ktex)
43.8
52.5
36.7
35.0
Minimum diameter
(µm)
16.8
18.9
14.3
16.6
Along-staple
variation (µm2)
1.63
1.20
2.09
4.29
Rate of change
(µm/mm)
0.19
0.13
0.09
0.11
Brad Crook
Source: Brown, Crook and Purvis (1999)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Brown, D., Crook, B.J. and Purvis, I.W. (1999). Assoc. Advmt. Anim. Breed. Genet. 13:
Twenty Merino ewes were maintained at Armidale NSW and 20 at Bakers Hill WA. In both environments, there were two bloodlines of sheep: fine and medium. Within each bloodline the animals were the progeny of two sires, the same sires being used in both environments to provide genetic linkage. There were 5 progeny per sire-bloodline-environment group. Sheep at Armidale were shorn in August whereas sheep at Bakers Hill were shorn in October.

## Slide 3: Between-flock variation in staple strength
Brad Crook
Source: Coelli et al. (1996)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Coelli, K.A., Casey, A.E., Atkins, K.D. and Semple, S.J. (1996). Supplement to Agfact A3.3.33, 1992. NSW Agriculture, Agdex 434/37
Data obtained from combined wether trials indicate that differences between flocks in staple strength are generally small, especially compared to differences between flocks in fleece weight and fibre diameter. The incidence of tender wool was very low (3%) in this data set. Also, no trend across fibre diameter is apparent.

## Slide 4: Between-sire variation
27.3
30.5
30.9
32.6
33.5
34.5
34.8
35.5
35.8
20
25
30
35
40
1
2
3
4
5
6
7
8
9
Sire group
N/ktex
Brad Crook
Source: Denney (1990)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Denney, G.D. (1990). Aust. J. Exp. Agric. 30: 463.
A flock of 198 two year old Merino sheep was maintained as a single mob in central-western NSW. Differences in staple strength between sire groups were evident.

## Slide 5: Phenotypic variation in staple strength
Aut.
Spr.
Spr.
Spr.
Spr.
Spr.
Spr.
Shorn
FLOCK
St. deviation
of SS
(N/ktex)
Great Southern Agricultural Research Inst. (WA)
Hogget rams
Commercial environment
Stud environment
Mature ewes
Turretfield Research Centre (SA)
10 mth of age (6 mth wool growth)
16 mth of age (6 mth wool growth)
CSIRO (Armidale)
F
ine wool (10 mth wool growth)
6.40
7.32
8.43
10.90
10.20
10.40
9.21
Brad Crook
Source: Greeff (1996)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Greeff, J. (1996). Genetics of Staple Strength. CRC for Premium Quality Wool, Wool Production Unit.
A trait must show variation for it to be exploited within a breeding program. Across a number of experimental flocks spanning a range of environments, strains, shearing times, and ages, within-flock variation in staple strength (as indicated by its standard deviation) ranges from 6 to 11 N/ktex.
Thus within a flock, a range in staple strength of at least 24 N/ktex between sheep would not be unusual.

## Slide 6: Heritability estimates of staple strength
FLOCK
Herit.
Great Southern Agricultural Research Inst. (WA)
Hogget rams
Commercial environment
Stud environment
Mature ewes
Turretfield Research Centre (SA)
10 mth of age (6 mth wool growth)
16 mth of age (6 mth wool growth)
CSIRO (Armidale)
Fine
wool (10 mth wool growth)
0.51
0.31
0.40
0.25
0.25
0.47
0.23
Aut.
Spr.
Spr.
Spr.
Spr.
Spr.
Spr.
Shorn
0.30
Brad Crook
Source: Greeff (1996)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Greeff, J. (1996). Genetics of Staple Strength. CRC for Premium Quality Wool, Wool Production Unit.
The proportion of the phenotypic variation that is under genetic control is given by the heritability. The heritability of staple strength varies across different flocks from 0.23 in the CSIRO fine wool flocks to 0.51 in hogget rams from GSARI. These differences could be due to different environments, strains, shearing times, sex, age at shearing, length of wool growth and flocks with different selection histories. However, it is clear that staple strength is a heritable trait in all flocks. Weighting these estimates according to their standard errors, provides an average estimate of 0.30.
There is greater scope for within-flock selection to improve staple strength than to exploit between-flock differences.

## Slide 7: Genetic gains in staple strength
Flock structure
Age (years)
2 3 4 5 6 Total
Rams 5 3 - - - 8
Ewes 100 90 80 70 60 400
Number of ewe and ram hoggets available for selection = 340
Heritability of staple SS = 0.30
Standard deviation of SS = 8.00 N/Ktex
Brad Crook
Source: Greeff (1996)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Greeff, J. (1996). Genetics of Staple Strength. CRC for Premium Quality Wool, Wool Production Unit.
The flock structure and genetic parameters shown above were used to predict the magnitude of genetic gain that can be achieved by within-flock selection for staple strength.

## Slide 8: Genetic gains in staple strength
Genetic gain = (im + if)/2 . h2 .SDss
(Lm + Lf)/2
1.4715 * 0.30 * 8.00
Genetic gain = -----------------------------
3.06
= 1.15 N/ktex per year
Pheno. SD
Generation
Length
Selection
Intensity
Heritability
Brad Crook
Source: Greeff (1996)
Notes: <number>
<footer>
Written by: Dr. Brad Crook, The University of New England.
Source: Greeff, J. (1996). Genetics of Staple Strength. CRC for Premium Quality Wool, Wool Production Unit.
The annual genetic gain is given by the above equation. The selection intensity and generation interval for males and females are calculated from the flock structure. Assuming that the standard deviation of staple strength is 8N/ktex and the heritability is 0.30 then staple strength can be improved by 1.15N/ktex per year.
This assumes selection only for staple strength. Inclusion of other traits in the breeding objective (e.g. fleece weight and fibre diameter) and use of additional selection criteria will impact on the extent to which these gains can be achieved.