## Slide 1: Wool: the Fibre
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module examines how fibres are classified and how they are produced.
It also examines some wool fibre properties in comparison to competing fibres. The differing requirements of fibre users along the processing chain are examined.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Fibre Classification
Natural
  wool
  cotton
  silk, cashmere, alpaca
  mineral
Regenerated
  natural raw material
    cellulose
    protein (discontinued)
  rayon
    ~1900
  re-launched Tencel
    1990’s
Synthetic
  polyester
    1940
  nylon
    1939
  acrylic
    1942
  polypropylene
    1960
  re-launched fibres
    1980’s onwards
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Fibres fall into the three broad classification listed; natural, regenerated and synthetic fibres.
Natural fibres have been used for millennia. The ancient Egyptians are known to have used cotton for clothing. Joseph’s coat of biblical renown was almost certainly wool.
Wool and cotton are the only natural fibres today which are used in significant enough quantities to be called major fibres. Cotton accounts for about 45% of world fibre production, while wool accounts for about 4%.
Regenerated fibres have used cellulose and protein as raw material, although those fibres based on cellulose are the only ones produced in any quantity today, accounting for about 9% of world fibre production, mostly as rayon. Like many artificial fibres, rayon has enjoyed some resurgence due to new fibre technology which saw it re-launched as Tencel™ in the 1990’s.
The development of synthetic fibres coincided with the technological advances of World War II, and also a supply of cheap raw material from the petroleum and coal industries. The only major new synthetic fibre since then has been polypropylene which coincided with the development of reliable polymerisation techniques. Some of these fibres, especially nylon and polyester have been re-launched as new fibres since the 1980’s coinciding with the development of new technology (e.g. microfibres).

## Slide 3: Fibre Production
wool
cotton
synthetic
regenerated
Raw
material
amino acids
carbohydrates
petroleum by-
products
cellulose
Polymer
synthesis
biosynthesis
biosynthesis
synthetic
polymerisation
N/A
(some modified)
Production
unit
follicle
boll
extruder /
spinneret
extruder /
spinneret
usable form
fibre
fibre
fibre
filament
fibre
filament
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
This table list some information comparing two natural fibres, wool and cotton, against synthetic fibres and regenerated fibres based on cellulose.
Using different raw materials and paths to polymer synthesis, and different production units, means the end result is:
  a product which has a very high length to diameter ratio
  relatively strong and pliable
  durable, and
  usable in common textile applications.
In other words the end result is a fibre. However, many properties and parameters determine the individual performance of the fibre.

## Slide 4: Fibre Properties
Peter Auer
Source: Morton, W.E. and Hearle, J.W.S. 1962
wool
cotton
polyester
rayon
diameter
15 – 25
µm
7-9 µm
(equiv.)
to 5 µm
~ 12 µm
length
(processed)
50 – 110mm
20 – 40 mm
able to be
specified
able to be
specified
strength
(fibre)
1.0
(relative)
2.5
3.5
1.3
elongation
at break
~40%
5 – 10%
10 – 40%
~25%
shape
elliptical
flat tube
varies
varies
surface
texture
scales
convoluted
able to be
modified
striated
absorbs
water
YES
YES
NO
YES
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: Morton, W.E. and Hearle, J.W.S. (1962), Physical Properties of Textile Fibres, Butterworths, Manchester & London
This table lists just a few of the many properties and parameters of fibres which have a bearing on their performance as textiles.
Which process the fibre is undergoing can determine which fibre property is paramount. For example, during carding where the fibres undergo their greatest test of strength, the tensile properties of fibre strength and elongation are important. However, when the fibres are incorporated in a yarn or ultimately a fabric, fibre properties such as bending rigidity and torsional shear become important. Similarly the moisture absorption properties become paramount during dyeing and finishing.
The usage of the fibre is another major determinant of which properties are paramount (e.g. a business shirt compared to a bullet-proof vest).

## Slide 5: Discussion
Peter Auer
Comment on the properties of wool compared to competing fibres
    see Fibre Properties
fibre fineness (diameter)
fibre length
fibre shape
tensile properties
surface properties
Notes: see next slide for answers

## Slide 6: Fibre Comparison: Wool
Peter Auer
relatively coarse
relatively long
high degree of fibre length variation
processed on a long staple system
  approx. 20 year technology lag
relatively weak but has good elongation
absorbs moisture well
  gives off heat when absorbing moisture
  finishes well (can be set)
subject to shrinkage in use (scales)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Using the Fibre Properties slide to compare different fibres, the conclusions on this slide would seem reasonable.
As a fibre, like any fibre, wool has advantages and disadvantages. The trick is to minimise the disadvantages while extolling the advantages of the fibre.

## Slide 7: Fibre Users: Early Stage
Peter Auer
Topmakers, Commission Combers
  quantity, diameter, processed length, short fibre content, specified VM, processing efficiency, colour
  yield, diameter, strength, length, contamination, colour
Spinners
  spinning efficiency, yarn evenness, yarn performance, colour, yarn faults
  diameter, CV diameter, processed length, short fibre content, contamination, colour
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
An illustration of how the importance of various fibre properties changes during the conversion of raw fibre to finished products is provided in the following three slides from early stage processing to consumers. Each stage has concerns about the product. These can be translated into terms of fibre properties.
Top-makers (and also commission combers) are primarily concerned with delivering a specified Top or Yarn to the next stage in processing, spinning, at a price. Therefore the concerns that they have with respect to their product are listed. These concerns can then be related to fibre properties. For example, if a Top has to be a certain diameter, then wool must be purchased which fits this specification. Yield affects how much of the raw material ends up in the top. Fibre strength and length will primarily affect fibre breakage and ultimately the length properties of the top, while the colour of the fibre will be retained in the top.
The concerns of spinners are expressed differently, and relate to their processing efficiency and product performance. These concerns can be translated into fibre concerns. For example the number of breakages during the spinning operation will affect the spinning efficiency. The number of breakages is known to be related to the amount of short fibres that are present in the top. Finer fibres make more even yarns. Longer fibres spin more efficiently.

## Slide 8: Fibre Users: Later Stage
Peter Auer
Weavers, Knitters, Dyers, Finishers
  yarn construction, yarn performance, fabric performance
  contamination, fibre type, colour
Garment-makers
  fabric performance, design, price
  contamination, colour, fibre type
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Fabric makers (weavers, knitters, dyers, finishers) are concerned with delivering a specified fabric to the next stage, the garment maker. Their product concerns are listed followed by the fibre properties that these concerns can be translated to. For example fabric makers are very concerned that no contamination is visible in their final fabric since this will be rejected, or face a discount from the garment maker.
The garment maker wants to produce a product that is pleasing to the retailer in terms of design, but that will also perform to expectations for repeat business. How these concerns translate to fibre properties is listed. For example a fabric that performs exceptionally as a suiting material would be made from wool fibre. A suiting material that performed less admirably at a price might be made from another fibre.

## Slide 9: Fibre Users: Retail
Peter Auer
Retailers
  price, design
  colour, fibre type
Customers
  comfort, easy care, performance, fashion, price
  colour, fibre type?
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Retailer want to satisfy their customers. They want to get the right designs on shelves at the right price points. They know their customers and their needs, and believe that the right garment design will satisfy their customers’ needs. For example, retailers know that certain designs will sell this year at certain prices. The use of particular fibres is determined as much by price as by aesthetic considerations.
A very important fact to remember is that the specifications for textile products originates at the retail end. The great majority of manufacture at earlier stages is undertaken to specified or expected orders. It is becoming more and more apparent that consumers are less and less fibre specific in their purchases, although certain fibres predominate in certain markets, (e.g. Kevlar for fireman, wool for business people).