## Slide 1: Carbonising
Produced for the CRC for Premium Quality Wool undergraduate program by;
Ms. Lorraine Osborne, The University of New South Wales.
Notes: This module gives a brief overview of the carbonising process and highlights some aspects of the process that require careful management due to their effect on fibre strength and colour.
Produced for the CRC for Premium Quality Wool undergraduate program by Ms. Lorraine Osborne, The University of New South Wales.

## Slide 2: Carbonising Process
brittle hydrocellulose
crushed and shaken out
wool neutralised with alkaline
solution, rinsed and dried
SCOUR
dilute Sulphuric bath
cellulose converted into brittle
hydrocellulose (charcoal)
ACIDISE
DRY/BAKE
CRUSH/DE-DUST
NEUTRALISE
CLEAN WOOL
Notes: <number>
<footer>
Written by: Ms. Lorraine Osborne, The University of New South Wales.
The aim of the carbonising process is to remove vegetable matter (VM) from the wool with no or little loss of fibre strength.
Scouring and carbonising occur sequentially as one continuous process. After scouring, the wool is squeeze dried, and then passed into a dilute sulphuric acid bath.
In the bath, a high penetration of acid into the VM is required, but with the lowest possible acid concentration so as to minimise fibre damage. This concentration of acid will vary depending on the nature of the VM to be removed, and the procedures used by the processing mill. The variables involved are a combination of acid concentration, temperature and time spent in the acid bath. A cold, dilute acid bath might have a 7-7.5% acid concentration, a concentration considered high, but the wool would remain in the bath for a very short time. Whilst a mildly warm bath, 32-38°C, would have an acid concentration of 4.5-6.5%, but the wool would remain in the bath for a longer time, say 2-5minutes. It has been found that an optimal acid concentration in the squeezed dried wool after the acid bath is 5.5%, with 7.5% being a critical level.
Auxiliary products such as wetting agents may also be added to minimise fibre damage. They have been shown to give some degree of protection to the wool fibre, but may not increase acid penetration to VM.
After acid soaking, the squeeze dried then proceeds into dryers (<70°C) and baking ovens (110-130°C). The drying process concentrates the acid. When the acid concentration in the VM is high enough, the cellulose is converted to brittle hydrocellulose(charcoal).
The wool then proceeds through crushers and de-dusters or shakers where the hydrocellulose/charcoal material is firstly crushed and then shaken out of the wool. The wool then passes into an alkaline bath, usually of soda ash but ammonia is sometimes used, where any residual acid in the wool is neutralised. The wool is then rinsed and dried.

## Slide 3: Potential Problems
Poor control may cause loss of fibre strength
    Acid concentration
    Drying
    Crushing stage
Fibre Loss
    debris removed from the de-duster contains a quantity of fibre
Discolouration
    carbonising may yellow the wool
    bleaching
Notes: <number>
<footer>
Written by: Ms. Lorraine Osborne, The University of New South Wales.
Fibre damage may occur during the carbonising process.
i) Poor control in any of the following can contribute to the loss of tensile strength in the fibres (weakening of the fibres):
a) Acid concentration: Too concentrated an acid or too long an immersion time in the acid bath can result in lasting fibre damage. Dilute acid penetrates easily into wool and attacks the intercellular material causing damage which results in lower fibre strength.
(b) Over drying: Drying the acid soaked wool at too high a temperature may cause the acid droplets to spot concentrate on the wool fibre causing localised damage. This damage may result in loss of fibre strength and extensibility.
(c) Crushing stage: During this stage the fibres can be damaged mechanically by becoming trapped between burrs and the fluted rollers of the burr-crushers..
ii) Fibre loss is also reported during the carbonising process, the debris removed from the de-duster contains an appreciable quantity of fibre.
iii) Discolouration or yellowing of the fibres takes place during the carbonising process and to overcome this mills often apply a mild bleach to the wool. This bleaching process, if not correctly managed can also cause damage to the wool and subsequently loss of fibre strength.