## Slide 1: Processing on the Woollen System
Produced for the CRC for Premium Quality Wool undergraduate program by;
Ms. Lorraine Osborne, The University of New South Wales.
Notes: This module explains the steps involved in the processing of wool through the Woollen system of yarn manufacture.
Produced for the CRC for Premium Quality Wool undergraduate program by Ms. Lorraine Osborne, The University of New South Wales.

## Slide 2: Blending prior to Carding
WHY BLEND?
To form a homogeneous batch
To be cost effective
To avoid irregularities of dyed colour
Add special effects or other fibres
More intimate fibre to fibre blending takes place during carding
Lorraine Osborne
Notes: <number>
<footer>
Written by: Ms. Lorraine Osborne, The University of New South Wales.
Blending is an essential process in woollen manufacture and is performed for the following reasons:
i) Uniformity of the batch/consignment
Since the woollen processing system has no gilling or combing steps to blend the fibres from the different wool batches, the blending of the wools into a homogeneous batch prior to carding is of vital importance.
Mills blend several different types of wools with similar properties together so as to maintain a standard type of blend and also to meet the specifications required for manufacture of a specific yarn type.
ii) Price
Blending allows wools of different prices to be incorporated into a batch without affecting the final quality of the yarn.
iii) Dyed Wool Colour
Careful blending is required if irregularities of colour are to be avoided when wools from different dye lots, which may vary slightly in shade, are mixed together.
iv) Special Effects
Special effect materials such as kemps, knops, silk, cotton and man-made fibres are introduced at the blending stage prior to carding.

## Slide 3: Systems of Woollen Blending
pile, stack or layer
batch
continuous
semi-continuous
Fearnought
Lorraine Osborne
Source: Brearley, A., (1965)
Notes: Written by: Ms. Lorraine Osborne, The University of New South Wales.
Source: Brearley, A., (1965) “The Woollen Industry”, Pitman Press, p47-53.
There are a variey of machines used in the blending process and the use of these depends on the quantity and degree of opening and mixing required. They also help to remove (clean) dust or dirt from the fibres. Oil is also added during blending.
Pile, Stack or Layer blending is the oldest method of blending. In this process thin layers of various components are laid one on top of the other in a sandwich formation over the floor and oil is added between the layers. The ‘sandwich’ is then broken down into armfuls containing some of each component and fed into a Fearnought (see below) or other opening machine. Stacking and opening is repeated until the required mixture is obtained.
The Batch System involves the dropping armfuls of the blend components in correct proportions down a hole in the floor where an air current carries the material to an opening machine. The material then flows into the first blend bin where a rotary spreader mixes the material. Holes in the bin floor allows the material to move to another bin where a second rotary spreader mixes it. Any number of intermixings can be carried out and when the blend is sufficiently mixed the material is passed to a fearnought and oiled.
In Continuous Blending the materials are weighed out in their correct proportions into a special weigh-pan that continuously feeds the blending system. No further handling takes place until the mixed blend emerges at the end having been mixed by centriblenders and fearnoughts and oiled.
A combination of the batch and continuous methods is called Semi-continuous blending. Here the materials are weighed as in continuous blending and then delivered into a bin with a rotary spreader as in the batch system. The feed is stopped and the material is transferred to a second bin and so on. Because the material is weighed out and pulled-down in the bins which can hold much more material than a centriblender, the semi-continuous system gives a better and more accurate mixing of the blend components than other methods.
The fearnought has a swift with two or more sets of workers and strippers and a doffer, an oiling device is often fitted to this machine at either the feed sheet or the delivery end. The progress of wool through the fearnought also assists to clean the wool as dust falls through the grid below the swift.

## Slide 4: Why Oil?
Minimise fibre breakage
Reduce fly
Quantities
  Worsted ½%
  Woollen 7%
cohesive properties make a stronger web
Lorraine Osborne
Notes: Written by: Ms. Lorraine Osborne, The University of New South Wales.
Oiling minimises fibre to fibre friction and fibre to metal friction thus reducing fibre breakage during carding. It also reduces fly and enhances the cohesive properties of the fibres allowing for a stronger web. The addition of lubricant also assists in the drafting in spinning.
Much higher levels of oil (7%) are placed on wools in the woollen system than those processed on the worsted system (½%). This is due to the shorter fibre lengths of the wools being carded and the greater need for its cohesive properties to aid easy sliver transfer at the intermediate feed and at the end of the carding process where the fibre web is divided into continuous ribbons of fibres.
For more information on lubricants see ‘Fibre Breakage in Carding‘ module.

## Slide 5: Typical Woollen Carding Set
Lorraine Osborne
Source: Brearley, A., (1965)
Notes: <number>
<footer>
Written by: Ms. Lorraine Osborne, The University of New South Wales.
Source: Brearley, A., (1965) “The Woollen Industry”, Pitman Press, p56.
The fundamental principle of the woollen card is the same as the worsted card. The wool fibres are disentangled, and reduced to a filmy web by working between two closely-spaced, relatively-moving surfaces clothed with sharp teeth. Just like the worsted card a woollen card consists of workers, strippers, fancys and doffers. For more information see “Carding Principles” module.
The woollen card however does NOT have any burr beaters. However, a device (‘Peralta’) consisting of 2 metal rollers with hydraulic pressure may be used to crush any vegetable matter present. This device is usually placed between the scribbler and the intermediate feed.
The woollen card consists of 2 or 3 sections. A 2 section card as seen above consists of a SCRIBBLER and CARDER . A three section card would have an intermediate section. The reason for division into several sections is to allow for better mixing of fibres by means of the intermediate feeds between each section.
The scribbler is the first part of the woollen card, it is here where the fibres are disentangled and the initial carding actions take place. Most of the fibre breakage and card waste produced will occur during carding in the scribbler section. After the final doffing in the scribbler the wool is in a continuous sliver, intermediate feed sliver, with the fibres separated but without much blending of fibres having taken place. The wool which lay say, to the right on the feed sheet will still be to the right in the sliver, i.e. NO BLENDING or MIXING of fibres has occurred across the width of the rollers on the scribbler.
This is the case with all carding worsted or woollen, but remember in the worsted system the fibres are mixed later during the gilling and combing processes, in woollen processing NO further mixing of fibres takes place other than that during the carding process.

## Slide 6: Transfer of Intermediate Sliver
Intermediate sliver from scribbler
Carder feed sheet
To carder
Scotch feed mechanism
Lorraine Osborne
Notes: Written by: Ms. Lorraine Osborne, The University of New South Wales.
The intermediate sliver is placed onto the feed sheet of the carder section at right angles to the way it left the scribbler, i.e. across the feed sheet (as seen above). This then allows for further mixing of the fibres to occur. The fibres are redistributed across the whole width of the rollers in the carder. Throughout the carder the normal process of carding the fibres takes place, it is only at the end of the carder that the rubbing of the web and slubbing/roving formation takes place. This occurs in the tape condenser.

## Slide 7: Tape Condenser
Lorraine Osborne
Source: Brearley, A., and Ireland J. A. (1981)
Slubbing
flat wool
ribbon
rubbing aprons
tape
Notes: Written by: Ms. Lorraine Osborne, The University of New South Wales.
Source:Brearley, A., and Ireland, J. A. (1981), “The Woollen Industry”, (WIRA: Leeds)
Before entry into the rubbing aprons of the tape condenser the carded web of fibres is divided into flat ribbons of fibres approximately 1cm in width. This can be performed either of 2 ways, by ring doffers or by tape condensers.
In ring doffing the last doffer of the carder is clothed with rings of card clothing with a small space between each ring. Fibres are removed from the swift by the rings of card clothing and subsequently mechanically stripped from the doffer and transferred to the rubbing aprons. Since the fibres on the swift adjacent to the spaces in card clothing on the doffer remain on the swift, the doffer usually makes a slow sideways transverse to allow for all fibres to be removed from the swift.
The most common type of tape condenser is the series tape that consists of 2 sets of leather or synthetic bands positioned side by side. After the final doffing the web of fibres pass between taking-in rollers. The bands pass around these rollers. The band which passes around the top rollers goes to the bottom of the machine and the one around the bottom roller goes to the top of the machine. As the web of fibres passes into the taking-in rollers they are divded into ribbons the width of each tape and are tranferred to the rubbing aprons
These ribbons of fibres are then converted into cylindrical slubbings by the rubbing action performed by rotating reciprocating aprons (see diagram). The rubbing action gives the slubbing a false twist which allows for better fibre cohesion during the spinning process.

## Slide 8
Ten individual slubbing
cheeses on each condenser
bobbin
Rubbing Aprons
Condenser bobbins
ready for transfer
to the spinning frame
Lorraine Osborne
Notes: Written by: Ms. Lorraine Osborne, The University of New South Wales.
When the slubbings leave the rubbing aprons each continuous slubbing is wound onto a condenser bobbin to form what is known as a cheese. The bobbins holding a set of cheeses are then transferred to the spinning frame for spinning into woollen yarn.
For more information see “Yarn Production” module.

## Slide 9: Spinning Comparison
WOOLLENS
WORSTED
INPUT
DRAFT
FIBRE CONTROL
TWIST
WINDING-ON
Slubbing Roving
1.3 30
False Twist Double apron
Ring Ring
Spindle Spindle
No. of FIBRES
IN X SECTION
100-120 35-45
Lorraine Osborne
Notes: Written by: Ms. Lorraine Osborne, The University of New South Wales.
A comparison of the spinning process for the worsted and woollen system is listed above.
Because of the delicate nature of the slubbing given that the fibres within the slubbing are generally short and randomly aligned, the slubbing is given a false twist to control the fibre movement during drafting. Drafting during woollen yarn preparation is much less than that in the worsted system where, because of the parallel alignment of fibres, rovings may be drafted 30 times. In woollen yarn manufacture the slubbing will only be drafted approximately 1.3 times.
There are two main types of machines used for woollen spinning - the woollen mule and the ring-frame. Since the 1960's when advancements were made in ring-frame spinning, the majority of woollen spinning is now performed on ring-frame machines. Woollen mule spinning frames although slow, produce a bulkier yarn than the ring frame, and are sometimes used to create upper market products from expensive fibres.
Because of the restricted spinning draft the count (thickness) of a woollen yarn and the production rate of the yarn manufacturing process are largely determined during carding.

## Slide 10: Recommended reading
Brearley, A., and Ireland, J. A. (1981), “The Woollen Industry”, (WIRA: Leeds)
Von Bergen, W., (1969), Wool Handbook, Vol 2, John Wiley & Sons.
Lorraine Osborne