## Slide 1: Comparison of Processing Systems: Worsted & Woollen
Produced for the CRC for Premium Quality Wool undergraduate program by;
Ms. Lorraine Osborne, The University of New South Wales.
Notes: On completion of this module the reader will have an understanding of the differences in the worsted and woollen processing systems, the raw materials which go into each system and the final products produced.
Produced for the CRC for Premium Quality Wool undergraduate program by Ms. Lorraine Osborne, The University of New South Wales.

## Slide 2: Australian Wool Clip
carbonising fleece, pieces and bellies, stain wools, etc
approx. 90%
of wool income
Skirtings
16%
Combing
fleece
67%
Locks
&
crutchings
6%
Other
5%
Weaners
& lambs
6%
Wool types by clean mass %: 1995-96
Lorraine Osborne
Notes: <number>
<footer>
Written by: Ms. Lorraine Osborne, The University of New South Wales.
Australian Merino wools are processed on either of two (2) processing systems:-
WORSTED
    or
    WOOLLEN
Australia produces mostly fine and medium Merino wools. Approximately 85% of Australia's raw wool, fleece and skirtings, is directed towards the WORSTED processing system. The other 15% are processed on the WOOLLEN processing system.
However, it should be noted woollen processing worldwide represents almost 50% of all wool processing. In countries such as the old USSR and China, where heavy military type uniforms were worn and where price differentials are of ultimate importance, woollen processing was and still is predominant.
The pie chart above shows a breakdown of the wool types produced in the 1995-96 season. In that year 83% of the Australian clip would have been processed through the worsted processing system, whilst 17% (the weaners, lambs, locks, crutchings and other) was destined for the woollen processing system.
It should be noted that the apporximately 90% of wool income comes from worsted combing wools. Thus far more emphasis is placed on research and development into the worsted processing system of yarn manufacture.

## Slide 3: Processing Systems For Wool
WOOLLENS
WORSTED
SCOUR
CARDING
GILLING & COMBING
TOP
WORSTED
YARN
SCOUR
CARBONISE
CARDING
CLEAN
WOOL
WOOLLEN
YARN
condensing
Slubbing
SPINNING
SPINNING
Lorraine Osborne
Notes: Written by: Ms. Lorraine Osborne, The University of New South Wales.
This slide explains diagramatically the steps in each of the processing systems. The woollen processing system is less complex than the worsted system. It includes a carbonising stage (see ‘Carbonising’ module) but does not have the gilling and combing sequences of the worsted system.
The carding machines in each system use the same THREE basic actions of, carding, stripping and raising (see “Carding Principles” module). However, the woollen card has no burr beaters or morels for burr removal. The only VM which is removed during woollen carding is that which falls out or is crushed by a Peralta device placed at the end of the first section of the card. See “Processing on the Woollen System” module for a more detailed description of a woollen card.
A major difference between the two processing systems is the output from the cards. The worsted card produces a sliver which is subsequently gilled and combed into a top, whilst the woollen card produces slubbings. These slubbings are collected on condenser bobbins which are then placed directly onto a spinning frame. The fibre alignment and linear density of a woollen yarn is primarily determined at the carding stage
Trading points for both systems of yarn manufacture are at the greasy wool and yarn stages. The other products traded are TOP in the worsted system and clean wool (scoured, or scoured and carbonised) for the woollen system.
There is also another method of processing called semi-worsted. This method although not widely used, is for the manufacture of long coarse wools making heavy weight yarns for the carpet and upholstery industries. The process is similar to the worsted system but without the combing sequence. Therefore the wool used must be VM free and long since there is no removal of short fibres and vegetable matter in the combing process. Mackie equipment from Belfast is specifically designed for this process.

## Slide 4: Differences between systems: Raw Material
Lorraine Osborne
WOOLLEN
Short virgin wool (Carding Wools)
Open or stretch broken TOP
Re-used waste (Worsted Noil etc)
Recycled material (Rags, tailors waste)
WORSTED
Virgin fleece and skirting wool
Notes: <number>
<footer>
Written by: Ms. Lorraine Osborne, The University of New South Wales.
The worsted system processes virgin fleece and skirting wools with a mean staple length of over 50mm. The WOOLLEN system however, processes (i) virgin wool of staple length less than 50mm, (ii) open and broken top from the worsted system, (iii) combing waste (noil) from the worsted system and (iv) recycled materials.
i) Short Wools:
Carding wools, consist of short wools such as lambs’ wool, crutchings, locks and prematurely shorn fleece wools. These wools are all processed on the woollen system, however it should be noted that commercial practice is to blend these wools into a homogeneous batch or consignment that will produce yarn with the count, evenness and tensile strength (tenacity) the customer requires. Lamb's wool is the only category of wool which is sometimes processed on the woollen system without blending with wools from other categories.
ii) Open and Broken Top:
Tops produced on the worsted system are sometimes reprocessed on the woollen system. The tops may be stretch broken to a specific fibre length or just opened and fed as raw material into the woollen card. Lambs’ wools are often used for this purpose to produce a final upper market product where the vegetable matter has been removed in the worsted processing system rather than in the carbonising process. The carbonising process may damage the wool, or alter the soft handle and bright colour which are features of lamb's wool.
iii) Combing waste (Noil):
Noil produced during combing in the worsted system consists of short fibres, usually less than 35mm and vegetable matter (VM). This noil is blended with other wools destined for the woollen system, carbonised to remove VM and then processed through the woollen system. The woollen system does NOT remove short fibres other than those which may be lost (e.g. as fly) during the carding process.
iv) Recycled material:
Rags, both new and old, thread waste from spinning, twisting and warping can be blended with virgin wool or other re-manufactured material or even used alone and processed through the woollen system.
New rags may be woven or knitted material and consist of waste clippings etc. from tailors, garment and cloth manufactures. Old rags are discarded garments both knitted and woven.

## Slide 5: Differences between systems: End Products
WOOLLEN - hairy, bulky, (often) heavy
e.g. Overcoats
Women’s winter skirts
Flannels
Blankets
WORSTED - lean, fine, smooth
Fine wool undergarments
Expensive men’s suits
Cool wool
Lorraine Osborne
Notes: <number>
<footer>
Written by: Ms. Lorraine Osborne, The University of New South Wales.
An important difference between the worsted and woollen processing systems is the end product produced. The worsted system produces a yarn which is lean and fine with the fibres aligned within the yarn. These yarns can be made into such garments as fine wool undergarments or expensive mens suits.
Yarns produced on the woollen system have a more random fibre array with fibres protruding above the yarn surface, giving the yarn a more hairy appearance. The garments produced on the woollen system are usually HAIRY, BULKY and HEAVY, such as overcoats, womens' winter skirts and mens' tweed sports jackets. However fine woollen knitting yarns are manufactured and this market area may increase as the trend for lighter finer garments increases.
Some of the other articles produced on the woollen system are flannels, billiard cloths, rugs and blankets. Some elite non wool animal fibres such as cashmere are also often processed on the woollen system.