## Slide 1: Blending Fibres
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module examines the technology used to blend fibre throughout the processing pipeline. The rationale for blending is explained, and some of the latest blended wool products are featured.
The processes of pre-scour blending and blending before spinning are explained.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Definition of a Blend
Intimate
  fibres fully mixed
  homogeneous sample of fibres
Separate
  within yarns
    folded (plied) yarns
    contain intimate blends
  within fabrics
    warp and weft (ortho-mixtures)
    unblended yarns
    blended yarns
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
A fibre blend can be either intimate or exist within a textile structure, such as a yarn or a fabric as a separate blend.
An intimate blend should return a homogeneous sample of fibres in the proportion of the blend if the blending has been carried out successfully. A separate blend wouldn’t achieve this if, for example, just the warp yarns were sampled in a fabric having warp yarns containing one fibre, and the weft yarns were constructed from another fibre. These type of blends have been considered somewhat outside the definition of a blend, and have been referred to as “ortho-mixtures”.
The situation can get quite complicated since each of the yarns used to make the fabric may themselves be constructed from blended strands.
Generally, a greater part of the development in wool fibre blends has concentrated on intimate blends of wool with other fibres such as cotton, nylon and lycra.
A recent notable exception is the development of Sportwool by CSIRO Textile and Fibre Technology. This is a separate blend in a knitted fabric. Pure wool yarn and pure polyester yarn are knitted so that the pure wool yarn is on the inside of the fabric next to the skin, while the polyester is on the outside of the fabric. In this way the wool does its work absorbing moisture, while the polyester can be printed. This is particularly suited to applications such as sports guernseys.

## Slide 3: Why Blend Fibres?
Peter Auer
New Products
  fibre blends
    wool / nylon
    wool / lycra
    wool / cotton
    wool / silk
    wool / microfibre
  yarn design
  fabric design
Product Evenness
  dyeing (top)
  composition
  doubling & drafting
Product Cost
  FAQ
  specified product
  least cost
Processing performance
  weaving
  dyeing
Product performance
  yarn
  fabric
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Fibres are blended for a number of reasons. The development of new products is one reason that has been to the fore in recent years. Developments such as wool / Lycra blends (about 1-2% Lycra), and wool / cotton blends (about 10 or 20% wool) have been commercialised over the last few years, although wool and cotton blending isn’t new.
These products have been developed for different reasons. Wool / Lycra blends are designed primarily to use the stretch-return properties of Lycra to enhance the wearability of wool, particularly in knitted configurations. Wool / cotton has been designed to make a softer product with enhanced thermal properties for the jeans / casual wear market.
When one considers the infinite varieties of yarns and fabrics that are available at any time world-wide, the common sense in utilising fibre blends to enhance product ranges becomes apparent.
There are more technical reasons why fibres are blended. In some countries, especially those with low levels of capital expenditure in dyeing technology, wool tops are dyed and then re-mixed after dyeing to make sure that the entire batch of tops is the same colour.
The evenness of the product could also refer to how intimate the achieved blend becomes during blending. A topmaker certainly wants to make sure that the skirtings are not discernible from the fleece wool when it is in a top.
A major route to achieving this level of intimate blending and also product evenness is using doubling and drafting. For more information see the modules “Evenness” and “Drafting”.
As discussed in the “Processing on the Woollen System” module blending may be carried out for cost reasons. The same reasoning can apply to topmaking. Topmakers are supplying a specified product at least cost, therefore they will attempt to make the most cost effective blend possible to meet their customers’ (the spinners) requirements.
The processing performance of yarns may be enhanced by blending, or it may cause concerns. Certainly a wool / nylon blend would perform better in weft insertion during weaving, however a wool/polyester blend is a more technically demanding proposition..
Some aspects of product performance were covered in the above section on fibre blends. It should be added that fibres can be blended to enhance the properties of one of the fibres in a blend. For example, Lycra is enhancing in wool/lycra, for wool / cotton blends, wool is enhancing.

## Slide 4: Where to Blend?
Peter Auer
Intimate
  pre-scouring
  carding
  gilling
  combing
  finisher gilling
  re-gilling / re-combing
    top dyeing
    synthetic staple tops
Separate
  doubling
  weaving
  knitting
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
It is reasonably straightforward to examine just where in the pipeline that fibre blending can occur. For more information see the “Textile Processes and Products” module.
There are a number of processing points before the yarn stage where intimate blending is possible. The points examined in this module are:
pre-scour blending
re-gilling / re-combing
The blending that occurs in carding, gilling and combing is thought of as secondary to the aim of fibre aligning and straightening, however this aspect of these processes will be covered in other modules.
Once twist has been inserted into an array of fibres in the spinning process, it is impossible to achieve any more intimacy in blending. Blending before this stage will be aimed to achieve intimate blends.
Therefore any blended products after the production of singles yarn would contain separate blends, e.g. a doubled yarn consisting of pure wool and nylon singles yarn.

## Slide 5: Blend Restrictions
dyeing
  reaction to heat, chemicals
finishing
  reaction to heat, water
back rollers
speed = X
front rollers
speed = 10X
FTE
FLE
Peter Auer
fibre properties
  diameter?
  length
  physical properties
    initial modulus
effect of regain
  static
  lubricants
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Before fibres can be successfully blended they must be matched in terms of several fibre properties.
Diameter is NOT a major technical issue since fibres of widely varying diameter can be successfully blended, e.g. Harris Tweed fabric, wool / mohair blends. However differences in fibre diameter may be manifested in yarn as uneven distribution in the yarn cross-section (coarser fibres tend to migrate to the outside of yarns), or in fabrics as undesirable aesthetic features such as poor appearance which can be related to the linear density evenness of the yarns themselves.
Length is the most critical fibre property that needs to be matched. The fibre length distribution in a fibre array must be such that drafting is controllable. Drafting usually occurs between two sets of rollers (the first set is slow, the second set is fast) which are set apart according to how long the longest fibres are. If the shortest fibres are relatively short they will not be well controlled and yarn evenness will be affected. If there is a complete lack of control the short fibre may cause the whole process to break down thus affecting machine efficiency.
The physical property of stiffness (more technically initial modulus), or how easily a fibre can be stretched can affect drafting as well. Imagine a fibre like elastic (Lycra) being drafted with wool. Fibre control is critical in this situation. The moduli below 2% extension is critical here, and should match. This illustrated in the next slide.
Static is always a problem in fibre processing. The moisture present as fibre regain dissipates the static charge built up through fibre / roller contact. If a fibre of low regain (e.g. polyester or nylon is being blended with a high regain fibre (e.g. wool), a lower ambient relative humidity is recommended (80% r.h. to 65% r.h.). This means that the use of an anti-static lubricant is necessary. The concentration of this anti-stat is generally higher than with a pure fibre since the presence of wool effectively reduced the level of lubricant. At 65% r.h. the order of decreasing electrostatic charge is wool > polyamide (nylon) > acrylic > polyester. It is believed that the absorption of the lubricant by the fibres is the critical factor.
Dyeing involves prolonged heating of fibres with various chemicals. The degree and length of heating are different for different fibres, therefore some blends of fibres are very difficult to dye without harming one of the fibres, e.g. for wool / polyester, wool will be damaged by the polyester dyeing conditions.
Finishing is achieved with heat and water, therefore if fibres react differently to each of these conditions they will achieve differing levels of set. A pure wool fabric would not finish the same as a wool / nylon fabric.
Note: FLE = Fibre Leading End; FTE = Fibre Trailing End

## Slide 6: Initial Fibre Modulus
Peter Auer
Source: von Bergen (1963)
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Source: von, Bergen, W. (1963), Wool Handbook, Volume 1, p.520, John Wiley & Sons, Inc.
This slide shows the stress-strain curves for wool fibres compared to polyester (including modified PET), nylon and acrylic fibres.
The final breaking strength (stress) and elongation (strain) are important components in determining yarn strength and fabric durability.
The initial modulus (slope of the line) is a measure of how stiff the fibres are at strains less than 2%. As far as fibre blending is concerned this is a critical region that equates to the level of strain that fibres undergo during flexing, bending and twisting during fibre processing and wear.
From this graph, it could be concluded that polyester and acrylic fibres match the low strain properties of the wool fibres better.

## Slide 7: Pre-Scour Blending
Peter Auer
topmaker
  spinner’s specifications
    diameter
    length
    VM etc.
  Prediction formula
    raw material costs
    variety of options, many bales
  Blending
    sorting (QC)
    blending order
    Accumulator
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The customers of the topmaker wants a top to suit their specifications as spinners. These specifications are covered in more detail in the module “Top Testing”.
The topmaker charges the spinner on a volume basis. A lot of costs are fixed. One way to optimise profits is to utilise Prediction formula, and thus meet the spinner’s specifications at least cost in terms of raw materials.
The Prediction formulae gives the topmaker a variety of options as far as raw material is concerned. The final make-up of the processing batch (consignment) will depend on supply of suitable wool, but it may be quite complex in terms of sale lots.
The trick is then to ensure that this consignment, consisting of many wool bales, returns a consistent batch of top. A vital part of this outcome is the blending that occurs before the batch is scoured.
Some topmakers use this as a quality control (QC) opportunity. The bales are laid out in an order such that the scour output will be homogenised. This can be done by experienced personnel, or by computer programs. The bales can then be individually inspected. This individual inspection was a feature of times when labour was cheaper, and so large contamination was often picked out of the bales.
Another approach is to “open” all the wool from the bales so that the bale demarcation is destroyed, and put all the opened wool in an Accumulator, which might be a machine or simply a big room. Once blended in the Accumulator the wool can then be scoured with more confidence that the scoured product will be homogeneous.

## Slide 8: Top Blending
re-gilling & re-combing
  doubling & drafting
  top dyeing
  wool tops
  tops of other fibres
wool matched to others
  cotton shorter
  standard synthetic tops
Peter Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
If gilling and combing are understood, then re-gilling and re-combing are self-explanatory. They are the same processes used at a different stage.
Tops are dyed by immersing them in hot water containing dyes and chemicals. This is a batch process. Unless the dyeing conditions are strictly controlled, it is very difficult to get the colour the same within batches of the same tops. Therefore the tops are re-gilled to maintain an even colour. They are also re-combed, since there is a certain amount of fibre breakage during re-gilling.
Re-gilling and re-combing are sometimes undertaken as a matter of course by spinners to ensure that their machines are not affected by the input material (tops). This is not that common, since it adds another process before spinning, but may be necessary if the spinner has a problem with the top supply.
Another likely scenario is that the wool top needs to be blended with another fibre. Since the wool fibre market is relatively small, it is more common for wool tops to be manufactured to suit blends with synthetic fibres. Synthetic tops are made to suit the synthetic staple yarn market, not the wool market.
In the case of matching cotton, that fibre is about 25-25mm in length. Therefore the wool must go through a process of stretch-breaking to match the fibre length properties of the cotton. For more information see the module “Textile Processes and Products”
A suitable blend is obtained by using tops of both types of fibres in the correct proportion to suit the blend, e.g. 55/45 wool/nylon would use an input equivalent to 55 wool tops and 45 nylon tops, assuming they have the same linear density. If the linear density varied, then the number of tops, or the linear density of the tops could be adjusted to suit the blend.