## Slide 1: Siroscour Technology
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
Notes: This module examines the concepts behind SIROSCOUR scouring technology which has been developed by CSIRO Textile & Fibre Technology (formerly Division of Wool Technology).
To date eight commercial Siroscour plants have now been sold, two of which are operating in Australia, three are operating in China and three are in the US. This represents about 65% of the wool scour market worldwide.
The licensee for Siroscour is Annett & Darling (ANDAR) (NZ).
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Jock Christoe, CSIRO Textile and Fibre Technology.

## Slide 2: Concepts behind SIROSCOUR
Multiple stage scouring
Contaminant recovery loops
Flexibility
Liquor flow optimisation
J. Christoe
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
SIROSCOUR scouring technology is a collection of technologies which investigates the nature of contamination and the mechanism for their removal.
The key concepts behind the Siroscour technology package are:
Multiple-stage scouring enables contaminant removal to be optimised without adverse affects on entanglement. This is achieved by making each bowl perform a specific function, and
The optimised contaminant-recovery loops have a number of specific effects:
  The scouring bowls are kept clear of accumulated contaminants allowing more effective scouring
  The efficient operation of the loops allows more efficient operation of the scour
  The wastewater from the scour is easier to treat.
  These loops represent an optimised primary treatment.
Because Siroscour involves changing the functions of the bowls, the scour itself can be operated in a number of ways depending on the type of wool. In CSIRO experience, three-stage offers the best mode of operation for a wide range of Australian wools.
The flow of scouring liquor between the bowls is not just counter-current flow from the last bowl to the first bowl as in conventional scouring. The flow pattern is arranged to optimise the use of the scouring liquors.

## Slide 3
CONVENTIONAL
Suint
Scour
Scour
Scour
Rinse
Rinse
Scour
Scour
Scour
Rinse
Rinse
Rinse
SIROSCOUR Three-Stage
J. Christoe
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
This slide compares the two forms of scouring - conventional and three-stage. Water and detergent consumptions are similar but the distribution of detergent between the bowls is very important. CSIRO recommend nonionic detergents for both methods of scouring.
Each of the contaminants of raw wool can be broadly classified as being either easy-to-remove or hard-to-remove. About 90% of each type of contaminant is easy to remove.
In conventional scouring, there are two or three scouring bowls, containing hot detergent solutions, followed by two or three rinsing bowls. In this configuration, the easy-to-remove contaminants are removed in the scouring bowls. The hard-to-remove contaminants require more time to hydrate and swell before they can be scoured. In a conventional scour there is little detergent action in the rinse bowls. Consequently, a high proportion of these contaminants is not properly removed from the wool.
Hard-to-remove contaminants not properly removed will re-deposit. Additionally, it has been discovered that if the proteinaceous contaminant layer (PCL) contaminants re-deposit they cannot be removed.
This residual contamination has implications for processing. A difference of as little as 0.2% ash or wool wax can have subtle processing implications, such as to reduce the effect of processing aids, increase wear on processing lines, and cause roller lapping.
In the Siroscour system each bowl performs a specific function. In the first stage - the desuint bowl- a high proportion of suint and dirt is removed without a concomitant removal of wool wax. In this bowl the detergent acts as a wetting agent. In the second stage, which is the first scouring stage, the easy-to remove contaminants such as water soluble material, wool wax and dirt are scoured from the wool. In the first scouring stage the detergent acts as an emulsifying agent. The first rinse bowl performs several functions. Not only does it remove entrained contaminants from the wool, but also it allows more time for the hard-to-remove contaminants to swell. In the third stage, these contaminants are scoured from the wool without being encumbered by the easy-to remove contaminants. Here the detergent acts as a traditional detergent and an anti redeposition agent.
Contaminant removal is achieved principally by chemistry rather than by brute mechanical action. This means that Siroscour technology achieves excellent contaminant removal coupled with minimal entanglement.

## Slide 4: Contaminant Recovery Loops
extended scour operation
higher productivity
more efficient detergency
  reduced contaminant levels
Sequential
  WRONZ loops
Parallel
  SIROSCOUR loops
J. Christoe
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
The contaminant recovery loops are a very important feature of a modern scouring train. They enable a scour to continue operating for extended periods without having to stop for a clean out and a subsequent loss in productivity. By reducing the levels of contaminants in the bowls, they improve the scouring process itself.
Productivity is an important aspect of the scouring operation. Since the late 1980’s scouring line production rates have increased by about 60% e.g. 1500kg/hr - 2.5 tons/hr.
These recovery loops use both dirt and wool wax recovery devices. Dirt recovery devices include settling tanks, hydrocyclones and centrifuges. Wax recovery is achieved by centrifuging.
These devices can be arranged sequentially or in parallel, which is the case for Siroscour loops.

## Slide 5: Conventional Recovery Loops
Strong Flow
Scouring Bowls
Dirt Recovery
Wax Recovery
Sludge
Recycle
J. Christoe
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
The conventional method for removing dirt and wool wax from scouring liquors is to arrange the dirt and wax recovery devices in series.
The liquor is pumped from the bottoms of the bowls into the dirt recovery device, such as a settling tank, in which dirt is removed by sedimentation.
The "clarified" liquor is then pumped to a centrifuge in which about 20-50% of the wool wax is recovered as a cream. The cream is converted to anhydrous wool grease by further centrifuging using different centrifuges.
Most of the treated liquor is returned to the scour, the remainder is discharged as a strong wastewater.
A major disadvantage of this system is that the operations of the two devices cannot be optimised together. This usually means that dirt tends to accumulate in the scouring bowls, leading to a deterioration in scouring performance and efficiency.

## Slide 6: SIROSCOUR Recovery Loops
Sludge
Strong Flow
Scouring Bowls
Dirt Recovery
Wax Recovery
Recycle
Recycle
Decanter
J. Christoe
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
One feature of the Siroscour technology is that the two recovery devices (for the dirt and the wax) operate independently. This enables the performance of both to be optimised for the take-off point in the scour and liquor flow rates.
For example, a high rate of flow from the bottoms of the bowls prevents the accumulation of any dirt in the bowls and enables all the settling of the dirt to occur in the device itself.
The feed for wax recovery is taken from a zone towards the top of the bowl where the wax concentrations are higher but the levels of grit and fibre are low.
The liquid sludges from dirt and wax recovery are then combined and fed to a decanter centrifuge that produces a spadable sludge containing about 50% solids. More than 50% of the dirt that was on the wool can be recovered in this sludge.

## Slide 7: Residual Dirt
Hauteur
Siroscour Solvent
Conventional
Suction drum Minibowl
>
>
Conventional Suction drum
Siroscour
Minibowl Solvent (De Smet)
<
<
J. Christoe
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
This overhead summarises the results obtained in a series of comparative scouring and topmaking trials. The trials were conducted at wool scours in Europe and Australia, operating under normal commercial conditions. The solvent scour used the De Smet principles. No comparative data is available for the Wooltech system.
At the outset, it must be appreciated that these trials presented a “snapshot” of the different scouring processes. Any scouring system can be operated poorly to produce an inferior product. The trends shown in this overhead combine the results for both a fleece and skirting wool lot.
In terms of cleanliness, Siroscour produced a significantly cleaner product. The suction-drum system, with its very gentle action, produced the dirtiest product. The solvent-scoured wool from the De Smet system appeared very clean, but analyses of the wool showed considerable amounts of dirt and water-soluble residues.
There are several ways of estimating the effects of entanglement introduced by the scouring process. The mean fibre length (Hauteur) of the resulting tops provides the most meaningful commercial message. Siroscour and the suction-drum system produced the longest tops whereas the conventional system which had the most severe mechanical action produced the shortest H. There was a difference of 6mm between extremes.
The same was found for the specific energy required to open the wool prior to carding (SOE). A higher SOE indicates more fibre entanglement. SOE is a measurement of the torque on a specific roller in the opening section of the card.