## Slide 1: An Introduction to Scouring
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: In this module the aims of the science of scouring are elucidated, as well as the problems which may occur during an uncontrolled scouring operation.
The types of contaminants present during scouring are discussed, and the problems the presence of residual contaminants may cause are explained.
The sequence of events leading to contaminant removal is also discussed, but this is further expanded in the module “Fundamental Processes in Aqueous Scouring”.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Scouring in ESP
Scouring
Carding
Gilling
Combing
Drawing
Scouring
Carbonising
Carding
Spinning
Spinning
Condensing
CLEANING PROCESS
INTERMEDIATE PROCESS
TOP
slubbing
Twisting
Twisting
YARN
YARN MANUFACTURE
P.Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Scouring is the only operation, apart from carbonising, which is unique to the early stage processing (ESP) of wool fibre, compared to other staple fibres. Synthetic fibres are not contaminated to any significant extent, and are not scoured.
This is not strictly true for later stage processing. For example, cotton fibre is scoured but this operation is usually performed when the fibre has been converted to fabric. The wax on raw cotton acts to protect the fibre throughout its processing route. Unfortunately the wax on wool inhibits processing to the extent that it must be removed.
This slide shows where scouring fits into the worsted and woollen processing sequences. In the worsted process, scouring occurs after the raw wool has been combined into processing batches.
The scouring operation can be part of an integrated ESP line, but may also exist as a separate operation. Scoured wool is an item of trade, and a significant portion of the Australian wool clip is traded in this form for the worsted and woollen industries.
There are two types of scouring systems:
Aqueous Scouring Systems: as the name implies these systems use water as the main component of the scouring liquor. Water also acts as the transport medium in some systems.
Solvent Scouring Systems: as the name implies these systems use organic solvents as the main component of the scouring liquor.
These are covered in more detail in the module “Scouring Systems”.

## Slide 3: Scouring Science
BALANCE
  cleanliness
  fibre entanglement (felting)
ACHIEVE
  contaminant removal
  efficiency (later processes)
WATCH
  costs
  pollution
P.Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Due to the nature of the wool fibre and its propensity to felt, scourers are faced with a contradiction when processing wool. They must deliver a product free of scourable contaminants, but also free of entanglements. To balance these requirements is the science of scouring.
Therefore scouring aims the greatest degree of contaminant removal while minimising fibre entanglement.
The level of contaminants remaining after scouring and the amount of fibre entanglement will affect the efficiency of operations later in ESP. Generally, cleanliness and fibre entanglement are opposing outcomes, i.e. the cleaner fibres become, the more entangled they are after scouring.
There are a number of approaches to this problem, embodied in technology, as aqueous scouring systems or non-aqueous scouring systems. These are examined in another module called “Scouring Systems”. Each system aims to minimise processing costs, and in a more environmentally conscious world, minimise the impact of pollution from these systems.
As far as aqueous systems are concerned, there are some fundamental processes occuring which are related to cleanliness, namely detergency, and fibre entanglement, namely felting. These are examined in the module “Fundamental Processes in Scouring”.

## Slide 4: Effect on Later Processing
Wax & other residuals
  inadequate lubricating properties
  deposits
  effect on processing additives
  effect on drafting in spinning
  effect on dye uptake
Fibre entanglement
  fibre breakage
P.Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Leaving aside the issue of VM, the residual contaminants will have effects in the following ways.
Wool wax is not a good lubricant in carding, therefore the aim is to remove as much of this as possible and replace it with synthetic lubricants to minimise fibre breakage during carding. Previous practice had been to leave a residual amount of grease (approx. 0.5%) on the fibre as a natural lubricant.
Contaminants are continually being deposited and re-deposited on the working surfaces of processing equipment (such as rollers) and the fibres themselves. When deposition exceeds re-deposition, there is an accumulation on the working surfaces. This can lead to more frequent stops, more rapid wear, and loss of processing additive. Wool wax and other residual contaminants can build up as deposits on rollers and cause machine stoppages in areas such as gillboxes and other drafting zones (e.g. roller lapping).
The presence of residual contaminants may cause increases in additive viscosity. The loss of additive means that a greater quantity needs to be applied for the same effect.
The possibility exists that changes in the level of fibre/fibre interactions may be lead to an increase in yarn unevenness, which in turn can lead to more ends down in spinning.
The amount of wool dye that is taken up by the fibre is affected by the surface condition of the fibre. Therefore dye uptake can be restricted by the presence of surface contaminants.
The amount of fibre entanglement can also be related to the amount of fibre breakage that occurs in later processing, especially during carding.

## Slide 5: Wool Damage
pH
  peptide bonds attacked at pH > 7
  yellowing > pH 9.5
  affected by suint content
Temperature
  prolonged exposure, mild conditions
Mechanical damage negligible
Properly controlled scouring should eliminate these problems
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Wool is a relatively weak fibre, compared to other staple fibres. During scouring wool undergoes various conditions which can potentially lead to fibre damage and loss of strength. There are three possible sources of fibre damage during scouring: mechanical damage, pH and temperature.
Mechanical damage will be fairly minimal since the actions of moving parts in scouring tend to be relatively gentle. As discussed, the entanglements caused by scouring will lead to subsequent breakage in carding.
Since it is a protein fibre, wool suffers a loss of tensile strength when it is wet. The nature of the protein chains in wool mean that hydrogen bonds are dissociated in aqueous conditions causing strength loss. Disulphide bonds can also be reduced in some conditions, causing further wet strength loss. This strength loss is generally reversible.
Wool can also become more susceptible to chemical damage in an aqueous medium, since the protein chains can be ionised and are attractive to small charged molecules such as acids and alkalis. Alkaline conditions (pH>7) are far more damaging than acid conditions. Conditions above pH 9.5 will cause yellowing and damage to the fibre. The alkaline nature of suint means that this is a potential source of alkalinity, therefore knowing the suint content of the wool before scouring is critical in setting scouring conditions.
Thermal degradation of wool fibre will occur with prolonged exposure to even relatively mild conditions such as those experienced during scouring. This degradation would be manifested as strength loss and yellowing.
Care must be taken to control the conditions which could lead to damage from these sources. The appropriate conditions and controls on a scour should ensure that wool damage during scouring is minimised.

## Slide 6: Wool Contaminants
Water soluble
  suint (sweat)
  stains (partly)
  Proteinaceous Contaminant Layer (PCL)
    soluble peptides
Water insoluble
  wax (grease)
    oxidised
    unoxidised
  VM
  mineral matter
  PCL
    skin flakes
The removal of ALL contaminants is not possible with any current scouring technology.
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
From an industrial point of view scouring or washing of wool could be seen as a multi-stage extraction process for removing contaminants from the wool fibre. These contaminants can be classified as water soluble and water insoluble.
Sweat or "suint" is readily water soluble. Suint is described as the potassium salt of various long chain fatty acids. It is soluble in warm water (>30°C), and can act as soap at pH >9. Therefore suint has a role as a detergent in its own right if conditions are alkaline. It has been shown that suint exists as two fractions of differing solubility.
Dried urine will also tend to be removed in the same processes as suint to some extent, although the occurrence of permanent urine stain is the single largest component of dark-fibre contamination.
In the last decade or so the presence of a further contaminant has been demonstrated. This was called the proteinaceous contaminant layer (PCL), and consists of mainly skin flakes and soluble peptides. Significantly the PCL is water soluble and water insoluble.
Wool grease is a misnomer, since the absence of glycerides or fats in analyses of this component classify the substance as a wax. It largely consists of the fatty acid esters of long chain alcohols, with a small amount of free fatty acid and free cholesterol. Wool wax exists as a solid or semi solid with a melting point around 43°C in a stable film around the fibre. Importantly there is an oxidised portion (mainly at the fibre tip) and an unoxidised portion (purest at the base of the fibre) present, which presents difficulties for the scourer. The role of oxidised grease in forming complexes with various other contaminants such as PCL and dirt has consequences both for contaminant removal and effluent treatment. While oxidised grease only forms 5% of the total, a complex containing oxidised grease acts as if it is all oxidised.
Vegetable matter (VM) and animals such as ticks and lice are also present in raw wool. These are largely removed in carding, although the moisture content of the scoured wool has a bearing on VM removal.
Mineral matter such as dirt dust and sand are acquired contaminants which exist in varying quantities depending on the source of the wool.

## Slide 7: Wool Contaminants
P.Auer
Easy to remove
  unoxidised wax
  most oxidised wax
  readily soluble suint
  loose dirt
Hard to remove
  fraction of oxidised wax
  slowly soluble suint
  sub-micron dirt
  adhering skin flakes
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Another way of thinking places the contaminants into two fractions: an easy-to-remove fraction and a hard-to-remove fraction.
The former includes the unoxidised grease, most of the oxidised grease, readily soluble suint and loosely held mineral, organic and proteinaceous dirt.
Harder to remove are a small fraction of the oxidised grease, slowly-soluble suint, submicron mineral dirt and proteinaceous flakes adhering to the wool.

## Slide 8: Contaminant Removal Sequence
  Aqueous Process
Penetration of wax
Swelling of wax
Formation of Globules
Removal of easy-to-remove complexes
Partial removal of hard-to-remove complexes
P.Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
The sequence thought to be followed during contaminant removal is as follows:
Penetration of the grease by water and surfactant followed by rapid swelling of both grease and proteinaceous contaminants (some micelles, or detergent globules, may form dissolving some oxidised grease).
Formation of grease globules (unoxidised in particular) within the swollen mass.
Removal of the complexed and uncomplexed easy-to-remove contaminants which are not strongly bound to the fibre surface.
Partial removal of the hard-to-remove contaminants such as swollen proteinaceous contaminants adhering to the fibre along with associated complexed grease and suint.
This sequence indicates that not all contaminants are amenable to removal, and that the roles of oxidised grease and PCL are significant in the non-removal of contaminants.
This sequence can be seen more clearly in the module “Fundamental Processes in Aqueous Scouring: Detergency, Felting”. How this sequence is applied to scouring technology can be seen in the module “Scouring Systems”, as well as the “Siroscour Technology” module.