## Slide 1: Fundamental Processes in Aqueous Scouring: Detergency & Felting
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Peter Auer, The University of New South Wales.
Notes: This module examines two processes that are fundamental to aqueous scouring, detergency and felting.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Peter Auer, The University of New South Wales.

## Slide 2: Detergency
removal of soil
Soil
  wax
  particulate matter
Substrate
  wool fibre
requirements
Surfactant
Wetting
Agitation
Prevent re-deposition
  emulsion
  suspension
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Detergency is integral to aqueous scouring. It is aimed at removing contaminants by the action of surfactants. The contaminants are then kept off the fibre in various states such as emulsions and suspensions. These activities in context are related to the Contaminant Removal Sequence outlined in the module, “An Introduction to Scouring”.
Essentially detergency involves the removal of soil from substrates. In the case of wool scouring the soil involved is the wool wax, and particulate matter such as dirt and skin flakes. The substrate cleaned is the fibre.
The requirements to achieve detergency in the case of aqueous wool scouring are surfactants, wetting of the surfaces (fibre, wax, soil), some form of agitation and mechanisms to prevent the soil re-depositing on the substrate.

## Slide 3: Surfactants
P.Auer
tail
head
hydrophilic
hydrophobic
non-ionic head
tail
head
CH CH O
2
2

CH CH O
2
2

CH CH O
2
2

CH CH O
2
2

Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales..
Surfactants are chemicals with special properties. They are long chain molecules in two parts, usually designated as a head and a tail. The tail is completely non-polar, which means that by themselves the tails have no attraction for water, a polar molecule. In fact in the presence of water the tails will want to stick together. This means that the tail is hydrophobic. The head of a surfactant molecule is polar, and therefore will experience some attraction for water. The head is hydrophilic.
If the surfactant is soap, there is a full negative charge on the head. This would be called an anionic surfactant. The head would be small and compact. This is represented at the top of the slide.
The head of a nonionic surfactant is relatively long and doesn't have a full charge but has many localised charges along its length. In effect though, the head is slightly polar and has an attraction for water. This is represented in the middle of the slide.
Generally non-ionic surfactants make the best detergents, mainly due to their dispersing properties and the fact that they are not affected significantly by hard water and temperature.
The most popular detergent used in the wool industry today is Lissapol TN450. This is a condensate of nonyl phenol with 8.5 moles of ethylene oxide. This means the head has on average 8.5 molecules of (CH2CH2O). The presence of oxygen causes localisation of the electrons along the head.
The presence of a benzene ring in the structure of Lissapol TN450, means that it takes slightly longer to biodegrade than a completely linear surfactant. While this may be a problem in colder climates, the milder conditions in Australia mean the difference is not critical. Nevertheless there has been some substitution of Lissapol TN450 with a similar, more biodegradable product called Softinol.
In summary, surfactants are molecules in two parts, one is attractive to water (hydrophilic) and the other part doesn’t like water (hydrophobic). These chemicals have special properties in water.

## Slide 4: Suspension of particles
dirt
fibre
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
This slide deals with the function of these surfactant molecules in water.
Firstly, if there is a surface or interface present e.g. between grease and water, or between dirt and fibre, the surfactant molecules will preferentially orientate at the interface, due to the differing polarities of the head and the tail. This is called surface activity.
The surfactant is said to be adsorbed at the interface (i.e. aligned but distinct). It can occur at any interface, e.g. between grease and water, between fibre and water, between dirt and fibre. The effect of adsorption is that the surface is expanded and the surface or interfacial tension is lowered by the presence of surfactant molecules. One outcome of lower interfacial tensions is that surfaces are easier to wet. Surfaces must be wet for detergency to occur. This certainly helps wool which has a hydrophobic surface.
Secondly, the heads of an ionic surfactant molecule will repel each other, because they have the same charge. This means that two surfaces coated with preferentially orientated surfactants will repel each other. This effect is greater for anionic surfactants due to their full negative charge, but still occurs with non-ionics to a lesser extent. This repulsion means that less work is required to separate the surfaces, and remove the contaminants.
Furthermore, the materials will be easier to keep separate or suspended with a surrounding adsorbed layer. For anionics this suspension is maintained through electrical repulsion. However the mechanism for non-ionics is more one of steric hindrance, i.e. the particles are separated by the coating of surfactant.
It is important to note that some form of agitation is necessary to dislodge the particles.

## Slide 5: Emulsion of wax in micelle
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Another phenomenon is that above a certain concentration of surfactant the molecules form clusters. Above this critical concentration the surfaces are crammed with surfactant but the surfactant is still in solution. The surfactants aggregate to form clusters called micelles.
These clusters can be viewed as a drop of liquid hydrocarbon, the tails of the surfactants forming the centre of a sphere covered with charged heads. This is represented in this slide.
Significantly for the emulsion of wool wax, non-polar materials can be dissolved inside the centre of the micelles. So the micelle is a stable structure which effectively removes the wax from the fibre by emulsifying it. An emulsion is stable in the prevailing conditions in a scour.

## Slide 6: Contaminant Removal Sequence
wax
fibre
P.Auer
Notes: Written by: Dr. Peter Auer, The University of New South Wales.
Detergency is a complex phenomena involving wetting, adsorption, suspension and the dissolving of nonpolar material in micelles.
This slide represents the sequence which is thought to occur during contaminant removal in aqueous scouring.
Firstly the fibre is covered in wax and dirt. The addition of water is insufficient to dislodge the dirt, mainly due to inefficient wetting and high surface tensions involved. However, the addition of hot water above the melting point of the wax makes it pliable and allows access to the surfactants.
When detergent is added it is adsorbed at all surfaces with the hydrophobic tails oriented to the surfaces. The interfacial tension are lowered aiding wetting and the spreading of surfactants.
Once adsorption is sufficiently advanced, the surfactant heads act by mutual repulsion and lower the adhesion between the soil and the substrate. During the swelling period, liquid grease tends to form into globules or balls due to the lower interfacial tensions caused by the surfactants.

## Slide 7: Contaminant Removal Sequence
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
When agitation is applied to the system the dirt and grease are dislodged into the bulk of the scouring medium or liquor. The soil remains suspended due to the adsorbed surfactants acting to make stable emulsions and suspensions.
Therefore the bulk of the contaminants are disassociated from the fibres and become part of the scour liquor.
The wax tends to stay emulsified and must be separated from the aqueous solution to alleviate pollution concerns.
The dirt tends to settle out of the liquor over time to the bottom of the scour vessel where it can be removed and separated as well.
A proportion of dust is not associated with the wax. This loose dust can be shaken out before scouring, or will tend to be washed off during scouring and settle in bottom of the scour bowls.

## Slide 8: Felting Requirements
fibre configuration
    freedom to move
    contact with other fibres
    opposed scales
water
  not essential but promotes felting
    lubricant
    scales raised
    flexibility increased
agitation - essential
DFE - essential
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
The next fundamental process in scouring is felting. Felting in a mild form is classified as fibre entanglement. In its most severe form it is actually the basis for a number of non-woven wool products such as felts. A mass of wool fibre can be felted to such an extent that the final dense mass can be cut with a saw.
Considering the essential requirements for felting, it is no surprise that this is a cause for concern in aqueous scouring.
Fibres need to have freedom to move and be in contact with other fibres. Once the staple structure has been broken down this is achieved and also, the scales can achieve an opposed configuration.
Water acts as a lubricant in a felting system allowing the fibres to move past each other. Wool also absorbs water which has the tendency to raise the scales of the fibre, and also increase the flexibility of the fibres.
Agitation is necessary to achieve relative movement of the fibres past each other. Even though the agitation in scouring is relatively gentle, it is still sufficient to cause a degree of felting.
A feature of all animal fibres and some textured synthetic fibres is the Directional Friction Effect (DFE). Essentially this means that the coefficient of friction against the scales is greater than the coefficient of friction with the scales.
Mathematically DFE is expressed thus:
DFE = µa - µw
µa + µw
where
µa is the coefficient of friction against the direction of scale
µw is the coefficient of friction with the direction of scale
Therefore if µa and µw were equal the DFE would be zero.
This concept is illustrated on the following slide.

## Slide 9: Directional Frictional Effect
fibre 1
fibre 2
ROOT
ROOT
fibre 2 moves to ROOT end
fibre 1
fibre 2
fibre 1
fibre 2 extended
P.Auer
Notes: <number>
<footer>
Written by: Dr. Peter Auer, The University of New South Wales.
Two fibres in proximity are labelled Fibre 1 and Fibre 2. The root end of the fibres are indicated. Adjacent scales are marked by white and red triangles.
In the second illustration Fibre 2 is extended by some form of mechanical agitation. Imagine that one end of the fibre is trapped by other fibres not shown. The adjacent scales are now separated.
In the third illustration, Fibre 2 is relaxed, but the fibre is prevented from returning to its original position relative to Fibre 1 by the fibre scales. Fibre 2 has effectively migrated relative to Fibre 1 in the direction of the root of Fibre 2.
This scenario is not possible when the wool is retained in a staple structure since the fibres in a staple are all oriented the same way. The scales must be opposed for this effect to happen.