## Slide 1: Fibre Entanglement in Scouring
Produced for the CRC for Premium Quality Wool undergraduate program by;
Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
Notes: Fibre entanglement leads to a loss in fibre length, an increase in combing noil and a decrease in the clarity of the card web due to nep formation. This module explores the concept of “working points” in a scour to explain where fibre entanglement may occur in an aqueous scour. Solutions to the problem of entanglement and its reduction are reviewed.
Produced for the CRC for Premium Quality Wool undergraduate program by Dr. Jock Christoe, CSIRO Textile and Fibre Technology.

## Slide 2: Working Points in an Aqueous Scour
1. SPRAY BOX
2. DUNKERS
3. RAKES
4. BOWL LEVEL
5. WOOL
TRANSFER
6. SQUEEZE
7. CONVEYOR
false bottom
J. Christoe
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
Using the analogy of working points in carding to open the wool, CSIRO Textile and Fibre Technology (TFT) have developed the concept of working points in wool scouring to explain how wool becomes entangled in a scouring line. Once entanglement is introduced it cannot be removed. As the wool proceeds down the scouring line the entanglement will not be reduced.
The severity of entanglement induced in the scouring process is a function of the severity of each working point coupled with the number of working points.
The working points include:
the method of feeding the wool to each bowl,
the dunkers
the transport mechanisms in the bowls
the way in which wool flows out of each bowl
the means used to assist this out-flow
the squeeze rollers
the conveyors between the bowls and,
the wet opening process if there any prior to the dryer.
All these points have the potential to entangle the wool. In fact, compared to the methods used to create felts, there are similarities to the actions occurring in a wool scour, albeit at much lower levels of intensity.

## Slide 3: Bowl Feed
Spray Box
  wool pushed into bowl
  turbulence
Dunkers
  wetting out
  push down and forward
  turbulence
J. Christoe
Notes: Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
As the wool falls off the interstage conveyor, it is pushed into the bowl by the recirculating scouring liquor being pumped into the bowl through the spray box. If this flow is turbulent it will encourage entanglement.
Dunkers are used to wet out and submerge the wool as it enters a bowl. In some scours they may be positioned along the bowl to improve the scouring action. However, in pushing the wool down and forward before releasing it, the wool can be given a very turbulent treatment. This up and down mechanical action encourages fibre entanglement.

## Slide 4: Wool Transport
J. Christoe
METHODS
rakes
  swing rakes
  harrows
  triple-crank rakes
suction drums
  floating mat
ENTANGLING ACTIONS (rakes)
general turbulence
needle felting
jagged motion
Notes: Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
There are four methods used to transport wool through a bowl, namely swing rakes, harrows, triple-crank rakes and suction-drums.
The last of these systems was developed by Fleissner GMB. In this system the wool mat essentially "floats” across the water before being sucked onto perforated suction-drums.
The other transport systems use pins or tines to push the wool through the scouring liquor. One could argue that they are simply the mechanisation of the actions of pitchforks that were used in the early scouring systems. The swing rake has a very severe action that most closely resembles the action of a pitch fork. Consequently, they have a great propensity for fibre entanglement.
Most modern scouring lines use triple-cranks. The degree of induced entanglement is probably less than the harrow action because they are able to be more smoothly driven.
There are three entangling actions that are associated with any rake system:
(1) general turbulence through pushing the wool through the scour;
(2) “needle felting” caused by individual tines as they penetrate the wool mat thus pushing pieces of wool through the mat. This analogous to needle punching nonwoven webs;
(3) if the motion of the rakes is not smooth, the wool is subjected to a jagged motion which is analogous to the action of felting machines for the hat industry.
The arrow on the slide indicates the direction of increasing entanglement, swing rakes being the worst.

## Slide 5: Squeeze Rollers
J. Christoe
Transfer to Nip
  wool pushed
  water level high
Methods
  Belgian lifts
  swing rakes
  head rakes
  main rake extensions
At the Squeeze Nip
  stuffer box effect
  turbulence
    major contributor
Notes: Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
At the end of a bowl the wool is pushed up an incline of the false bottom until it reaches the breast from which it descends to the nip of the squeezing rollers. At the nip, foam may develop which can cause fibre entanglement.
A major contributor to entanglement in the modern wool scour can be at the squeezing rollers where water is being pushed through the wool. The wool is being held at one end, allowing the free end of the fibre to move and entangle with new fibres coming through.
Some scourers believe that the water level in the bowl needs to be adjusted so that the flow of the scouring liquor over the breast carries the wool with it. Others believe that the level should be adjusted so that the wool flowing down the incline to the nip of the squeezing rollers should contain as little water as possible.
In the latter case there is a very high potential for entanglement because the mechanical system for transferring the wool over the breast is essentially that of repetitively pushing the wool as a mat for some time until it topples over and down into the nip.
Most scouring lines have a separate mechanical system to the main rakes for transferring the wool from the bowl to the squeezing rollers. Like the main rakes these have differing degrees of severity. In order of decreasing severity, these include Belgian lifts (old system like pitch forks), swing rakes (similar to Belgian lifts only level with the bowl), head rakes and extensions to the main rakes (this was common with harrows in which the tines were progressively shortened to allow the wool to be pushed up the incline of the false bottom). The arrow indicates the severity of the action.

## Slide 6: Entanglement Reduction
J. Christoe
Modify existing machines
Radical changes to the scouring machines
Change the scouring medium
  aqueous
  solvent
    de Smet
    Wooltech
Change the scouring configuration
  Siroscour
Notes: <number>
<footer>
Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
This slide lists four ways by which entanglement can be reduced. The first two methods reduce entanglement by decreasing the amount of mechanical energy imparted to the wool during scouring. The third method reduces entanglement (in theory) by replacing the aqueous scouring environment with one that does not enhance the differential friction effect nor render the fibres more flexible (i.e. solvent medium).
One must remember that the main purpose of scouring is to remove contaminants to acceptable levels of residual contaminants. This limits the extent that one can change the scouring configuration. From an entanglement point of view, the best configuration would involve no agitation or one in which the wool is overly restrained. Looking at these ways in more detail:
Modification of existing machines
The principle here involves reducing the number of working points for example by shortening the bowls or changing the dunkers. Minibowl scours are a good example of this approach.
Radical changes to scouring machines
In this case the principle involves eliminating working points, for example by conveying the wool through washing zones using porous conveyors or drums. Because of the gentle action and the way the wool is held, it retains higher levels of residual dirt. Three systems have been developed: (1) CSIRO jet scouring machine (the wool is sprayed with alkaline detergent solution while supported by porous conveyors); (2) UNSW jet scouring machine (the wool is sprayed with alkaline detergent solution while held on porous drums); (3) Fleissner Suction Drum System
Changing the scouring medium
Examples in which solvents are used to wash the wool include the De Smet (Solvent) process in which wool is sprayed with both hexane and an isopropanol/water mixture and the Wooltech process in which wool is washed in trichloroethylene. A Wooltech plant operates in Trieste, Italy. Organic solvents need to be carefully managed to overcome potential environmental and occupational health and safety problems. High levels of solvent encourage micro entanglements. Whilst in aqueous scouring temperature, pH levels and mechanical action cause entanglement.
Changing the scouring configuration
In this approach, chemistry rather than mechanical action is to used remove the contaminants. The best example of this is Siroscour and three-stage scouring.

## Slide 7: Fibre Effects in Scouring
Diameter (decrease)
  higher detergent concentration required
    more surface area
  more entanglement possible
    more fibre / fibre contacts
Crimp Frequency (increase)
    associated with diameter decrease
  more entanglement
    more fibre / fibre contacts
Crimp Definition (increase)
  less entanglement
J. Christoe
Notes: Written by: Dr. Jock Christoe, CSIRO Textile and Fibre Technology.
There are also a number of fibre properties that can have an effect on the level of fibre entanglement during scouring.
Diameter is critical as far as fibre entanglement is concerned. For instance, the New Zealand 32 µm plus wools have no entanglement problems during scouring whilst great care is required with Australian superfine Merino wools to limit fibre entanglement.
For a given unit mass, the finer wools have a greater surface area, more wax and dirt, a greater number of fibres. Finer wools require a higher detergent level to clean them. The biggest problem being the removal of wool wax.
The level of fibre crimp can also have an effect. For a given volume, finer wool will have more fibre / fibre contacts which would encourage entanglement.
The degree of fibre alignment before scouring can also have an effect. Poorly aligned fibres already have a degree of fibre entanglement before scouring begins.