## Slide 1: Wool Colour and Fleece Rot Topic 4
Notes: Prepared by S.I. Mortimer, NSW Agriculture.
This topic describes greasy colour of fleece wool on the sheep in the context of two types of unscourable discolourations that develop under certain conditions of moisture, temperature and bacterial activity, namely yellow discolouration and fleece rot.
The colour of greasy Merino wool can vary. It varies from near white through to shades of cream and yellow, with intense yellow discolouration in greasy wool known as ‘canary stain’. Yellow discolouration results from chemical reactions occurring within the fleece under the influence of moisture, temperature and bacterial activity. Due to moisture and bacterial activity at skin level inducing fleece rot, other discolourations can often occur. Discolouration can range from red, orange, pink, violet and blue as well as the more usual discolourations of yellow, grey, brown and green.

## Slide 2: Average discounts for colour grades in Merino fleece wool
 | Superfine | Fine | Medium | Broad
 | 17-18.5µm | 18.6-20.5 µm | 20.6-22.5 µm | 22.6-25 µm
H1, light unscourable | -3.1% | -2.1% | -1.1% | -0.8%
H2, medium unscourable | -5.8% | -5.8% | -4.1% | -3.6%
H3, heavy unscourable | -8.9% | -8.8% | -8.4% | -8.2%
Source: Australian Wool Innovation 2004
% discounts relative to wool that has no unscourable colour during 2001/02 to 2003/04 auction season
Notes: Prepared by S.I. Mortimer, NSW Agriculture.
Wool colour will influence the price achieved for a sale lot under the auction system. Wool is discounted if it is perceived to have an ‘unscourable’ colour as the type of products the wool can be used for and dyed is expected to be more limited. Wools that scour ‘white’ can be dyed any colour, including pastel shades. In contrast, wools with increasing degrees of yellowness after scouring are more difficult to dye pastel shades and therefore have more limited end uses.
Before sale, greasy wool is appraised visually as being either scourable or unscourable, with wools considered unscourable graded for the degree of discolouration present based on the AWEX-ID system. Wool with scourable colour will be creamy-white after scouring (washing to remove impurities). Wool with unscourable colour will be off white or yellow after scouring and subsequently discounted. The AWEX-ID system provides three grades for appraising greasy wool discolouration: H1, light unscourable colour; H2, moderate unscourable colour; and H3, heavy unscourable colour. An additional category, N1 (light water stain) is provided for bacterial discolouration and water stain. The table shows the average discounts for the unscourable colour grades in a range of Merino wool types over the last three full wool auction seasons (2000/01 to 2002/2003). As discolouration increases, the level of discount increases. As well, discounts are greater as wool type becomes finer. Greasy wool colour is of greater economic importance to fine wool production as compared to broad wool production.

## Slide 3: Measured wool colour
Two components:
  brightness (reflectance)
    Y value: as Y , brightness 
  yellowness (colour)
    Y- Z value: as Y- Z  , yellowness 
Usually measured as clean colour (i.e. after scouring)
Greasy colour may or may not be scourable
Greasy colour, either measured or visually assessed, weakly related to measured clean colour
Notes: <number>
<footer>
<header>
<date/time>
Prepared by S.I. Mortimer, NSW Agriculture and based on material prepared by B.J. Crook, University of New England.
Both greasy and clean scoured wool can be objectively measured and described by the components of brightness (the opposite of dullness or greyness) and yellowness (to provide a scale from white through to intense yellow). Wool colour is determined using a spectrophotometer or a colorimeter. Colour measurement systems allow colours to be represented by a mixture of three defined colours (notionally red, green and blue) expressed by the derived tristimulus values X, Y and Z. In wool colour measurement, the Y value is indicative of brightness and the Y-Z value indicative of yellowness. Brightness of wool increases as Y value increases and its yellowness increases as Y-Z value increases. The colour is best described in yellowness (Y-Z) units, which can range from 7 to 18 units. Most Australian fleece wools have Y-Z values between 7 and 12 units.
Greasy wool colour has been shown to be a poor predictor of clean wool colour following scouring. Measured clean colour is related weakly to both measured greasy colour and visually assessed greasy colour. This indicates that discounts applied on the basis of a visual appraisal of greasy colour may not always be justified, as some wool perceived as being discoloured could often produce clean white wool after scouring. Where greasy wool colour is appraised as unscourable for a sale lot, measurement of clean wool colour could be useful in reducing the size of price discounts applied to that wool. While greasy sale lots can be measured for clean wool colour, much less than 10% of fleece wool sale lots are measured currently for this trait.

## Slide 4: Development of yellow wool discolouration
also microbe-specific pigments (e.g. red, blue, green, brown) occurring in bands
Decomposition of fibre keratin
  exposure to UV light (sunlight)
  heating
  alkaline conditions (high pH)
Reactions among non-fibre components of the fleece
  chemical reactivity of suint components
  by-products of microbial activity
Notes: <number>
<footer>
<header>
<date/time>
Prepared by S.I. Mortimer, NSW Agriculture and based on material produced by B.J. Crook, University of New England.
Yellow discolouration in wool can occur irrespective of whether wool is on the sheep in the paddock or in shorn greasy, semi-processed or final fabric form. Yellow discolouration can develop due to decomposition of the fibre protein as a result of exposure to ultra-violet light, sustained high temperature and alkaline conditions. However, the natural yellow discolouration that can be seen in some fleeces in the paddock is generally the result of a series of chemical reactions among non-fibre components occurring within the fleece under the effects of certain environmental conditions (moisture and temperature) and bacterial activity.

## Slide 5: Reactions involved in wool discolouration: Maillard reaction
Potassium salts of various carboxylic acids in suint are metabolised by bacteria
Simple carbohydrates (e.g. glycolaldehyde) are derived
These carbohydrates react with amino acids in “yolk” and skin debris to produce yellow discolouration
Wool fibres absorb discolouration, leading to unscourable colour
Notes: <number>
<footer>
<header>
<date/time>
Prepared by S.I. Mortimer, NSW Agriculture.
One of the reactions involved in wool discolouration is the Maillard Reaction, a ‘browning’ effect that results from the interaction of reactive carbohydrates and proteins within the fleece. It was demonstrated when white Merino wool was induced to discolour after being placed into solutions of the reactive carbohydrates, glyceraldehyde or glycolaldehyde.
Within the normal fleece environment, a Maillard reaction involving non-fibre proteins within the fleece occurs following the generation of reactive carbohydrates as a result of the metabolism of suint components by bacterial populations within the fleece. Suint consists mainly of potassium salts of various carboxylic acids. The Maillard reaction occurring in the fleece can be described as follows:
1. Simple carbohydrates such as glycolaldehyde are derived from the metabolism of potassium salts of various carboxylic acids in the suint by bacterial populations on the skin surface.
2. These carbohydrates react with amino acids within the yolk of the fleece and skin debris to produce yellow discolouration.
3. Wool fibres absorb the yellow discolouration.

## Slide 6: Other reactions involved in wool discolouration
Formation of carbonates and bicarbonates by bacterial activity also occurs as reactive carbohydrates are produced
  as fleece becomes more alkaline, wool fibres more prone to decomposing and absorbing yellow discolouration
Deamination of amino acids: bacteria may degrade skin and “yolk” proteins to amino acids, producing ammonia
  potassium may act as a catalyst in this breakdown
  potassium may aid the speed of absorption of yellow pigments associated with discolouration
Notes: Prepared by S.I. Mortimer, NSW Agriculture.
Other reactions within the fleece are involved in wool discolouration. During the production of the reactive carbohydrates, the bacterial activity also generates carbonates and bicarbonates, causing a rise in the pH of the fleece. As conditions become more alkaline, the wool fibres become more susceptible to decomposing and absorbing the yellow discolouration present in the yolk of the fleece. Also, the bacterial population is implicated in wool discolouration via the formation of ammonia following degradation of the non-fibre protein components of the fleece. During this process of bacterial deamination of amino acids, potassium present in the suint is likely to act as a catalyst. Additionally, the potassium component may possibly increase the rate of absorption of discolouration into the fibre.
Given these possible reactions, the following factors are likely to be important in determining the level of yellow discolouration present in wool:
1. Suint content of the fleece, influencing the concentration of reactive carbohydrates (derived via the Maillard reaction) and carbonates and bicarbonates (effect of more alkaline conditions) and total amount of potassium present.
2. Potassium concentration in the suint, influencing the bacterial degradation of amino acids that produces ammonia (deamination).
3. Bacterial activity, influencing the rates of production of reactive compounds.
4. Temperature and moisture, influencing the size of the bacterial population and rate of bacterial activity.

## Slide 7: Yellow wool discolouration
expression of discolouration depends on warm temperatures and high humidity
  chemical reactivity
    temperature dependent e.g. Maillard reaction
  microbial activity
    moisture and temperature dependent
  rate of colour absorption by fibre
    faster in wet conditions than in dry
Notes: Prepared by S.I. Mortimer, NSW Agriculture.
As a combination of moisture and warm temperature is required for discolouration to occur, susceptible sheep can only express their propensity to discolour if the environmental conditions are conducive to the development of discolouration. Observation and recording of discolouration in sheep is then not always possible. There are a number of implications of this for Merino breeding programs:
1. The emphasis given to wool colour in a breeding program is likely to vary with location, where greater emphasis is likely in environments characterised by a summer-dominant rainfall pattern (providing conditions of moisture combined with warm temperatures).
2. Susceptible animals cannot be assessed and identified for culling unless seasonal conditions favour the development of discolouration.
3. If wool colour is in the breeding objective, selection and purchase of rams in a breeding program will need to consider the environmental conditions under which the rams are raised as compared to those environmental conditions under which their progeny would be born. As a result of genotype by environment interaction, progeny may only express their propensity to discolour only under certain environmental conditions.

## Slide 8: Fleece traits associated with yellow wool discolouration
Yellow wool discolouration can be expressed
  naturally in the fleece
  induced in greasy wool samples in an incubated colour test
Fleeces resistant to discolouration tend to have
  lower suint content and potassium content of suint and less alkaline suint
  higher wax/suint ratio
  lower fibre diameter
Notes: Prepared by S.I. Mortimer, NSW Agriculture.
A procedure has been developed whereby a greasy wool sample is artificially challenged to induce yellow discolouration. The procedure involves incubating the sample at both high temperature (40OC) and humidity for 1-7 days. This incubated colour test simulates the environmental conditions necessary to induce discolouration in susceptible fleeces. Following incubation, the development of colour is scored on a scale from 1 (bright and white) to 5 (dark brown/yellow discolouration). The procedure is used to assess the development of discolouration by measuring the absorbance at 430 nm on a colour extract taken from the wool samples following incubation. Under this approach, susceptibility to yellow discolouration increases as absorbance increases. Each of the traits associated with susceptibility to yellow discolouration has been shown to be correlated strongly (at the phenotypic level) with the level of discolouration developed under the incubated colour test. Fleeces resistant to discolouration show a lower level of suint (as a percentage of greasy sample weight) and a lower concentration of potassium in the suint and a less alkaline suint. Fleeces resistant to discolouration may also tend to be of lower fibre diameter and higher yield. Wax/suint ratio, but not wax content, is associated with yellow discolouration, with resistant fleeces tending to have higher ratios.
As there is little economic incentive for its use in Australia, little commercial use of the incubated colour test has occurred in Australia, with more attention given to its application in New Zealand.

## Slide 9: Development of fleece rot
Bacteria present on
normal skin
Proliferation of bacteria
Production of pigments
(bacterial stain)
Predisposition to blowfly strike
Fleece rot
Warm and moist conditions
(prolonged wetting of skin)
Serous exudate
from skin
Dried crusts adhering
to wool fibres
Notes: Prepared by S.I. Mortimer, NSW Agriculture and based on material produced by B.J. Crook, University of New England.
Fleece rot is a skin disease that develops in the fleeces of susceptible animals after prolonged wetting and bacterial proliferation at the skin level. It is best described as a mild superficial dermatitis. Other names for fleece rot include ‘water stain’, ‘weather stain’, ‘water rot’, ‘wool rot’, ‘pink rot’, ‘cakey yolk’ and ‘dead yolk’.
Fleece rot develops following prolonged wetting of the fleece that results in moisture at skin level. The presence of free moisture on the skin causes a breakdown in the wax layer on the skin and the release of serous exudate that matts the fibres together in bands. The serous exudate provides a medium for the growth of a range of bacteria, including Pseudomonas aeruginosa. The bacteria usually produce pigments that stain the fleece in well-defined bands, so that most forms of fleece rot are associated with bacterial stain. The colour of the resultant stain is dependent on the various bacteria present in the fleece. For example, P. aeruginosa usually produces a blue-green pigment (pyocyanin). The serous exudate eventually dries into a crusted band which is characteristic of fleece rot. Bacterial staining without skin exudation is not considered exudative fleece rot but the condition of weather stain.
The economic impact of fleece rot in a flock is evident in reductions in wool production and quality and in deaths of animals or the need to cull animals affected with fleece rot. For a given incidence of fleece rot, a proportion of animals with fleece rot will have fleeces or areas of the fleece that are discoloured (with unscourable colour) and/or tender leading to a reduced value of the wool as discounts for these faults are incurred.
Fleece rot also has economic consequences because of its role as a major pre-disposing factor influencing the development of body strike in susceptible Merino sheep. The bands of serous exudate and the odours produced during fleece rot development are highly attractive to gravid (pregnant) sheep blowflies (namely Lucilia cuprina). The serous exudate also provides ideal conditions for egg laying and hatching and subsequent larval growth.
Fleece rot can result in unscourable colour.

## Slide 10: Sheep traits associated with fleece rot
Resistant sheep tend to have
  lower average diameter and diameter variation
  longer, thinner staples of lower crimp frequency
  lower wax/suint ratio
  whiter fleeces
Conformational faults of the withers
  high shoulder blades, broad withers and ’pinch’ behind the withers increase susceptibility
Age of sheep
  adult sheep more resistant
Notes: Prepared by S.I. Mortimer, NSW Agriculture.
Amount of rainfall, bacterial activity, age of sheep and flock management will influence the incidence and the severity of fleece rot in a flock. Young sheep (less than 12 months of age) are more severely affected by fleece rot than adult sheep, so that culling of affected young animals can improve a flock’s level of resistance to fleece rot. Sheep with 4-6 months wool growth are most susceptible to fleece rot during critical times of the year. Strategic timing of shearing is important to consider if periods of prolonged rainfall are likely to coincide with sheep having 4-6 months wool growth. Also, lamb shearing (tipping) could increase the susceptibility of young sheep to fleece rot.
A number of fleece, skin and immunological characteristics of sheep within a flock have been studied for their association with fleece rot. These studies show that the phenotypic correlations are small (range between 0.3 and –0.3) and often inconsistent in the direction of the association. The characteristics studied should be used carefully to identify animals for culling due to their relative inefficiency as predictors of fleece rot resistance. However, the fleeces of more resistant animals have: whiter colour; longer, thinner staples of higher crimp frequency; lower average and variability of fibre diameter; higher wax content; lower suint content; and higher wax/suint ratio. Factors that are components of fleece structure (e.g. average and variability of fibre diameter) will influence fleece wettability and the retention of moisture in the fleece.
Sheep classers are able to grade animals resistant to fleece rot within a flock, with the phenotypic association between predicted and observed fleece rot ranging between 0.05 to 0.39. Visual fleece and skin traits used by sheep classers include handle, crimp, fibre diameter, staple length, staple thickness and its uniformity, staple tip formation, greasy fleece colour, fleece condition and yield, fleece density, and the skin’s thickness, tone and texture. Conformational faults of the withers on the sheep increase the susceptibility of sheep to fleece rot. These faults include high shoulder blades, broad withers and ‘pinch’ (an abnormal narrowing which may be seen as a depression) behind the withers.

## Slide 11: Variation in fleece rot incidence in Merinos
Strain differences are large
  resistance increases from strong to medium to fine wool Merinos
  differences increase as average incidence of fleece rot increases
Bloodline within strain differences are large
  resistant bloodlines tend to have finer fibre diameter, better style and colour but lower fleece weight, body weight and shorter staples
Fleece rot easily assessed by scoring
  bloodline substitution offers a means of rapidly improving resistance
Notes: Prepared by S.I. Mortimer, NSW Agriculture.
Within the Merino breed, large differences between strains in resistance to fleece rot occur. The order of resistance increases from the strong wool to medium wool to fine wool strains. These differences become greater as the average incidence of fleece rot increases in response to more favourable conditions for the development of fleece rot. As well, there are significant differences between bloodlines within a strain in the average level of resistance to fleece rot. These differences between strains and bloodlines within strain are due to many influences such as differences in breeding programs (use of selective breeding and crossbreeding) and environments. The differences present a means of rapidly improving resistance to fleece rot through bloodline substitution, but choice of bloodline would need to consider other economically important traits to the production system.
Between bloodline correlations indicate that bloodlines of greater resistance to fleece rot are associated with finer fibre diameter and better style and colour but reduced clean fleece weight, yield and body weight and shorter staple length. However, these traits would need to be used cautiously as predictors of resistance to fleece rot when considering different bloodlines.
At the breed level, there is inconclusive evidence for differences between breeds in resistance to fleece rot, due to a lack of designed studies to compare breeds under the same environment and management conditions.
Scoring sheep for fleece rot provides an easy and cheap method of assessing the severity of the condition and of grading individuals on their relative susceptibility to fleece rot. The information then allows decisions on the culling of animals within a mob to be made. A detailed scoring system, developed by NSW Agriculture, is available to the sheep industry.

## Slide 12
End of Summary Slides
Close Window