## Slide 1: Textile properties of wool and other fibres
Topic 20 – Lecture 1
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Commercially important properties of wool
Fibre diameter
Fibre length and strength
Colour
Crimp/bulk/lustre
Vegetable matter content
Medullation content

## Slide 3: Fibre diameter
The most important textile property
Determines suitability of wool for end-use
Controls fineness to which a yarn can be spun
Fine wools produce fine, soft-handling fabrics
Unit: micron – 1 micron = 1/1,000,000 metre

## Slide 4: Fibre diameter requirements for wool products

## Slide 5: Fibre diameter distribution
Wide variation in fibre diameter in a flock or individual fleece
Fibre diameter distribution depicts diameter range
Mean Fibre Diameter used as fineness indicator
Coefficient of variation of fibre diameter CVD measures range of diameters
Modern instruments OFDA and Laserscan provide complete fibre diameter distribution

## Slide 6: Typical fibre diameter distribution
25
30
15
20
Fibre diameter (m)
30
20
10
Number of fibres
Mean fibre diameter = 25 microns
Standard deviation of 10 microns gives CVD of 40%

## Slide 7: Fibre diameter and fibre bending
Consider fibre as a flexible rod
Force required to bend varies as square of diameter
  eg, a 20 micron fibre is 4 times more flexible than a 40 micron fibre
Reason for diameter effect on fabric handle and drape
Fabric prickle explained by Euler’s theory

## Slide 8: Physics of prickle

## Slide 9: Fibre length and strength
Determines most suitable processing system
As important as fibre diameter for coarser wools
Because of fibre breakage in carding (mostly) fibre length can change significantly
Longer/stronger wools easier to spin and better yarns
Staple length and strength measurements used to assess these fibre properties

## Slide 10: Changes in fibre length in carding
Fibre length distribution after carding
Fibre length distribution before carding
Fibre length distribution shifts to the left, depending on amount of fibre breakage
Number of fibres
Fibre length
LONG
SHORT

## Slide 11: Length and strength requirements
Worsted processing
  Sound, long wools preferred otherwise reduced yield, inferior yarn
  Combing removes short fibres but at expense of yield
Woollen processing
  Handles shorter wools (provided not extreme)
  Very long wools cause problems
Semiworsted processing
  No combing so long, sound wools essential

## Slide 12: Colour
White and bright wools preferred for most products
Yellow wools limit dyeing options
  Also may indicate microbial damage
Pigmented fibres to be avoided for apparel
Specified by X, Y, Z tristimulus values:
  Brightness: Y (the higher the better)
  Yellowness: Y – Z (the lower the better)

## Slide 13: Effect of colour on dyeing

## Slide 14: Crimp and its effects
Crimp has an important influence on:
Bulk (the ability of wool to fill space)
Resistance to Compression (compressibility of fibres)
Lustre (level of shininess of fibres)
Low crimp
High crimp
Low bulk, low resistance to compression, high lustre, generally coarser wools
High bulk, high resistance to compression, lower lustre, generally finer wools

## Slide 15: Crimp in wool products
Is beneficial in knitwear and carpets
  Springy handle and warmth
Low crimp (ie, high lustre) less desirable in machine-made carpets
Higher crimp frequency is disadvantageous in worsted processing
  produces shorter tops
  yarns weaker and more irregular
  low crimp better for smoother, soft-handling fabrics

## Slide 16: Vegetable matter
Cellulosic contaminant: burrs, grass seeds, thistles, hard heads, chaff, twigs,….
Some types (eg, shive) more of a problem for removal in processing, hence discounted
High levels may necessitate carbonising
Measured as part of Yield Test (NaOH digestion)
  Report VM level (%) and type(s)

## Slide 17: Medullation
Hollow core (medulla) in some coarser wool fibres
Remnant of outer coat of primitive sheep breeds, goats
Bred out of finer breeds to eliminate in apparel
Acceptable in carpet blends – unique properties
Medullated fibres won’t take dye as ordinary fibres do
Types of medullation

## Slide 18: Wool’s competitors
Regenerated fibres
  Rayon (1900) – from wood pulp
Synthetic fibres – from petrochemical industry
  Polyamide (ie, Nylon) (1939)
  Polyester (1940)
  Acrylic (1942)
  Polypropylene (1960)
Cotton complementary rather than a competitor

## Slide 19: Wool blends
Blending different wools
  to produce a yarn meeting a specification at cheapest price
  To add special features, eg, bulk
Woollen spinning – more diverse types combined
Worsted and semiworsted spinning – more uniform, better quality types

## Slide 20: Blends of wool with other fibres
Purpose:
  Combine best features of the fibres, or
  Produce wool-like properties similar to 100% wool
Some common combinations:
  Wool/cotton (Viyella) – light-weight apparel
  100% Wool/ 80% nylon – for abrasion resistance
  Wool/polyester – easy-care fabrics
  Wool-Lycra – to add stretch

## Slide 21
End of Summary Slides
Close Window