## Slide 1: Topic 6
Style and Type
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Style Descriptors and AWEX-ID Number
Traditional Descriptor | AWEX ID Number
Choice | MF1
Superior | MF2
Spinners | MF3
Best Topmakers (BTM) | MF4
Good Topmakers (GTM) | MF5
Average Topmakers (ATM) | MF6
Inferior | MF7

## Slide 3
Importance of Raw Wool Characteristics
**** Major Impact
*** Secondary Impact
** Minor Impact
* No Significant Impact
(a) Mean Fibre Strength
(b) Mean Fibre Length
(c) Effects on dyeing
Minor effect on spinning
Raw Wool Attribute | Overall | Topmaker | Spinner
Mean Diameter | **** | **** | ****
Yield | **** | **** | 
Staple Strength | *** | *** (a) | ** (a)
Position of Break | *** | *** (b) | ** (b)
Staple Length | *** | ** | **
Clean Colour | *** | ** | (c)
VM Type | *** |  | 
VM Content | *** |  | 
Coloured Fibres | *** |  | (c)
Staple Length Variability | ** | * | * (d)
CVd | ** | * | * (d)
Crimp/Resistance to Compression | ** |  | 
Cotts | ** |  | 
Staple Tip | * |  | 
Style/Type… Handle | * |  | 
Breed/Age/Fleece Portion | * |  | 
Source: Plate (1978)

## Slide 4
micron
25%
strength
38%
mid breaks 6%
length
7%
colour
<1%
style 10%
staple
measurement 2%
marketing
factors
8%
Value Determining Characteristics 2003/04: 17.0-18.5 Micron Merino Fleece Wool Source: The Woolmark Company (2005)
VM 4%

## Slide 5
Value Determining Characteristics 2003/04: 18.6-24.5 Micron Merino Fleece Wool Source: The Woolmark Company (2005)
micron
49%
strength
15%
mid breaks
3%
length
8%
colour 3%
style 1%
staple measurement
6%
marketing factors*
5%
VM
10%

## Slide 6: Web Site Links
www.wool.com /pricemaker
www.awex.com.au

## Slide 7: Suggested Reading
AWEX – ID ...Description of the Non-Measured Characteristics
of Greasy Wool –Appraisal Guidelines., V2.0,1999
publ. Aust. Wool Exchange, Sydney.
Woolspec 94,
Specification of Australian Wool & its Implications
for Marketing and Processing, 1994
publ. CSIRO (Division of Wool Technology &
International Wool Secretariat) Sydney
Specific papers are:
- Crowe & Stevens
- Ford & Jackson
- Stevens & Crowe

## Slide 8: MF1 – Spinners Style
The following images show the 7 style grades. The grades differ in:
Staple density
Tip dust penetration
Degree of staple weathering
Regularity & consistency of the appraisal sample
Crimp character, regularity & definition
Staple tip structure (if weaners)
Frib content (if pieces)
Visual appearance

## Slide 9: MF2 – Superior Style

## Slide 10: MF3 – Spinners Style

## Slide 11: MF4- Best Topmakers Style

## Slide 12: MF5 Style – Good Topmakers Style

## Slide 13: MF6 – Average Topmakers Style

## Slide 14: MF7 – Inferior Topmakers Style

## Slide 15
End of Summary Slides
Close Window