## Slide 1: Traditional Classing and the Impact of Pre-sale Testing
Topic 2 – Lecture 1

## Slide 2
1. Traditional clip preparation procedures emphasised visual uniformity to:
  Assist valuation and
  Prepare wool for particular processing pathways
  2. Preparation consisted of two major steps:
  Separation of fleece wool and belly wool during shearing and
  Separation of pieces, locks and stains during skirting

## Slide 3
The proportions by weight of the wool components of the fleeces from a single mob are:
Source: Charlton (1983)
 | Average | Range
Skirted Fleeces | 73% | 66-82%
Pieces | 15 | 5-22
Bellies | 7 | 6 – 8
Locks | 3 | 1 – 6
Stains | 2 | 0 -11

## Slide 4
Traditional clip preparation paid most attention to the “classing” of the skirted fleeces:
Separating fine from coarse fleeces for example:
AAA v AAACOM
AA v AACOM
Separating high yielding and/or longer fleeces from lower yielding and/or shorter fleeces for example:
AAA v AA
AAACOM v AACOM
Separating short, very coarse, tender, cotted or other faulty fleeces if they occur

## Slide 5
1. Testing of mill consignments for yield and average fibre diameter (post-sale testing) increased rapidly after 1960
2. As the sale lots comprising these consignments were still appraised subjectively the woolgrowers had little indication of the true yield, vegetable fault content and fibre diameter of his/her sale lots
3. The introduction, after 1970, of pre-sale testing, firstly for yield, vegetable fault and fibre diameter and, later, for staple length, staple strength and colour provided the essential linkage between grower and processor based on the measured characteristics that determine processing performance and, consequently, value

## Slide 6
Yield and fibre diameter were the major factors determining the clean price of wool and research revealed that:
differences achieved by classing skirted fleeces for fibre diameter, yield and staple length were small
differences among sale lots from different mobs/farms appraised as having the same fibre diameter, yield and staple length were very large

## Slide 7
The reason for these results was the poor relationships between subjective and objective appraisal. It was demonstrated that:
Sale lots having the same subjectively appraised yield varied by + 6% (95% conf.int.) about the measured value
Sale lots having the same quality number of “visual micron” varied by + 2.5um about the measured fibre diameter
Similar large variations between measured and appraised characteristics were observed for vegetable fault, staple length, staple strength and colour

## Slide 8: Relationship between fibre diameter and crimps/inch among fleeces from the same mob (number of fleeces in circles)
Source: Whiteley, 1974

## Slide 9
1. Due to its significance throughout processing and in the end use of wool textiles the issue of fibre diameter deserves special consideration
2. The classer uses quality number to class for fineness and the estimate is based primarily on staple crimp frequency
3. As the aim is to produce differences in fibre diameter the procedure can be described as indirect selection
4. The success of the classer in producing classed lines that differ in fibre diameter depends upon:
The correlation between crimp frequency and fibre diameter and
The variation in fibre diameter among fleeces in the mob

## Slide 10: Selection of a portion,  (mean diameter d) from a population (mean diameter D)
Source: Whiteley and Wilkins, 1973

## Slide 11: Relationship between correlation of crimp with diameter and the variation in diameter among fleeces within a mob
Source: Whiteley and Wilkins, 1973

## Slide 12
Expected differences between the fibre diameters of the fine and coarse halves of the fleeces from a mob
Difference in Fibre Diameter (um) |  |  |  |  |  |  | 
High | -0.5 | 0.8 | 1.1 | 1.4 | 1.6 | 1.8 | 2.0
 | -0.4 | 0.6 | 0.9 | 1.1 | 1.3 | 1.4 | 1.6
Correlation between crimp and fibre diameter | -0.3 | 0.5 | 0.7 | 0.8 | 1.0 | 1.1 | 1.1
 | -0.2 | 0.3 | 0.5 | 0.6 | 0.6 | 0.7 | 0.8
 | -0.1 | 0.2 | 0.2 | 0.3 | 0.3 | 0.4 | 0.4
 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0
 | +0.1 | -0.2 | -0.2 | -0.3 | -0.3 | -0.4 | -0.4
Low | +0.2 | -0.3 | -0.5 | -0.6 | -0.6 | -0.7 | -0.8
 |  | 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0
Variance (um2) |  |  |  |  |  |  | 
Source: Whiteley and Wilkins, 1973

## Slide 13
1. Table 1 shows how the correlation between fibre diameter and crimp frequency influences the magnitude of the difference in fibre diameter when the separation of the fleeces is based on staple crimp frequency
2. The differences are related to the average fibre diameter of the mob, the coarser the mob the greater the variation among fleeces and the higher the correlation between fibre diameter and crimp frequency
3. In contrast, the superfine mobs tend to have reduced variation among fleeces in fibre diameter and a very poor correlation between fibre diameter and crimp frequency
4. For superfine mobs the correlation may be zero or even positive. This would indicate that the fleeces with a higher crimp frequency would have a larger fibre diameter. In other words, the “fine” lines would have a larger fibre diameter than the “coarse” lines
5. Sale catalogues should be examined to confirm these observations for traditionally classed clips

## Slide 14
End of Topic Summary
Close Window