## Slide 1: Classing Systems
Topic 7
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2
Table 1 Count to Micron Converter
Count | Diameter (um) | Breed
74 | 18 | Merino
70 | 19 | “
64/70 | 20 | “
64 | 21 | “
64/60 | 22 | “
60 | 23 | “ / Comeback (Polwarth)
60/58 | 24 | “ / “ “
58 | 25 | “ / “ “ / Corriedale
58/56 | 26 | Comeback – Corriedale
56 | 27 | “ “
56/50 | 28 | “ “
50 | 30 | “ “
46 | 32 | Crossbreds
44 | 33 | “
40 | 35 | “
36/32 | 38 | “
Note 1um = 1,000,000 of a meter

## Slide 3
Table 2
Line | Average % | Range %
Skirted Fleece | 73 | 66-82
Pieces | 15 | 5-22
Bellies | 7 | 6-8
Locks | 3 | 1-5
Stains | 2 | 0-11

## Slide 4
Table 4. Components of Variation for Diameter
and
Staple Length in Objectively Classed Clip Lines
Variation | Diameter # % Variation | Staple Length * % Variation
Between & Along Fibres | 80 | 80
Between Staples | 8 | 10
Between Fleece | 8 | 5
Between Lines | 4 | 5
Soureces: # Andrews et.al. (1979) * Rottenbury & Andrews (1975)

## Slide 5
Table 5. Additivity of Processing Performance
Clip | Total Losses % |  | Hauteur (mm) | 
 | Calculated | Actual | Calculated | Actual
B | 25.0 | 24.7 | 56 | 57
C | 18.3 | 18.5 | 71 | 74
D | 30.2 | 33.9 | 62 | 59
E | 19.3 | 18.6 | 62 | 60
F | 14.3 | 13.9 | 62 | 63
K | 12.1 | 13.4 | 67 | 69
Combined | 19.9 | 19.9 | 63 | 64
Source: Rottenbury 1983

## Slide 6
Table 6. Differences in Processing Attributes for Traditional Main Line & Mob Unit
Attribute | Top Diameter |  | Top Length | 
 | Diameter (um) | CVd (%) | Hauteur (mm) | CV Ha (%)
AAA Line | 22.1 | 22.8 | 65 | 42
Mob Unit | 22.0 | 23.2 | 64 | 43
Note: these differences are not practically or statistically different.

## Slide 7
Classing Systems
Traditional – On-Farm
Lot Building & Bulk Classing
Objective Bulk Classing
Reduced Skirting Systems
Fleece Separation
Objective Classing Systems – On-Farm Testing

## Slide 8: Diameter and Curvilinear Price Relationships

## Slide 9
NZ Pac Concept
S.Africa & NZ
S.American
UK/Europe
USA
Central Europe
Overseas Developments

## Slide 10: AWEX Code of Practice - Principles
The code describes the 3 key principles in preparation of wool for sale:-
The need for even lines of wool suitable for processors
The need to eliminate contamination, and
The appropriate identification and documentation of the wool
on-farm and at the point of sale.

## Slide 11
End of Summary Slides
Close Window