## Slide 1: Staple Strength and General Preparation Procedures
Topic 2 – Lecture 3

## Slide 2
1. Staple strength is considered as a wool fault and grouped with other faults such as cotted and coloured fleece
2. Staple strength variations are caused by changes in the diameter of wool fibres along their length due, primarily, to varying nutritional conditions
3. Therefore, among the fleeces from a single mob, staple strength is related to fibre diameter variability

## Slide 3
1. Within a mob there are wide variations in staple strength among fleeces
2. This contrasts with fibre diameter and length where the major variation occurs within fleeces
Sources of variation of staple strength
Component | Total Variation (%)
Within Fleece Sites | 20
Among Fleece Sites | 20
Among Fleeces Within Mob | 60
Source: Rottenbury and Smith, 1979, Rottenbury 1981

## Slide 4
1. Staple strength is measured in newtons/kilotex (N/ktex) and sound wools have a value of 30 N/ktex and above
2. Mob averages of 30 N/ktex to 50 N/ktex are common but values as high as 100 N/ktex have been reported
3. Due to the force necessary to break a staple, subjective methods are only effective up to strengths of 30 N/ktex
4. Wool with staple strengths greater than 30 N/ktex give better processing performance and cannot be evaluated by subjective methods
5. Wool with a staple strength below 30 N/ktex is likely to be classified as tender using subjective methods

## Slide 5: Distribution of staple strength among the fleeces of a mob of sheep grown under constant levels of nutrition
FREQUENCY
0 20 40 60 80
Mean 40
Staple Strength (N/ktex)
Source: Rottenbury and Smith 1979

## Slide 6
1. While fleeces within mobs vary over a wide range there are also large differences among mobs from different farms
2. These effects are demonstrated in the next table for clips prepared in the traditional manner and tested presale
3. Note that the subjectively-appraised tender lines from each of the three mobs have staple strengths of about 20 N/ktex due to the method of appraisal whereas the main AAA lines vary substantially

## Slide 7: Staple Strength of Sound and Tender Lines
Mob | Staple Strength (N/ktex) | 
 | Tender | AAA
Farm A | 22 | 42
Farm B | 20 | 33
Farm C | 20 | 27
Source: Rottenbury and Smith, 1979

## Slide 8
1. The processing performances of these three mobs are shown in the following table
2. Note that the strong clip (Farm A), produces the longest fibre length in the top and, although the tender line is shorter, it is still longer than the AAA lines from the other two mobs
3. In other words there are similarities in the processing performances of the sound and tender lines from the same mob. A good demonstration lies in the results for short fibre content
4. This may be due to the fact that although there are differences in strength their staple profiles would be similar as the sheep have been run under similar conditions throughout the growing season

## Slide 9
1. The differences between the classed lines is largest in strong clips but the size of the tender line in these clips would be small
2. Blending the AAA line with the small amount of tender wool would not influence the processing performance of the main line
3. In the mobs of lower staple strength where the average is about 30N/ktex the tender line will obviously be much larger but the difference between the sound and tender lines is very small so little is achieved by separating them if presale test results are available
4. It is important to note that current regulations require that tender fleeces are removed

## Slide 10: Processing Sound and Tender Wools
Mob | Line | Card Loss (%) | Noil (%) | Top Length (mm) | Short Fibre (<25mm)
Farm A | AAA TDR | 6.2 7.0 | 4.8 6.2 | 78 65 | 3 4
Farm B | AAA TDR | 5.4 5.7 | 7.1 8.5 | 61 57 | 17 19
Farm C | AAA TDR | 5.2 6.4 | 6.9 7.8 | 61 58 | 13 13
Source: Rottenbury and Smith, 1979

## Slide 11
1. “Lower Lines” comprise pieces, bellies, locks and stains
2. They constitute almost 30% of the weight of wool from a mob of sheep
Mob Structure (% by weight of 18 clips)
3. Lower lines commonly have higher levels of vegetable fault and dark fibres
4. They are separated from the fleece as they may be processed by different pathways
 | Average (%) | Range (%)
Skirted Fleece | 73 | 66 - 82
Pieces | 15 | 5 – 22
Bellies | 7 | 6 – 8
Locks | 3 | 1 – 5
Stains | 2 | 0 - 11
Source: Charlton, 1983

## Slide 12
1. The lower lines are finer in fibre diameter and lower in staple length and staple strength than fleece wool
Influence of Preparation on some Raw Wool Characteristics – Average for all clips
Line | Fibre Diameter (um) | Staple Length (mm) | Staple Strength (N/ktex
AAAM | 20.9 | 91 | 40
Unclassed/Skirted Fleeces | 21.2 | 92 | 41
Unclassed/Unskirted Fleeces | 21.0 | 92 | 41
Mob Unit | 21.0 | 90 | 40
PCS | 19.9 | 79 | 38
BLS | 20.7 | 73 | 29
Non FLC | 20.5 | 75 | 37
Source: Charlton, 1983

## Slide 13
These raw wool properties are reflected in fibre length in the top
although, as expected, there is very little effect on CV of fibre length
in the top
Influence of Preparation on Top Diameter and Length
Line | Fibre Diameter |  | Fibre Length – Hauteur | 
 | Mean (um) | CV (%) | Mean (mm) | CV (%)
AAAM | 22.6 | 21.4 | 67 | 50
Unclassed/Skirted Fleeces | 22.8 | 21.9 | 68 | 50
Unclassed/Unskirted Fleeces | 22.8 | 22.3 | 66 | 51
Mob Unit | 22.7 | 22.0 | 64 | 51
PCS | 22.2 | 22.0 | 57 | 52
BLS | 22.8 | 21.1 | 54 | 51
Non FLC | 22.3 | 23.0 | 55 | 52
Source: Rottenbury, 1983

## Slide 14
1. The key issues in the processing of lower lines are colour, vegetable fault and dark fibres (following table)
2. Both the brightness and the yellowness of the lower lines are inferior to the fleece wool
3. The number of vegetable matter particles in the lower lines is significantly greater regardless of whether the VM content of the greasy wool was high or low
4. Of greatest significance, there are dramatic increases in the dark fibre contents of the lower lines

## Slide 15: Influence of Preparation on Top Faults
Line | Colour* |  | VM Particles** (/100g) |  | Dark Fibres (/100g)
 | Brightness (units) | Yellowness (units) | High | Low | 
AAAM | 83 | 11 | 115 | 50 | 75
Unclassed/Skirted Fleeces | 83 | 11 | 134 | 72 | 55
Unclassed/Unskirted Fleeces | 83 | 12 | 150 | 72 | 45
Mob Unit | 82 | 12 | 206 | 62 | 1735
PCS | 81 | 13 | 420 | 143 | 475
BLS | 80 | 13 | 436 | 152 | 5210
NON FLC | 80 | 14 | 436 | 140 | 8865
* High values indicate higher levels of Brightness and higher levels of Yellowness
** The 18 clips were divided into two groups representing high and low levels of VM contamination
Source: Rottenbury, 1983

## Slide 16
1. The lower lines were converted to top without difficulty
2. The “mob unit” comprising a mixture of all the lines also processed satisfactorily and in a manner predictable from the raw wool measurements (following table)
3. Wool from lower lines does not present any difficulties in processing
4. However, tops produced from wool comprising both fleece and lower lines are poor in colour, contain more vegetable particles and have unacceptable levels of dark fibres
5. Separation is therefore an essential part of clip preparation. From a processing point of view it is more important than the classing of skirted fleeces.

## Slide 17: Additivity of Processing – Predicted and Actual Performance of the Mob Unit
Clip | Card + Noil Loss (%) |  | Top Fibre Length – Hauteur (mm) | 
 | Actual | Predicted | Actual | Predicted
B | 24.7 | 25.0 | 57 | 56
C | 18.5 | 18.3 | 74 | 71
D | 33.9 | 30.2 | 59 | 62
E | 18.6 | 19.3 | 60 | 62
F | 13.9 | 14.3 | 63 | 62
K | 13.4 | 12.1 | 69 | 67
Mean | 19.9 | 19.9 | 64 | 63
Source: Rottenbury, 1983

## Slide 18
End of Summary Slides
Close Window