## Slide 1: Influence of Clip Preparation Methods on Fibre Diameter, Length and Processing Performance
Topic 2 – Lecture 2

## Slide 2
1. The small differences achieved in fibre diameter between lines cast doubts on the value of fleece classing, whilst the large differences among lots appraised as being of the same fineness, yield and length required further explanation
2. It was also established the classing did little to improve the uniformity of the important measured characteristics of sale lots despite the fact that the classer produced fleece lines of high visual uniformity
3. The answer to these apparent anomalies lay in the components of variation of important characteristics together with the correlations between them and the characteristics, such as crimp frequency, that the classer used to estimate them

## Slide 3
1. The bulk of the variation in fibre diameter, 70% - 80%, lies within the single staple
2. It is composed of two parts:
Variation among fibres due to the complex structure of the follicle population and
Variation along the fibres due to nutritional conditions throughout the growing season
3. The classer is not able to influence these components as he/she is limited mainly to the variation in fibre diameter that exists among fleeces
4. This component of variation is only equal to ¼ of the variation that exists within the staple in sound wool and even less in tender wool
5. However the classes can only influence the among-fleece component of variation indirectly through the correlation between crimp frequency and fibre diameter, which is not strong

## Slide 4
Source of Variation | Variance (um 2)
Among fibres within a staple | 16
Along fibres within a staple Sound wool Tender wool | 4 16
Among staples within the fleece | 1
Amopng fleeces within a mob | 4
Among fleeces within a classed line | 3.9 – 3.6
Among classed lines within a mob | 0.1 – 0.4
TOTAL | 25
Source: Whiteley, 1974

## Slide 5
1. Previous table shows that the classer has to operate on a variance component of 4um2 and can only reduce this figure to 3.9um2 by separating fleeces on the basis of quality number
2. Presale testing came too late in the sequence to help the classer but it did provide the buyer with the ability to reduce the large differences that occurred among sale lots of the same apparent fineness
3. This led to the concept of objective clip preparation (OCP) under which fleeces from the same mob were kept together in one major line but then tested presale for matching purposes by the buyer
4. There was still concern that this large line exhibiting a range of up to three quality numbers would not process as well as the classed lines.

## Slide 6
1. To validate the OCP procedure, trials were undertaken to demonstrate the characteristics of the OCP line and its processing performance
2. For these trials the skirted fleeces from single mobs were split into three groups comprising the traditional fine and coarse lines and one group of unclassed fleeces
3. Note that the diameter of the lines does not change significantly during processing and the OCP line lies in an intermediate position between the fine and coarse lines in terms of both average fibre diameter and its variability
4. Note also that the crimp frequency varies as would be expected when selection is based on quality number
5. Further, the OCP line performed as expected in worsted spinning performance and in yarn quality

## Slide 7
1. Staple length differs from fibre diameter in that there is very extensive breakage of fibres during processing so that length is substantially reduced
2. Nevertheless there is a strong relationship between staple length and fibre length in the top
3. Staple strength does cause deviations from this relationship but staple length remains the dominant factor in determining fibre length in the top. The length of staples can be more easily appraised by the classer and the buyer than was the case with fibre diameter
4. However, the variation in staple length over the fleece and among fleeces makes the task difficult

## Slide 8: The relationship between mean fibre and staple length in greasy wool
Source: Bow, 1979

## Slide 9: The linear relationship between fibre length in the top and mean staple length of the greasy wool
Source: Bow, 1979

## Slide 10: Sources of variation in fibre length
Source: Andrews, 1974

## Slide 11
Fibre Length variation
Source of Variation | %
Within the staple | 80
Over the fleece | 10
Between fleeces | 10
TOTAL | 100%
Source: Andrews, 1974

## Slide 12: Staple Length in Classed Lines
Staple Length in Classed Lines |  | 
Line | Staple Length Mean (mm CV (%) | 
AAAM | 90 | 13
AAM | 87 | 13
AM | 80 | 15
AAACOM | 93 | 12
AACOM | 92 | 13
Unclassed | 88.4 | 13
BKN FLC | 82 | 18
Source: Andres 1974

## Slide 13
1. The results show that the differences in length between classed lines are small. Although the AAM and AACOM are comprised mainly of wools of “heavier condition and/or shorter” the differences of these lines from the AAAM and AAACOM lines are only 1mm-2mm. However, a top maker may have his 100ton lot rejected if it is 1-2mm shorter than that specified on the sales contract.
2. The AM line, reserved for very short fleeces, is 10mm shorter but is usually only very small
3. The most significant feature is that if the fleeces were unclassed the mean length of this line (88.4mm) would be very close to that of the major classed lines
In addition, the CV of fibre length of the unclassed line does not differ from the classed lines. Classing had little or no effect on reducing the variability of staple length within lines unless classers mix tender and sound wools
5. Wools from lower lines (eg. AM, AAACOM, AACOM, BKNFLC) are more difficult to predict their processing performance. They require more opening, better burr removal and as a consequence more fibres are broken during carding

## Slide 14: Variation in staple length among fleeces within a mob of sheep
Source: Andrews, 1974

## Slide 15
1. It was still considered necessary to demonstrate that the processing performance of fleeces that were unclassed for staple length was satisfactory
2. To do this, fleeces from individual mobs were sorted into three categories namely long (L), medium (M) and short (S)
3. Comparisons were made between these lines and various combinations of them

## Slide 16
Comparison of Staple Lengths – Greasy Wool and Top
Line | Greasy |  |  |  | Top | 
 | Staple Length |  | Fibre Length |  | Fibre Length | 
 | Mean (mm) | CV (%) | Mean (mm) | CV (%) | Mean (mm) | CV (%)
Long (L) | 90 | 15 |  |  | 69 | 50
Medium (M) | 79 | 14 | 94 | 25 | 67 | 44
Short (S) | 69 | 13 |  |  | 62 | 43
L+M+S | 79 | 15 | 95 | 26 | 66 | 44
L + S | 78 | 18 | 94 | 27 | 65 | 45
Source: Rottenbury and Smith 1979

## Slide 17
Variation in staple length within lines comprising the long, medium and short fleeces from a single mob of sheep
Source: Andrews, 1974

## Slide 18
1. As expected the three length groups differ by about 10mm in staple length and this order is maintained in the fibre length of the resulting tops
The fibre length differences in the top are quite small, the long and the short lines differing by only 7mm. This is due to the levelling action of the carding operation
3. Differences in CV staple length are small and are reflected in the CV fibre length in the top
4. CV fibre length is very much greater than CV staple length because, as was the case with fibre diameter, most of the variation in fibre length occurs within the staple. The variation is increased during carding due to fibre breakage
5. Classing has very little effect on the CV fibre length in the top

## Slide 19
1. In the Comparison of Staple Lengths table, the L+M+S group represents a line unclassed for staple length so that its mean would be expected to match that of the M group but it would have a greater CV staple length
2. The mean values are identical and the CV values differ by only 1% point
3. The mean fibre lengths in the top differ by only 1mm and the CV fibre length is identical for both lots
Even when the long and short lots are mixed to increase variability the mean fibre length and CV fibre length in the top show very little effect
NB: From a processing point of view the provision of presale test results for fibre diameter yield, and staple length remove the requirement to class skirted fleeces from the same mob into separate lines on the basis of quality number, condition and staple length.

## Slide 20
End of Topic Summary
Close Window