## Slide 1: WOOL 372/472/572 Wool Biology/Metrology
Topic 8
Yield
Rodney Barry

## Slide 2: LEARNING OBJECTIVES
UNDERSTAND IMPORTANCE OF YIELD TO PROCESSOR
UNDERSTAND PROCESSES USED TO PRODUCE ESTIMATE OF YIELD
UNDERSTAND COMPONENTS LEADING TO ESTIMATES OF YIELD
KNOWLEDGE OF DIFFERENT YIELD ESTIMATES AVAILABLE
UNDERSTANDING REQUIREMENTS

## Slide 3: YIELD
INTRODUCTION

## Slide 4: INTRODUCTION
THIS LECTURE FOCUSES ON:
- PURPOSE OF MEASUREMENT
- COMPONENTS OF YIELD
- PRINCIPLES
- EQUIPMENT
- PROCEDURES
- STANDARDS
- DERIVED YIELD ESTIMATES
- YIELD TESTING OF FLEECES

## Slide 5: YIELD
5.1 PURPOSE OF MEASUREMENT

## Slide 6: 5.1 PURPOSE OF MEASUREMENT
AMOUNT OF USABLE WOOL FIBRE IS OF VITAL INTEREST TO TEXTILE MANUFACTURER
ACTUAL PROCESSING PERFORMANCE OF WOOL CAN BE CALCULATED
VALID OBJECTIONS TO HIGH AND LOW YIELD VALUES

## Slide 7: YIELD
5.2 COMPONENTS OF
YIELD

## Slide 8: 5.2 COMPONENTS OF YIELD
WOOL BASE
SPINNING QUALITY
GREASE CONTENT
LENGTH
DENSITY
MINERAL MATTER
VEGETABLE MATTER
COLOUR
WATER WASHED APPEARANCE

## Slide 9: YIELD
5.3 PRINCIPLES

## Slide 10: 5.3 PRINCIPLES
EACH BALE IN A LOT IS SAMPLED
TEST SPECIMENS ARE TAKEN FROM EACH SUBSAMPLE
ALL IWTO CERTIFICATES SHOW WB TO 2 DP AND VMB TO 1 DP
GUIDELINES IN IWTO-19 ENSURE THAT REPEATABLE VALUES FOR COMMERCIAL YIELD ARE ACHIEVED

## Slide 11: YIELD
5.4 EQUIPMENT

## Slide 12: 5.4 EQUIPMENT
CORING MACHINE
BLENDING MACHINE
BALANCES
SCOURING BOWL (+ SIEVE)
CENTRIFUGE
DRIER
FURNACE (+ CRUCIBLES)
ALKALI RESISTANT CONTAINER (+ SIEVE)
SOXHLET APPARATUS (OR NIR MACHINE)

## Slide 13: YIELD
5.5 PROCEDURES

## Slide 14: 5.5 PROCEDURES
APPROX 1000g OF CORE SAMPLE IS OBTAINED

## Slide 15: 5.5 PROCEDURES (cont’d)
SAMPLE IS WEIGHED, BLENDED AND WEIGHED AGAIN

## Slide 16: 5.5 PROCEDURES (cont’d)
SAMPLE IS SCOURED, CENTRIFUGED, DRIED & WEIGHED

## Slide 17: 5.5 PROCEDURES (cont’d)
SAMPLE IS MEASURED FOR GREASE CONTENT USING EITHER:
- SOXHLET METHOD OR
- NIR METHOD

## Slide 18: 5.5 PROCEDURES (cont’d)
SAMPLE IS ASHED TO DETERMINE MINERAL CONTENT

## Slide 19: 5.5 PROCEDURES (cont’d)
WOOL IS DISSOLVED, TO ENABLE ASSESSMENT OF VM

## Slide 20: 5.5 PROCEDURES (cont’d)
WB CALCULATED BY DEDUCTING % IMPURITIES FROM OVEN DRY SAMPLE
% WB CONVERTED TO % YIELD BY USING APPROPRIATE CONVERSION FACTOR AND PROC. ALLOWANCE

## Slide 21: YIELD
5.6 STANDARDS

## Slide 22: 5.6 STANDARDS
INT’L STANDARDS MUST BE MET TO ISSUE CERTIFICATES FOR YIELD
IWTO-19: USED TO DETERMINE WB, VMB AND YIELD
IWTO CORE TEST REGS: USED FOR CALCULATION OF COMM. YIELDS
AS/NZS 4492.2: USED TO DETERMINE WASHING YIELD OF FLEECES

## Slide 23: YIELD
5.7 DERIVED YIELD
ESTIMATES

## Slide 24: 5.7 DERIVED YIELD ESTIMATES
THEORETICAL TOP & NOIL YIELD
ESTIMATED TOP & NOIL YIELD
IWTO SCHLUMBERGER DRY TOP & NOIL YIELD
THEORETICAL CARD SLIVER YIELD
EST. COMM. CARD SLIVER YIELD

## Slide 25: 5.7 DERIVED YIELD ESTIMATES (cont’d)
IWTO SCOURED YIELD, 17% REGAIN
JAPANESE CLEAN SCOURED YIELD
AUSTRALIAN CARBONISING YIELD
ASTM CLEAN WOOL FIBRE CONTENT
WASHING YIELD

## Slide 26: YIELD
5.8 YIELD TESTING OF
FLEECES

## Slide 27: 5.8 YIELD TESTING OF FLEECES
IMPORTANT FOR:
- SELECTION OF RAMS & EWES FOR
BREEDING
- WOOL CLASSING
WOOL SAMPLE TAKEN FROM RIGHT MID SIDE OF FLEECE
MID SIDE PRODUCES YIELD CLOSE TO AVERAGE OF FLEECE

## Slide 28: 5.8 YIELD TESTING OF FLEECES (cont’d)
MIDSIDE SAMPLES TAKEN TO TEST HOUSE AND YIELD TESTED BY:
- SCOURING
- CENTRIFUGING
- DRYING
- CALCULATION

## Slide 29: YIELD
SUMMARY

## Slide 30: SUMMARY
COMMERCIAL YIELD DEPENDS ON TYPE OF PROCESSING
YIELD IS IMPORTANT TO
- PARTIES BUYING & SELLING WOOL
- TOP MAKERS
- PROCESSORS