## Slide 1: WOOL 372/472/572 Wool Biology/Metrology Topic 11 Wool Colour Measurement Errol Wood
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Colour perception involves:
A source of light (illuminant)
A coloured object
A detector (eye or instrument)
BRAIN !!
Brain
Light source (sun or lamp)
Material
Eye

## Slide 3: Colour matching functions
The eye’s light receptors are the rods and cones
The three types of cones are sensitive to different wavelength ranges of light
Their responses are represented by three colour matching functions (r, g, b) – ‘the standard observer’
r
g
b

## Slide 4: Colour involves 3 attributes
Hue
Saturation (or chroma)
Lightness (or value)

## Slide 5: Effects of lightness and saturation on ‘redness’

## Slide 6: Calculation of tristimulus values
R = reflectance spectrum of object
E = spectral energy function of illuminant
b, g, r = colour matching functions for the standard observer

## Slide 7: CIELAB colour space
Opponent colour space with 3 axes:
  L* - lightness (or value) black-grey-white
  a* - green-red axis
  b* - blue-yellow axis
Most widely used today in industry

## Slide 8: Instrumentation - colorimeter
X = RED
Y = GREEN
Z = BLUE
Incident light
Photodetectors
SIGNAL OUTPUTS
Wool sample compressed against glass window
Colour filters

## Slide 9: Instrumentation - spectrophotometer
Light source
Reflection grating disperses light into its components
Detector
AMPLIFIER
COMPUTER
X Y Z
Wool sample in cell

## Slide 10: How X, Y and Z describe wool colour
A dull grey wool absorbs similar amounts of red, green and blue
A yellow wool absorbs more blue than red and green
A white wool absorbs only a small amount of red, green, blue
X ~ Y > Z
X ~ Y ~ Z (all low)
X ~ Y ~ Z (all high)

## Slide 11: Specifying wool colour *
X
Y
Z
Y
Y-Z
Brightness Y:
60 (dull) to 70+ (very bright)
Yellowness Y-Z:
<9 (white) to >16 (very yellow)
(Tristimulus results from instrument)
* D65/10o colour space

## Slide 12: Importance of wool colour (Y-Z values in C/2o colour space)

## Slide 13: Key factors in wool colour measurement
Calibration for agreement between instruments
  Reference wools now replaced by ceramic tiles
Recent change in illuminant in IWTO 56-03
  Obsolete C/2o replaced by D65/10o
Homogenous, clean sample essential
  Blending, scouring, drying, removal of VM
Presentation of sample to instrument
  Pressed against glass window at constant density or pressure

## Slide 14: Colour and wool scouring
Delivery of wool with acceptable colour is a key objective of process, but
Scoured wool colour ‘as-is’ colour result cannot match base colour result
Difference ΔY = Ybase – Y as-is
  measures effectiveness of scouring treatment
Effect of different scouring efficiency on yarn colour

## Slide 15: Near infrared reflectance for in-scour colour measurement

## Slide 16: Thank you
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen