## Slide 1: WOOL 372/472/572 Wool Biology/Metrology
Topic 13
Fibre Curvature, Crimp Frequency, Resistance to Compression and Bulk
Victoria Fish

## Slide 2: Overview
Fibre Curvature, Staple Crimp, Resistance to Compression & Bulk:-
Are each related to fibre shape;
Can influence breeding decisions;
Can affect processing & product performance.

## Slide 3: Resistance to Compression (RtC)
RtC is the pressure required to compress 2.5g of Shirley Analysed wool to a volume of 23.56cm3 in a cylindrical chamber of 50mm diameter
For Merino wool, the expected range of values is between 8kPa and 12kPa
Australian Standard 3535-1988 was developed for RtC

## Slide 4: BULK – New Zealand measurement
Bulk is the volume occupied by 2.5g of carded wool under a pressure of 1kPa in a cylinder of 50mm diameter
Measurement is preceded by 2 precompression steps using a pressure of 3kPa
NZS 8716:1994 was developed in New Zealand for testing the Bulk of core samples

## Slide 5: Relationship between RtC & Bulk

## Slide 6: Crimp Frequency
Crimp Frequency refers to the generally regular, or wavy pattern of ripples along the staple & is defined as the number of waves, or crimps, per cm
Can be measured manually though automatic measurement is being developed – Refer Style lecture
Manual measurement has some operator dependency

## Slide 7: Fibre Curvature
The mathematical definition of curvature, K, is the inverse radius of a circle such that:
K = 1/r
Measured as a by product of diameter measurement of snippets or single fibres (OFDA2000)
The units for measurement of fibre curvature in the wool industry (IWTO) are degrees per millimetre (°/mm)

## Slide 8: Fibre Curvature Measurement
Both Laserscan & OFDA measure curvature as a 2 dimensional projection of the 3 dimensional shape of a snippet or fibre
In OFDA Curvature is measured in a 2-stage process:
  An arc is formed from a trace along the edge of a fibre or snippet for a predetermined distance;
  The angle subtended by the arc at the centre of its circle is measured.
In Laserscan Curvature is determined by a projection of a fibre snippet impinging on a circular ring of optical detectors

## Slide 9: Fibre Curvature Measurement
There is currently:
  No means of calibration for fibre curvature measurement;
  No standardised preparation system for Fibre Curvature measurement; and
  No IWTO Standard for the measurement of Fibre Curvature

## Slide 10: The Effects on Fibre Curvature Measurement of Different Aspects of Preparation & Measurement
By introduction of fibre strains or hygral absorption, the following characteristics affect the value of measured fibre curvature:
1. Preparation processes:
  Unbroken fibre or fibre snippet; fleece, core or top sample; Shirley Analysed or not; minicore versus guillotine; number of minicorings & size of subsample (for snippet testing); aqueous or non-aqueous scouring
2. Measurement:
  Testing in air, isopropanol/water mixture or water; choice of test instrument

## Slide 11: Conclusion
The most direct measurement of fibre shape is Mean Fibre Curvature.
However, there are a number of factors which limit the usability of Fibre Curvature Measurement.
Automatic measurement of Staple Crimp Frequency might offer the best solution to shape measurement for greasy wool