## Slide 1: WOOL 372/472/572 Wool Biology/Metrology
Topic 15
Use of Measurement in Sheep Production, Greasy Wool Commerce & Commercial use of Prediction Technology
Bob Couchman
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: TEAM Trials (1,2 & 3) 1980 - 2004
Developed formulae to predict from greasy wool:
  Hauteur (average length)
  Coefficient of Variation of Hauteur
  Romaine (noil)
  Barbe (TEAM 2)
Represents world averages in processing performances.

## Slide 3: TEAM 2 - Hauteur
Hauteur = 0.52L + 0.47S + 0.95 D - 0.45 V - 0.19 M* - 3.5 (+MA)
L = length (millimetres)
S = strength (N/ktex)
D = fibre diameter (micron)
V = vegetable matter base
M* = percentage of middle breaks(%)
if between 0-45% use 45
if greater use actual figure
3.5 = constant

## Slide 4: TEAM 2 – CVHa & Romaine (noil)
CVHa = 0.12 L - 0.41 S - 0.35 D + 0.20 M * + 49.3 (+MA)
Romaine% = - 0.11 L - 0.14 S - 0.35 D + 0.94 V + 27.7 (+MA)
(Romaine = quantity of noil expressed as a percentage, of the combined quantity of top and noil)

## Slide 5: TEAM 2 - Barbe
B = 0.73 L+ 0.32 S + 0.96 D -0.51 V-0.086 M*- 5.3 (+MA)
L = length (millimetres)
S = strength (N/ktex)
D = fibre diameter (um)
V = vegetable matter base
M* = percentage of middle breaks(%)
if between 0-45% use 45
if greater use actual figure
5.3= constant
Barbe ---> Hauteur: B = Ha (1+ CVHa2 )

## Slide 6: Mill Adjustment Factors
Determined by differences in:
  machinery processing performance
  processing procedure
  variations in wool being processed
Determined for individual mills

## Slide 7
An Example Of Calculating A Mill Correction Factor
Actual Hauteur
Predicted Hauteur
Difference Between
Ach
ie
ved by Mill
Using the TEAM Actual and Predicted
Formula Hauteur
(mm)
(mm) (mm)
73.
9
73.1
0.8
73.6
73.0
0.6
57.3
55.5
1.8
59.0
58.4
0.6
66.0
66.9
-
0.9
58.1
55.8
2.3
58.7
57.7
1.0
61.2
58.8
2.4
58.3
54.3
4.0
59.4
57.9
1
.5
65.1
67.2
-
2.1
71.4
77.7
-
6.3
60.6
60.0
0.6
67.6
66.9
0.7
72.9
72.4
0.5
MEAN
0.5

## Slide 8: Information for Prediction is Obtained from Post Sale Test Certificates
Combined Certificates:-
IWTO COMBINED CERTIFICATE (Core)
  Micron, yield and vegetable matter
IWTO COMBINED STAPLE TEST CERTIFICATE
  Length, strength and position of break

## Slide 9: Using Prediction in Buying Specifications
Requirement TEAM (Ha) prediction = 70mm,
(MAF = +4.0 mm),
Required Risk Level = 1 in 40,
s.d. of Prediction:Processing = 5.7 mm.
Calculation:
Required Ha - MAF + (2 x s.d.)
= 70 - 4 + (2 x 5.7)
= 77.4 mm
The Mill must purchase wool that predicts as:-
77.4 mm Ha to have a 1:40 chance of failing to meet 70mm in the processed top.

## Slide 10: Example of TEAM used as a Quality Management Tool

## Slide 11: TEAM 3 Formulae
Hauteur = 0.43L + 0.35S + 1.38D – 0.15M – 0.45V – 0.59CVD – 0.32CVL + 21.8 + MA
CV Hauteur = 0.30L – 0.37S – 0.88D + 0.17M + 0.38CVL + 35.6 +MA
Romaine = – 0.13L – 0.18S – 0.63D + 0.78V + 38.6 +MA

## Slide 12: Thank you
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen