## Slide 1: WOOL 372/472/572 Wool Biology/Metrology
Topic 10
Staple Length, Strength & Position of Break David Crowe & Trevor Mahar

## Slide 2: Learning Objectives
understanding of the limitations associated with subjective appraisal of these parameters
an understanding of the relationship between Staple and Fibre properties
an understanding of the principles of objective measurement on an ATLAS instrument

## Slide 3: Subjective Appraisal- Staple Strength
Visual Perception
Sampling Bias

## Slide 4: Subjective Appraisal- Staple Length
the force exerted by the appraisers
the thickness of staples selected
the number of staples evaluated

## Slide 5: Relationship between Staple & Fibre Properties
Staple Length & Fibre Length
Staple Strength & Fibre Tenacity
Intrinsic fibre strength

## Slide 6: The Principles of Objective Measurement
Staple Length Measurement
Measurement of Peak Force to Break and Staple Mass
Calculations

## Slide 7: Staple Length Measurement

## Slide 8: Measurement of Peak Force to Break and Staple Mass

## Slide 9: Calculations

## Slide 10: Precision
Measurement | Wool Type | 1 Operator | 2 Operators | 4 Operators
Staple Length (mm) | Fleece | ±5.8 | ±5.3 | ±4.8
Staple Length (mm) | Non-Fleece | ±6.7 | ±5.8 | ±5.4
Staple Strength N/ktex) | Fleece & Non-Fleece | ±6.0 | ±5.9 | ±5.9

## Slide 11: Source of Variation
Sources of Variation | Staple Length | Staple Strength
Between Staples | 207.00 | 185.00
Between Grabs | 38.00 | 49.00
Between Operators | 3.26 | 0.54
Between Laboratories | 0.1 | 1.65
Between Instruments | 0.38 | 2.05
Total Variance | 307.64 | 314.19

## Slide 12: New Measurements
De-crimped Staple Length (DSL)
De-crimping Ratio (DR)
Specific Work of Rupture