## Slide 1: Scoured Wool Quality and Testing
Topic 6
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Certificated testing of scoured wool
Fully representatives sample (core and full length) are taken in the scour using prescribed procedures
Tested according to IWTO standards by test house for contractual (ie, trading) purposes:
    Yield (especially residual grease content)
    Colour
    Diameter (identical to greasy wool test method)
    Length After Carding
    Moisture content (regain)

## Slide 3: Sampling in the scour
Spear-head sampling probe to extract full-length sample for Length After Carding Test
Core sampling machine for dense bales
Source: New Zealand Wool Services International Ltd.

## Slide 4: Testing in the scour
In-scour testing carried out
    for quality control purposes
    to maintain consistent scouring performance
Sampling generally as for sample for test house, but hand samples may be used
Usual range of tests:
    Regain (Weigh/Dry/Weigh or NIRA)
    Residual grease content (Rapid grease test or NIRA)
    As-is colour (colorimeter or NIRA)
    pH

## Slide 5: Yield of scoured wool
Scouring removes most contaminants so yield results close to 100%
Depending on type of wool some contaminants remain:
    <0.5% residual grease
    <1.5% mineral matter (dirt)
Cleaning post-scour improves colour and reduces dust level of wool
IWTO yield test also gives VM, residual grease (alcohol solvent) and ash content
IWTO residual grease test uses dichloromethane (DCM) as the solvent

## Slide 6: Length after Carding (LAC) Test
NZ Standard test for scoured wool consignments
Uses full length sample taken in scour by special sampling probe prior to dense baling
Sample (~ 1kg) forwarded to test house
Test simulates actual processing, steps are:
    Carding to open clumps of wool, blend fibres
    Gilling to align fibres, form sliver
    Almeter system: samples and measures fibres
LAC results relevant to processors

## Slide 7: Colour of scoured wool
Base colour of wool
    IWTO test carried out by a test house on a thoroughly cleaned sample to give X, Y and Z
    This test gives the best colour than can be achieved with a wool (an ‘ideal’ result)
As-is colour
    In-plant test on sample of scoured wool after drying (without additional cleaning)
    Invariably the as-is colour results are poorer than base colour (presence of contaminants)
    Difference in colour (Delta Y) is an indicator of scouring quality (the smaller the better)

## Slide 8: Near Infrared Reflectance Analysis
NIRA is now a widely used measurement technology in NZ wool scours
Provides estimates of the following scoured wool quality parameters on every bale as it is produced:
    Moisture content
    Residual grease content
    As-is colour
    Mean fibre diameter and medullation content (if required)

## Slide 9: The Near Infrared
The infrared region of the electromagnetic radiation spectrum is just beyond the visible
Infrared energy is emitted by hot objects
Infrared energy is absorbed by molecules which vibrate at specific frequencies
This specific absorption enables NIRA techniques to be used to identify and measure the presence of particular substances in materials (eg water, grease in wool)

## Slide 10: Integrated process control with NIRA

## Slide 11: Pros and cons of NIRA in scours
PROS:
    Performs well in challenging environment
    Results produced rapidly on every bale, so
    Corrective action to scouring conditions is possible
    Much quicker than test house services, which provide only average of entire consignment (after a day or two)
    Accuracy and precision levels generally compare well with test house results
CONS:
    Equipment expensive
    Calibration an exacting procedure
    Results can’t be certificated yet (not IWTO tests)

## Slide 12
End of Summary Slides
Close Window