## Slide 1: Chemical Treatments in Woolscouring
Topic 11
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: General considerations
Chemical treatments almost always involve water – energy required to dry
When applied in scouring, take advantage of wetting out, squeezing and drying operations
Contaminants can reduce effectiveness of treatment
Some chemical treatments require high concentrations and temperatures and may be corrosive – also may be hazardous
Immersion time short (~ 1 minute) and high liquor ratio – conditions may be unsuitable
Advantages in scouring:
  Applied to loose stock for blending later, continuous process, energy saving (only dry once)

## Slide 3: Bleaching
Bleaching improves whiteness of wool
May be carried out on loose stock, sliver, top, yarn or fabric
Two kinds of bleaching agent
Reducing agents and oxidising agents – chemically alter natural colouring in fibre
Fluorescent brightening agents – make a fibre appear white, but may revert to original colour especially when wet (not used in wool scouring

## Slide 4: Reduction bleaching
Modern method involves solution of sodium metabisulphite
Carried out in last, scouring bowl (0.4% solution, pH 6, temperature < 55oC)
Disadvantages:
Lack of permanence
Carryover of contaminants from previous bowls can affect bleaching solution
Escape of SO2 gas may corrode plant and buildings (to avoid gas escaping, the pH must be controlled)

## Slide 5: Oxidation bleaching
Use more frequently than bisulphite method
Oxidising agent is hydrogen peroxide
Bleaching effect more permanent – colour of natural pigments removed
Yellow wools do not bleach well unless treatment is severe (but may damage fibres)
Peroxide bleaching usually carried out under acid conditions because:
  The wool feels the same or even softer;
  The wool dyes better because acid dyeing is normally used

## Slide 6: Peroxide bleaching in scouring
Widely used in scours for ~30 years
Treatment carried out in last bowl before dryer
A padding or ‘dry-in’ process – no colour change in bowl, but wool colour improves in dryer
Colour improvement: wool becomes lighter (Increased Y) and less yellow (reduced Y-Z)
Bowl charged with dilute solution of H2O2 – strength 0.55 – 1.1%
Strength depends on wool type, level of bleaching required
Solution kept acidic (pH 4-6) with formic acid
Peroxide concentration monitored by titration

## Slide 7: Insect-resist treatments
Necessary to provide protection to wool against moths and beetles
Level of protection depends on product and where it will be used
Treatments involve agents that are fixed permanently to the wool (resist washing, dry cleaning, light)
Various types of agents are available, especially:
  Synthetic pyrethroids such as ‘Permethrin’
  Insect growth regulators (IGRs)
Applied in liquid form in final rinse bowl or specialised treatment bowl, usually under acid conditions
Concentration depends on agent, level of treatment

## Slide 8: Wool pH
pH is a 0 –14 scale indicating the acidity or alkalinity of a solution
SCALE: 0-1 = strongly acidic; 5-6 = weakly acidic; 7 = neutral; 8-9 = weakly alkaline; 13-14 = strongly alkaline
pH measured by immersing wool sample in water for a period, then test solution for pH
Merino wools tend to be neutral or slightly acidic; crossbred wools are slightly alkaline
A slightly acid pH helps in dyeing
Adjusted by metering a weak acid such as acetic or formic into the last rinse bowl

## Slide 9: Other chemical treatments in the scour
Flame-resist using borax, boric acid or phosphoric acid
Odour control
Antiphotobleaching using Lanalbin APB
Differentiated fibre technologies from Canesis:
  Glacial: whiter, brighter cleaner wool
  Strike!: rapid wettability and dye uptake
  Aurora: for differential dyeing
  FERNplus EP: lustre reduction

## Slide 10: Safe chemical practices
Hydrogen peroxide, sulphuric acid need to be treated with respect
Store and handle chemicals with care
Use correct concentrations
Combine chemicals in the recommended way
Use protective clothing, gloves and goggles as directed
Know first aid and fire-fighting procedures
Check location of first aid and safety equipment
Check that metering equipment works
Use correct testing procedures to check additions
In the event of a chemical accident - WATER!

## Slide 11
End of Summary Slides
Close Window