## Slide 1
Woolgrease and its Recovery
Topic 6
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Production of wool wax
Wool wax is the secretion of the sebaceous glands in the skin of sheep
It is deposited on the fibres as they grow
It gradually oxidises on exposure to air
Woolgrease is the lipid material or grease recovered during scouring

## Slide 3: Nature of wool wax
A greasy substance, melting at ~ 40oC
A mixture of organic compounds – mostly esters plus free acids and free alcohols
Readily dissolves in non-polar organic solvents
Only partly dissolves in some polar organic solvents such as ethanol
Does not dissolve in water
When recovered by scouring the material is termed ‘woolgrease’
Colour of woolgrease poorer (ie, darker) from crossbred sheep than Merinos

## Slide 4: Importance of woolgrease recovery
Without recovery it is not possible to continuously scour wool in the same liquor and still achieve acceptable scouring quality
Recovery is profitable when done efficiently, and when selling price is good
Greatly reduces pollution of waterways etc.
Main method of recovery – centrifuging the aqueous scouring liquor

## Slide 5: Centrifuging
Scour liquor separates out slowly under gravity
Spinning liquor at high speed separates solids and liquids of different densities
Centrifuging method of recovery:
  Is profitable
  Yields good quality woolgrease
  Continuously cleans scouring liquor before recycling
Involves separating droplets of emulsified grease from liquor and unite droplets into larger masses

## Slide 6: Separation of scouring liquor
A container of heated scour liquor will slowly separate by gravity into 3 phases, according to the relative densities (RD) of water, grease and dirt
Centrifuging performs this separation continuously and rapidly by applying artificial ‘gravity’
Upper phase, mostly woolgrease, RD ~ 0.94
Middle phase mostly water and detergent plus some woolgrease, dirt. RD ~ 1
Lower phase composed of water, detergent and heavy solids, RD > 1

## Slide 7: The centrifugal separator
Liquor in
Sludge out
Emulsion out
Primary cream out
Stack of conical disks with holes
Gravity disc
Rotating spindle
Source: Anderson (1969)

## Slide 8: The centrifuging process (1)
Temperature of liquor at least 64oC on entry
High rotation speed (6000 rpm) produces a very strong centrifugal force on emulsion
Bowl contains a stack of cone-shaped discs with spacing 0.5 – 1mm
Bowl enclosed by covers which feed liquor in, and collect the phases
Source: Andar Holdings Ltd.

## Slide 9: The centrifuging process (2)
The scouring liquor is fed into the machine at the top
It travels down into the bowl to emerge in the disc stack
It rises up through the holes in the discs and into the spaces between the discs
As the liquor enters the discs, the centrifugal force separates the liquor into its different phases – cream, degreased liquor, solids,..
The output phases from the bowl emerge from drain spouts from the covers surrounding the bowl

## Slide 10: Nature of the 3 phases
PRIMARY CREAM: This is the lightest phase, which contains relatively un-oxidised woolgrease (plus some detergent)
EMULSION: This middle phase consists of partly degreased liquor and a little dirt. Recycled back into the scour.
SOLIDS: The lowest (and heaviest) phase is thrown against the wall of the bowl. The solids are continuously discharged along with liquor through jets in the bowl wall. Largely consists of degreased liquor, but with high dirt concentration

## Slide 11: Factors affecting efficiency of the centrifuge
Diameter of the gravity disc:
  Increasing diameter increases concentration of grease in cream
Liquor feed rate into centrifuge:
  Increasing feed rate increases amount of woolgrease recovered
  But dilution of cream occurs above a certain feed rate
Temperature of the feed liquor:
  Increasing temperature increases amount of woolgrease recovered
  More concentrated woolgrease cream produced

## Slide 12: Gravity disc
Located near top of centrifuge where emulsion and cream flow to different outlets
Provides back-pressure on aqueous phase emerging
Along with feed rate, controls the type of separation of the phases by the centrifuge
Optimum efficiency is achieved by using correct size of gravity disc with highest practical feed rate and high possible temperature
This gives the required grease content of the cream

## Slide 13: Role of the gravity disc
Gravity disc with large hole: low threshold, clean light phase
Gravity disc with small hole: high threshold, clean heavy phase

## Slide 14: Subsequent steps in grease recovery
In NZ usually have two-stage centrifuging system
Grease content of primary stage cream: 60-90%
THERMAL CRACKING: Cream fed to heated tank and undisturbed for > 6 hours ~85-90oC
Heat further separates cream into 3 phases, with bottom layer comprising:
  Water containing a little grease
  Dirt
  Water-soluble matter from the wool
Secondary centrifuging separates more grease:
  Treat cracked grease and emulsion layers with fresh hot water
  Produces woolgrease with moisture <1.0%

## Slide 15: Two-stage grease recovery

## Slide 16: Three stage system
Used for high woolgrease content wools; mostly finer wools for topmaking
Three centrifuging stages
Two concentrator steps followed by purifier step

## Slide 17: Uses of woolgrease
Refined woolgrease is called lanolin – used in soaps, cosmetics, emulsifier for pharmaceuticals
Other derivatives of woolgrease include wool wax alcohols (from which cholesterol is recovered)
Destructive distillation of woolgrease provides:
  Textile processing lubricant
  Axle bearing lubricants
  Leather dressings
  Roofing compounds
High temperature lubricants in steel industry
Woolgrease may be used as a boiler fuel
Lighter colour woolgrease more valuable, easier to refine

## Slide 18
End of Summary Slides
Close Window