## Slide 1: Carbonising
Topic 8
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Steps in the Carbonising Process
Neutralise
Acidise
Dry/bake
Crush/de-dust
Scour
Scouring to remove wax, suint and dirt
Impregnate VM with sulphuric acid
Concentrate acid and convert VM to hydrocellulose
Removal of the hydrocellulose
Alkaline wash, rinse and dry
Notes: The aim of the carbonising process is to remove vegetable matter (VM) from the wool with minimal loss of fibre strength.
Scouring and carbonising occur sequentially as one continuous process. After scouring and rinsing the wool is passed into a dilute sulphuric acid bath.
In the bath, a high penetration of acid into the VM is required, but with the lowest possible acid concentration so as to minimise damage to the wool fibre. This concentration of acid will vary depending on the nature of the VM to be removed, and the procedures used by the processing mill. The variables involved are a combination of acid concentration, temperature and time spent in the acid bath. A cold acid bath might have a concentration of 6-7% sulphuric acid, a concentration considered high, but the wool would remain in the bath for only 1-2 minutes. Whilst a mildly warm bath, 32-38°C, would have an acid concentration of 4.5-6.5%, but the wool would remain in the bath for a longer time, say 2-5minutes. It has been found that an optimal acid concentration in the squeezed dried wool after the acid bath is 5.5%, with 7.5% being a critical level.
Surfactants are often added to the acid bath to aid in wetting and so spread the acid evenly. This helps to minimise fibre damage due to localised concentration of acid. Whilst they have been shown to give some degree of protection to the wool fibre, they may not increase acid penetration into the VM.
After acid soaking, the squeezed/centrifuged wool is dried at <70°C and then baked at 90-120°C. The drying process concentrates the acid on the VM. When the acid concentration is high enough, the cellulose is converted to brittle hydrocellulose (charcoal).
The wool then proceeds through crushers and de-dusters or shakers where the hydrocellulose/charcoal material is firstly crushed and then shaken out of the wool. The wool then passes into an alkaline bath, usually of soda ash, where any residual acid in the wool is neutralised. The wool is then rinsed, sometimes bleached and then dried.

## Slide 3
Source: ADM Group Ltd.
Notes: This slide, courtesy of ADM Group Ltd., demonstrates the stages involved in the carbonising process. In this case the process includes a double baking and crushing/dedusting operation for maximum removal of charcoal from high VM wools.

## Slide 4: Parameters to monitor and control
Acid content
Moisture content of wool entering dryer
Time and temperature of baking
Crusher and deduster settings
Neutralising sequence, pH of wool
Alkali solubility
Colour
Tensile strength
Notes: There are a number of parameters that should be monitored and controlled in the carbonising process.
Acid content of the wool should not be too high as excessive damage will occur.
Moisture content of the wool entering the dryer should be as low as possible to reduce energy costs and minimise the acid content on the wool.
Time and temperature of baking is critical. Too low a baking time or temperature will lead to ineffective embrittlement of the VM. Too long a time or temperature can result in excessive fibre damage and yellowing.
Crusher and deduster settings need to be controlled to prevent undue loss of fibre due to breakage.
Neutralising should be controlled to ensure the finished wool has a neutral pH.
Alkali solubility is a commonly used test to determine the degree of fibre damage.
Colour of the carbonised wool is often adjusted by the use of a bleach bath after neutralisation.
Tensile strength of the carbonised wool is important. A significant reduction in strength can lead to downstream processing problems and poor wear performance.

## Slide 5: Potential Problems
Poor control may cause loss of fibre strength
    Acid concentration
    Drying
    Baking
    Crushing stage
Fibre loss
    Debris removed from the de-duster may contain excessive fibre
Yellowing
    carbonising may yellow the wool
    bleaching
Notes: A number of factors can lead to fibre damage occurring during the carbonising process.
i) Poor control in any of the following can contribute to the loss of tensile strength in the fibres (weakening of the fibres):
a) Acid concentration: Too concentrated an acid or too long an immersion time in the acid bath can result in lasting fibre damage. Dilute acid penetrates easily into wool and attacks the intercellular material causing damage which results in lower fibre strength.
(b) Over drying: Drying the acid soaked wool at too high a temperature may cause the acid droplets to spot concentrate on the wool fibre causing localised damage. This damage may result in loss of fibre strength and extensibility.
(c) Baking: Too high a temperature in the baking stage can result in excessive hydrolysis and yellowing of the wool fibre.
(d) Crushing stage: During this stage the fibres can be damaged mechanically by becoming trapped between burrs and the fluted rollers of the burr-crushers..
ii) Fibre loss is also reported during the carbonising process, the debris removed from the de-duster can contain an appreciable quantity of fibre.
iii) Yellowing of the fibres takes place during the carbonising process and to overcome this mills often apply a mild bleach to the wool. This bleaching process, if not correctly managed can also cause damage to the wool and subsequently loss of fibre strength.

## Slide 6
Wool entering the acid bowl
The acidising bowl

## Slide 7
Carbonised wool
Combined flat bred and drum baking oven ex Fleissner

## Slide 8
Fleissner crushing roller set
Crushing rollers in situ

## Slide 9
End of Summary Slides
Close Window