## Slide 1
Topic 4
Aqueous Wool Scouring & Detergents
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Mixing and separating of liquids
Oil and water do not mix
Shaking them forms an emulsion (this may be unstable, liquids will eventually separate)
The less dense liquid (oil) rises to the top
Interface
Less dense liquid (oil)
Denser liquid (water)

## Slide 3: Nature of the interface
The boundary between the two liquids or around droplets of liquids is called the interface
If the tension at the interface is low, the liquids mix easily
If the tension at the interface is high the liquids will not mix – they remain separate
In wool scouring a soap or detergent is used to wet the fibre, detach the grease and create interfacial tension around droplets of grease (so the grease is not redeposited on the fibre)

## Slide 4: Nature of a detergent
Detergents are cleansing agents containing surface acting agents (or surfactants)
A surfactant can alter the interfacial tension between water and other liquids or solids
The surfactant
  spreads water over the complete surface of the fibres,
  loosens and removes grease and dirt, and
  suspends the molecules of grease and dirt in globules so they can be rinsed away.

## Slide 5: Structure of surfactant molecules
Surfactant molecules are like tadpoles (head and tail)
The long tail is hydrophobic (an affinity for oil and grease, and repels water)
The compact ‘head’ is hydrophilic (an affinity for water and repelled by oil and grease)
Water-seeking head
Grease-seeking tail

## Slide 6: Types of surfactants (1)
CATIONIC: head carries a positive charge
ANIONIC: surfactant carries a negative charge, concentrated in its head
_
Na+
+
Cl-

## Slide 7: Types of surfactants (2)
AMPHOTERIC: molecules carries positive and negative charge (may be anion or cation depending on pH of solution)
NON-IONIC: molecule not charged, but hydrophilic group (polyethylene oxide) usually attached
+
-

## Slide 8: Sequence of grease removal
Detergent is added to water and becomes evenly distributed through it
Detergent completely surrounds fibre, with oil-seeking end of molecule attaching to grease
Surfactant molecules get under the film of grease and dirt; grease rolls up into droplets
Grease droplet is detached from fibre, surrounded by layer of surfactant molecules
Water-seeking end of surfactant molecules point outwards into water, so grease droplet less likely to be re-deposited
Agitation by the rakes and the liquor flow floats grease droplets away from fibre

## Slide 9: Sequence of grease removal
Surfactant molecules
Grease on fibre
Grease droplet removed from fibre
Grease droplet
Clean wool

## Slide 10: Separation of grease droplet

## Slide 11: Particles of dirt are removed by:
Agitation of the liquor
Washing away with the grease droplets
Mutual repulsion between fibre and dirt

## Slide 12: Stability of the emulsion
If the detergent falls below a minimum level:
The amount of woolgrease removed drops;
Droplets of emulsified grease my re-deposit on the fibre
Grease droplets may combine to form large masses
This will break down the emulsion and form a layer of grease on the surface of the liquor
Emulsion stability is maintained by having sufficient detergent present in the liquor to surround the surfaces of all fibres

## Slide 13: Synthetic scouring detergents
Synthetic non-ionic detergents of alkylphenol / ethylene oxide type mostly used today
Water seeking head made up of ethylene oxide units
Size and number of hydrocarbon units in tail determines how well it seeks oil
Usually 8-10 EO units make good scouring detergent
O – ( CH2 – CH2 – O)n H
C9H19
nonyl group
The ‘tail’ or oil-seeking end of the detergent molecule
phenol group
poly(ethylene oxide) group
(The ‘head’ or water-seeking end of the molecule)

## Slide 14: Detergent level
The amount of detergent required depends on wool type (e.g. fleece wool versus dag blend)
Excess detergent does not give better scouring, also leaves deposit on fibres
Need to check that:
  Detergent added to bowls regularly
  Detergent tank doesn’t empty
  Stopcocks on pump are open
  Pump mechanism is unblocked
  Pump motor in good working order

## Slide 15: Oxidised grease
Wool grease is of two types – unoxidised and oxidised
During wool growth grease near tip of fibres becomes chemically degraded (oxidised)
Newer grease on fibres at base of staple is unoxidised
Oxidised grease is harder to remove
Residual grease left on fibre after scouring is mostly oxidised grease

## Slide 16: Removing dirt
Dirt harder to remove than woolgrease
Requires vigorous mechanical action
Squeezing important – pressure sufficient to ensure
  maximum dirt and grease removal,
  minimum dirty liquor carried to next bowl
Most dirt and impurities removed in first bowl
After last bowl, virtually all impurities removed except for 0.1 – 0.4% grease
Dirt on scoured wool causes problems later

## Slide 17: Entanglement and felting
Scouring provides right conditions for entanglement and felting to occur: (1) differential frictional effect, (2) moisture, (3) agitation

## Slide 18: Squeezing efficiency
Very important after first scouring bowl
Also after final rinse bowl for efficient drying
Squeeze roller efficiency determines amount of liquor (regain) on wool before drying
Factors controlling squeezing efficiency:
  Roller lapping in poor state (needs replacing?)
  Squeeze pressure too low
  Wool feed uneven
  Rollers bowing under excess pressure

## Slide 19: Roller lapping
Different lapping combinations affect amount of liquor squeezed out (hence dirt/grease removal)
Length of life varies with type
Must not contaminate wool with loose fibres
Overall cost important, including amount of subsequent wool drying required
Maintenance important to avoid costly stoppages
Various types (vary in cost and durability):
  Wool top over base rope foundation
  Nylon tow over wool top and base rope
  Wool/nylon or nylon rope

## Slide 20
End of Summary Slides
Close Window