## Slide 1: Wool Scouring systems
Topic 7
Notes: Mr Chairman
Members of the Board
Ladies and Gentlemen

## Slide 2: Wool scouring systems
Solvent scouring
Aqueous scouring methods:
    Soap and soda scouring (obsolete)
    Duhamel process (suint scouring) – not commercial
    WRONZ Comprehensive Scouring System (basis of modern coarse/carpet wool scouring)
    Lo-Flo, leading to…
    Siroscour (basis of modern fine wool scouring)

## Slide 3: Contaminant removal in solvent scouring
Woolgrease – readily dissolved in organic non-polar solvents
Suint (or sweat) – insoluble in organic solvents (soluble in water)
Dirt – insoluble, removed by sedimentation

## Slide 4: Pros and Cons of Solvent Scouring
As only woolgrease removed, wool needs further treatment (emulsion scouring)
Effluent is less polluted
Wool quality better because less entanglement
Care need in choosing safe solvents
Some solvent lost through evaporation
More costly system to establish and operate

## Slide 5: Contaminant removal in aqueous scouring
Suint being water-soluble is easily removed
Woolgrease is insoluble in water, requires emulsification or saponification
Surface soiling (dust, VM etc.) is removed by agitation in liquor and squeezing

## Slide 6: WRONZ Comprehensive Scouring System
Counterflow method: wool flows in one direction through the bowls, liquor flows in reverse direction
Scour bowl temperatures – 60-70oC; Final rinse bowl – 55oC
3 scouring bowls, 3 rinse bowls

## Slide 7: Benefits of WRONZ system
Increased woolgrease recovery
Heat exchanges recover heat from effluent
Effective effluent treatment
Mini-bowls give reduced water utilisation, also
Less energy used
Longer scouring runs before cleaning
Increased production
Improved quality and efficiency

## Slide 8: The Advantages of Mini-Bowls
1/3 length of conventional bowls (scouring efficiency does not depend on immersion time)
Wool immersed for 1/6 of usual time
Wool given greater agitation, but does not cause felting (short immersion time)
Mat thickness about half that of conventional bowls
Wool completely immersed by perforated dunker roller

## Slide 9: The Mini-Bowl
Source: Andar Holdings Ltd (a)

## Slide 10: Siroscour system
This is a more complex scouring system, developed in Australia specifically for fine wools
Incorporates an initial ‘suint bowl’ to remove dirt without the grease
Two stages or three stages, depending on yield of wool

## Slide 11: Siroscour – effluent treatment

## Slide 12
End of Summary Slides
Close Window